## Slide 1: Relation between the newly derived ECR criterion and the QUENCH LOCA test results
H.G. Sonnenburg, GRS
19th International QUENCH Workshop
Karlsruhe Institute of Technology Campus North, H.-von-Helmholtz-Platz 1, 76344 Egg.-Leopoldshafen November 19-21, 2013

## Slide 2: Overview
  Phenomena During LOCA Transient
  Development of a New ECR-Criterion
  KIT QUENCH LOCA Tests for Safety Assessment

## Slide 3
Time
Temperature at burst
~800°C
Oxidation
secondary Hydriding
Temperature
Thermal shock
Quenching fluid shakes the broken fuel rod
135°C
Depletion phenomenon seen in HALDEN and STUDSVIK
Depletion phenomenon seen in
STUDSVIK by shaking the rod
Depletion of ~ 0.1 m fuel if: a) cladding burst
b) high burn-up
Depletion of ~ 1.5 m fuel if:
a) cladding is already burst
b) no residual ductility left
c) high burn-up
Phenomena during LOCA

## Slide 4: Present Regulatory Limit for LOCA (international)
Maintain coolable geometry
Keep fuel inside cladding
Prevent breaking cladding
Maintain residual ductility in cladding
Limit oxidation
(Limit hydriding - not considered yet)
  Oxidation limits
    Keep equivalent cladding reacted below 17%  ECR < 17%
    Keep oxidation temperature below 1200°C  PCT < 1200°C
    Keep hydriding below ???  ECR=ECR(H)

## Slide 5: Need for new ECR Criterion
Proposal from U.S.NRC derived from Ring Compression Tests (offset strain >2%)
Proposed criterion relies on a few tests which fall close to zero ductility
17% ECR
Secondary Hydriding
during
LOCA ?

## Slide 6: Alternative Approach to Derive the ECR Criterion

## Slide 7: Finite Element Method
0
100
200
300
400
500
600
700
0
1
2
3
4
Load (N)
Displacement (mm)
Ring Compression Test (ANL)
  ECR  total O-up-take
  Leistikov  ZrO-, ZrO2-layers  O in prior-b-layer
  MATPRO  E(O), n(O), K(O)  sYield(O)
  Finite Element (ADINA): localization of maximum equivalent stress  sBurst(e)
ADINA
sBurst(e)

## Slide 8: Burst Stresses from 65 RCTs (room temperature) out of 102 RCTs

## Slide 9: Stress Ratio R = Function (Material, TRCT, ECR, ppm H)
Zero-ductility: R = 1
ECR = 17%

## Slide 10: Linear Regression for Stress Ratio R
 | Estimate | Std. Error | p-value
 | 1.62 | 3.5 . 10-2 | < 2 . 10-16
 | 1.8 . 10-3 | 3.6 . 10-4 | 1.6 . 10-6
(Zry-4, ZIRLO) | -4.2 . 10-2 | 3.0 . 10-3 | < 2 . 10-16
(M5) | -3.7 . 10-2 | 2.8 . 10-3 | 4.1 . 10-9
(Zry-4 HBR) | -6.5 . 10-2 | 4.2 . 10-3 | < 2 . 10-16
 | -1.05 . 10-4 | 1.7 . 10-5 | 1.0 . 10-8
 | -1.08 . 10-4 | 1.7 . 10-5 | 4.1 . 10-9
 | Estimate | Std. Error | p-value
 | 1.62 | 3.5 . 10-2 | < 2 . 10-16
 | 1.8 . 10-3 | 3.6 . 10-4 | 1.6 . 10-6
 | -4.2 . 10-2 | 3.0 . 10-3 | < 2 . 10-16
 | -3.7 . 10-2 | 2.8 . 10-3 | 4.1 . 10-9
 | -6.5 . 10-2 | 4.2 . 10-3 | < 2 . 10-16
 | -1.05 . 10-4 | 1.7 . 10-5 | 1.0 . 10-8
 | -1.08 . 10-4 | 1.7 . 10-5 | 4.1 . 10-9
based on 102 RCTs

## Slide 11
Zero-Ductility
ECR in %
H in wppm
secondary hydriding
during
LOCA ?

## Slide 12: Conservatism of ECRR=1
  ECRR=1  Burst stress at yield stress level
  Accuracy of burst stress is 20%
  Yield stress ranges from 500 MPa to 900 MPa (MATPRO)
  Thermo-elasticity: Estimated stress level for thermal shock (Quenching DT 800°C  135°C)
  ECRR=1 implies huge conservatism against breaking of fuel rods

## Slide 13: Prototypic Fuel Rod Bundle Tests for Safety Assessment
obsolete 17% ECR limit
ECR (%)
Oxidation/Hydriding inacceptable
Oxidation/Hydriding acceptable
Expected Prototypic Bundle Tests at KIT
ECRR=1
OCZL#19
ECRR>1
ECRR<1

## Slide 14: Conclusion
  Fuel rod behaviour under LOCA can be assessed including hydriding / oxidation near burst opening even at high H content
  New criterion: ECRR=1 prevents
  KIT bundle tests (QUENCH LOCA test) provide combination of hydriding and oxidation near burst opening
  Safety assessment  Comparison between H / ECR and ECRR=1