## Slide 1
First Results of Neutron Radiography and Tomography of QUENCH-L0 cladding tubes Mirco Grosse, Camille Goulet

## Slide 2: Content
Neutron radiography
Secondary hydriding
Experiments
Results
- Radiography
- Tomography
Conclusions

## Slide 3: Neutron radiography
GKSS Geesthacht 1991
X-ray radiography
neutron radiography

## Slide 4
Neutron transmission:
Total macroscopic neutron cross section:
N: number density of the isotope
σ: microscopic neutron cross section
Neutron radiography

## Slide 5: Neutron radiography
System Zr - H

## Slide 6: Neutron radiography
Calibration

## Slide 7: Secondary hydriding
M. Billone et al. NUREG/CR-6967/ANL-07/04

## Slide 8: Experiments
ICON facility (SINQ, PSI Villigen, CH)
13.-16.08.2010 (radiography)
09.-17.09.2010 (tomography)
Illumination time per image: 300 s (radiography)
625 x 90 s (tomography)
Spatial resolution: ~ 23 µm

## Slide 9: Radiography, rod 15 (pi = 3 bar)
Z=700mm
Z=1120mm
Σ = 0.215,
Is in the range measured for not- oxidized Zry-4
(Σ = 0.197 .. 0.216)

## Slide 10: Radiography, rod 03 (pi = 55 bar, Δt = 104 s)

## Slide 11: Radiography, rod 03 (pi = 55 bar, Δt = 104 s)
rod rotated by 90°

## Slide 12: Radiography, rod 06 (pi = 35 bar, Δt = 93 s)

## Slide 13: Radiography, rod 08 (pi = 50 bar, Δt = 101 s)

## Slide 14: Radiography, rod 10 (pi = 45 bar, Δt = 49 s)

## Slide 15: Radiography, rod 17 (pi = 40 bar, Δt = 71 s)

## Slide 16: Tomography, rod 01 (pi = 50 bar, Δt = 112 s)
xH = 1330 wppm

## Slide 17: Tomography, rod 01 (pi = 50 bar, Δt = 112 s)

## Slide 18: Tomography, rod 03 (pi = 55 bar, Δt = 104 s)
xH = 1300 wppm

## Slide 19: Tomography, rod 05 (pi = 40 bar, Δt = 93 s)
xH = 1060 wppm

## Slide 20: Summary and Conclusions
Secondary hydriding was investigated by means of neutron radiography and tomography.
The hydrogen distribution is not symmetric.
The extension of the hydrided zone seems to depend on the time between bursting and quenching.
Maximal hydrogen concentrations of ~1300 ppm was determined (preliminary results).
No influence of inner pressure or crack length is obvious.

## Slide 21
Thanks
The QUENCH-LOCA tests and pre-test investigations are sponsored by VGB
KIT:
The QUENCH team, particularly J. Moch und C. Roessger
PSI:
A. Kaestner
Thanks for your attention,
questions?