## Slide 1
Pre-EV1 experiment
A.P. Alexandrov Research Institute of Technology
ISTC EVAN Project
# 3345
Presented by S. Bechta
1st EVAN meeting

## Slide 2: Contents
Test objectives
Basic test conditions
Induction furnace schematics
Optimization of the gas flow in the furnace
Gas-aerosol system schematics
Test procedure
Experimental results
Posttest analysis
Conclusions

## Slide 3
Test operation of the gas-aerosol system and the furnace
Determine optimal content of the oxidant in the gas mixture
Evaluate melt oxidation kinetics
Determine melt evaporation rate at different melt oxidation indexes
Test objectives

## Slide 4
Melt mass: 1600 g
Initial melt composition, mass.%:UO2-74.1; ZrO2-19.7; Zr-6.2
Initial corium oxidation index: С-70
U/Zr = 1.2
No fission product simulants
Pretest conditions correspond to the main experiment:
Melt
Above-melt atmosphere
High-purity Ar during the molten pool formation and at stationary regimes
Ar flow-rate 10 l/min
The same flow rate of Ar/O2 mixture with a volume fraction up to 20 vol.% in oxidation transients
Basic test conditions

## Slide 5
1 – Main aerosol line
2 – Furnace lid
3 – Quartz tube
4 – Inductor
5 – Melt
6 – Cold crucible
7 – Bottom calorimeter
8 – Cold crucible manifold
9 – Pyrometer shaft
Induction furnace schematics
To reduce transport losses the molten pool was raised to the crucible top (minimal distance from the molten pool to the crucible edge is 25 mm)
Pyrometer shaft was temporally lowered for precise temperature measurements
Gas was supplied via the crucible manifold
1
2
3
4
5
6
7
8
9

## Slide 6
Final geometry: Temperature and velocity vectors
Q = 10 l/min, Ar/O2=80:20;
Minimal aerosol deposition on the furnace lid
Maximal aerosol holdup by the carrier gas
Optimization of the gas flow in the furnace

## Slide 7
Gas-aerosol system schematics
1 – Argon and oxygen tanks; 2 –Bronkhorst flow rate regulators; 3 – Gas mixing chamber; 4 – Oxygen sensor; 5 – IMCC furnace; 6 – Medium area filter (MAF); 7 – Analytical filter (AAF); 8 – Bubblers; 9- Flowmeter; 10 - Pressure meter, 11 – Vacuum pump.
Ar and O2 mixing unit was used for the oxidant supply to the furnace
Electrochemical sensors were used for online control of oxygen balance
The bubblers contained potassium hydroxide and persulphate solutions for Ru absorption

## Slide 8
Test procedure
Regimes 1, 2, 4, 5, 7- stationary
Regimes 3, 6 – transition (oxidation in progress)

## Slide 9
Experimental results (1)
Tm- pyrometer indications; Ia – anode current; Ua- plate voltage;
1-7 Time intervals of aerosol sampling to the AAF and MAF filters
Anode current and voltage dynamics. Pyrometer indications

## Slide 10
2565
2545
2630
2655
2700
Experimental results (2)
Melt surface temperatures at different stationary regimes

## Slide 11
Regime parameters
Regimes 1, 2, 4, 5, 7- stationary
Regimes 3, 6 – transition (oxidation in progress).
Experimental results (3)

## Slide 12
Aerosols from the crucible quartz tube
Aerosols from sections
Aerosol deposition on furnace components
Aerosols from the lid
Experimental results (4)

## Slide 13
  Posttest analysis (1)
Imbalance +50.4 g indicates that during the experiment not only metallic zirconium got oxidized; also a part of U+4 was oxidized to U+6
Aerosol mass on the filters is much smaller than the mass of aerosol transport loss. The transport losses are taken into account in calculations of mass release rate
Material balance

## Slide 14
Admixtures and О from the residue
Average sample of aerosols collected from crucible sections, lid and quartz tube
Uranium content in the melt decreased due to the evaporation
Aerosol mass composition – uranium oxides (IV, VI) with zirconium oxide admixtures
Stoichiometry of uranium oxides in corium is calculated – UO2.08 while in aerosols - UO2.37
  Posttest analysis (2)
XRF and chemical analysis

## Slide 15
– mass of total aerosols collected in the furnace, mg;
– mass of aerosol deposits on the MAF, mg;
– mass of aerosol deposits on the AAF, mg;
- melt surface area, 39.6 cm2.
– time of sampling to the AAF, h;
  Posttest analysis (3)
Aerosol release rates (1)

## Slide 16
Aerosol release rates are very sensitive to the temperature
  Posttest analysis (4)
Aerosol release rates (2)

## Slide 17
Oxygen absorption rate
1st oxidation period:
9.3 (±0.3) mg О2/с
2nd oxidation period:
7.3 (±0.2) mg О2/с
  Posttest analysis (5)
Evolution of the melt oxidation
Oxidation index
Oxygen absorption mass

## Slide 18
Conclusions
20 % vol. oxidant concentration in the gas mixture has been chosen for the main experiment; it ensures the accident-free experimental procedure
Reliable performance of the furnace and all system has been demonstrated. However aerosol transport losses are significant
It has been established that the melt oxidation rate is not sensitive to the oxidation index, i.e. free zirconium concentration (oxygen starvation regime)
Data on aerosol mass release rate at different temperatures and oxidation indexes have been measured