## Slide 1: Main results of the completed ISTC project #833.2. “Study of corium melt interaction with NPP reactor vessel steel” (METCOR-2) and status of the ISTC project #3592 (METCOR-P)
Presented by S. Bechta
11th CEG-SAM meting
Dresden, Germany
March 7-9, 2007
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
METCOR project:
General information
Project meetings
Experimental matrixes
Experimental methodology
Tests with suboxidized corium
Tests with oxidized corium
Reporting
Publications
Conclusions
METCOR-P project:
General information
Experimental matrix for the METCOR-P project
Interaction at vertically positioned interface
Interaction at molten corium oxidation transients
Interaction of molten corium with European vessel steel
Short-term plans

## Slide 3: METCOR project general information
Qualification and quantification of physicochemical phenomena of corium melt interactions with reactor vessel steel
Experimental data application:
Analysis of in-vessel corium retention (IVR)
Project objectives:

## Slide 4: METCOR project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatome ANP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZR, Germany
FORTUM, Finland

## Slide 5: Meetings of METCOR.2 projects
▼ 1st meeting of the Steering Committee, 3 October 2002, Karlsruhe, Germany
▼ 2nd meeting of the Steering Committee, 29 January 2003, Aix-en-Provence, France
▼ 3rd meeting of the Steering Committee, 16 September 2003, St. Petersburg, Russia
▼ 4th meeting of the Steering Committee, 10 February 2004, Paris, France
▼ 5th meeting of the Steering Committee, 14 September 2004, Dimitrovgrad, Russia
▼ 6th meeting of the Steering Committee, 12 July 2005, St. Petersburg, Russia
▼ 7th meeting of the Steering Committee, 14 June 2006, St. Petersburg, Russia
Last project meeting will be held in SPb, May 31, 2007

## Slide 6: Experimental matrix of METCOR
Phase 1: Tests with fully oxidized melts

## Slide 7: Experimental matrix of METCOR
Phase 2: Tests with suboxidized corium and tests with oxidized corium in steam

## Slide 8: Experimental methodology: Furnace section
1 – pyrometer shaft; 2 – cover; 3, 18, 19 – electromagnetic screens; 4 – quartz tube; 5 – crucible sections; 6 – inductor; 7 –melt; 8 – acoustic defect; 9 – fused ZrO2 grains; 10 – ZrO2 powder insulation; 11 – vessel steel specimen; 12 – top specimen calorimeter; 13 – bottom specimen calorimeter; 14 – kaolin wool insulation; 15 –ultrasonic sensor; 16 – thermocouples; 17 – crust; 20 – cylindrical support of the specimen
Technology of the induction melting in a cold crucible
Atmosphere: air, steam, argon
Long-term expositions in a stationary regime
On-line measurements:
specimen temperature
melt surface temperature
specimen ablation depth
electric parameters
power deposition in the furnace components

## Slide 9: Experimental methodology: Posttest analyses
Calculation of the whole electromagnetic system
Power deposition in the melt and its electric resistivity are determined Measured electric parameters of the system and power deposited into the furnace components are used in the numeric modeling
Integrated calculation of the electromagnetic system and melt thermohydrodynamics
Radial heat flux distribution in the specimen top is determined. Calculations of the whole electromagnetic system and boundary conditions on the crucible and specimen surfaces are used
Calculation of the specimen temperature conditions
Results of previous calculations, boundary conditions on the crucible surface and specimen calorimeters are used. The adequate agreement between calculations and thermocouple measurements is achieved by varying heat flux into the specimen and thermal resistance of the specimen side insulation
Physicochemical analysis of the ingot, specimen and interaction zone
XRF; SEM/EDX; optical microscopy; chemical analyses. Elemental and mass balances, initial and final compositions of the system and its components are determined

## Slide 10: Tests with oxidized corium
Elemental phase composition
Element/ Phase 1 Phase 2
oxide w% w%
U M - 83.78
Zr K - 0.243
Fe K 70.00 3.85
O 29.00 12.11
UO2 - 95.00
ZrO2 0.30 0.40
Fe2O3 99.70 4.6
Identified phenomenon of steel corrosion: surface oxidation of vessel steel; the rate of oxidation is controlled by Fe+ diffusion through the corrosion layer; corrosion layer thickness is sensitive to the corium composition and heat flux
Example of corrosion and coexisting layers in MC-2
steel
oxidic
layers
corium

## Slide 11: Tests with oxidized corium (continued)
Corrosion rates in air and in steam are similar
Decrease of corrosion rate following increase of iron oxides content in corium melt
Intensification of corrosion after reaching eutectic temperature of the interface between corrosion layer and corium
Experimental data in form of Arrhenius plot
16UO2-64ZrO2-20FeO
Air
56UO2-24ZrO2-20FeO
70UO2-30ZrO2
Steam
56UO2-24ZrO2-20FeO

## Slide 12
Tests with oxidized corium (continued) Corrosion model: modified Tamman equation for:
UO2+x- ZrO2 - FeOy corium
FeOy=20…30%, U/Zr=0.11…1.05
UO2+x- ZrO2 (С-100 corium),
U/Zr  1.0
Ts=720…1050oC
q =0.30…1.15 MW/m2
Ts = 1035…1235oC
q = 0.95…1.1MW/m2
W – mm/h; q - MW/m2 ; T - K
Before eutectic melting of corrosion layer

## Slide 13: Tests with suboxidized corium
Identified phenomenon of steel corrosion: U, Zr, O partitioning (similar to MASCA) and partial eutectic melting (dissolution) of the vessel steel , IZ depth is limited by the position of isotherm 1090 oC
Axial sections of specimens
EDX images of Interaction Zone
МС6
МС7
МС8
МС9
Shrinkage cavity
Chip
Acoustic defect
10 µm
500 µm
100 µm
Teut~1090ºC (DTA)
DTA of IZ in MC-8

## Slide 14: Tests with suboxidized corium (continued)
Model of ablation kinetics
2 main periods of ablation: incubation and fast ablation
Incubation period: - oxidic melt tinc=8000+200 (70-Cn), s 30  Cn  70 - metallic melt tinc=0
fast ablation resulting in saturation
, mm/s
Tint – current temperature of steel surface 1090  Тint  1440C
TB – final temperature of steel surface after interaction termination (1090 oC for reactor application)

## Slide 15: Reporting

## Slide 16: METCOR papers
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, D.B. Lopukh, Yu.B. Petrov, A.Yu. Petchenkov, I.V. Kulagin, V.S. Granovsky, S.V. Kovtunova, V.V. Martinov, V.V. Gusarov. Experimental studies of oxidic molten corium – vessel steel interaction // Nucl. Eng. Design 210 (2001) 193-224.
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer, G. Cognet, O. Kymäläinen. New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel //Proceedings of ICAPP’04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4114
S.V. Bechta, V. B. Khabensky, V.S. Granovsky, E.V. Kroushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, L.P. Mezentseva, Yu.B. Petrov, D.B. Lopukh, M. Fischer, D. Bottomley, W. Tromm, M. Barrachin, E. Altstadt, P. Piluso, F. Fichot, S. Hellmann, F Defoort. CORPHAD and METCOR ISTC projects / Proc. of the first European Review Meeting on Severe Accident Research (ERMSAR-2005), Aix-en-Provence, France, 14-16 November 2005
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky, D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm, D. Bottomley, H. Tuomisto. Corrosion of vessel steel during its interaction with molten corium. Part 1: Experimental // NED, vol.236, 2006, pp 1810-1829

## Slide 17: METCOR papers (continued)
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky,D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm, D. Bottomley, H. Tuomisto. Corrosion of vessel steel during its interaction with molten corium. Part 2: Model development // NED, vol.236, 2006, issue 13, pp 1362-1370,
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer, P. Piluso, A. Miassoedov, E. Altstadt, H.G. Willschütz, F. Fichot. Experimental Study of Interactions Between Suboxidized Corium and Reactor Vessel Steel // Proceedings of ICAPP’06, Reno, NV USA, June 4-8, 2006, Paper 6054
In preparation (draft titles):
Interactions of oxidized corium melt with vessel steel of VVER reactor (Analysis of the tests done in air and steam )
Corrosion of VVER vessel steel in conditions of in-vessel corium melt retention (Summarized results of the 1st and 2nd phases of METCOR, examples of plant application)

## Slide 18: Conclusions
VVER steel corrosion mechanisms have been clarified for different melt compositions and interaction conditions
Simple correlations have been developed to be used in the IVR analyses
Note:
METCOR project did not examine the full range of IVR conditions, in particular, vessel steel composition and surface spatial orientation

## Slide 19: METCOR-P project
Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel (#3592 METCOR-P)
Work plan of ISTC proposal has been prepared in the end of METCOR and approved by the project collaborators
Actuality and principle technical content of METCOR-P have been discussed during:
  7th meeting of the METCOR Steering Committee, 14 June 2006, St. Petersburg, Russia
  10th CEG-SAM meeting, Kurchatov-City, Republic of Kazakhstan, September 5-8, 2006
The project was approved for funding during ISTC GB#41 in December 2006
Contract agreement between ISTC and NITI is expected to be signed in May 2007

## Slide 20: METCOR-P project general information
IRSN,
France
KAERI,
Korea
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZD, Germany
FORTUM, Finland
Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel (#3592 METCOR-P)

## Slide 21
Objectives of METCOR-P project
Qualification and quantification of physicochemical phenomena of corium melt interactions with reactor vessel steel with particular interest to:
Spatial orientation of interaction surface
Corium oxidation transients
Vessel steel composition of European reactors

## Slide 22: Experimental matrix for the METCOR-P project

## Slide 23: Furnace schematics (1)
1 – crucible section;
2– water-cooled pyrometer shaft; 3 - inductor; 4 – vessel steel specimen; 5 – top calorimeter of the specimen; 6 – ultrasonic sensor
7 – K-type thermocouples; 8 - melt;
Convenient specimen position
Applicability of ultrasonic sensor
Interaction at vertically positioned interface
Large pool volume
Possible crust on the surface within pyrometer sighting spot
Complex sealing of furnace volume
+
-

## Slide 24: Furnace schematics (2)
Developed interaction surface
Applicability of ultrasonic sensor
Interaction at vertically positioned interface
Low efficiency of inductor
Shallow molten pool
Complex sealing of inductor
+
-
1 – water-cooled cover;
2 – water-cooled pyrometer shaft; 3 – vessel steel specimen; 4 – calorimeter of the specimen; 5 – ultrasonic sensor
6 –inductor;
7 - melt;
8 – K-type thermocouples;
9 – quartz tube;

## Slide 25: Furnace schematics (3)
Lid
Water cooled screen
Quartz tube
Cold crucible
Melt
Inductor
TC hot junctions
Vessel steel specimen
Bottom calorimeter
Simple design
Tested crucible
High efficiency factor of furnace
Interaction at vertically positioned interface
Not enough space for ultrasonic sensor
+
-

## Slide 26
Interaction at vertically positioned interface
Pre-test DNS of molten pool and vessel specimen

## Slide 27
Principle test procedure
Furnace schematics corresponds to MC 11 with steam
Specimen surface is positioned horizontally
С-30 melt is prepared in the inert atmosphere
Melt is exposed during 10 hours in order to form the interaction zone
Steam is supplied into the furnace after ablation saturation
Evolution of interaction zone is estimated by thermocouple readings, ultrasonic sounding and post test analysis
Interaction at molten corium oxidation transients
Vessel steel ablation during molten corium oxidation by steam (1)

## Slide 28
Interaction at molten corium oxidation transients
Vessel steel ablation during molten corium oxidation by steam (2)
 | U | Zr | Fe | Cr
mass.% | 25.6 | 4.8 | 58.3 | 2.3
mol.% | 6.1 | 3.0 | 56.7 | 2.5
 | Ni | Mn | Si | O
mass.% | 0.7 | 0.5 | 0.3 | 7.5
mol.% | 0.7 | 0.5 | 0.6 | 26.8
Experiment MC6
Interaction zone approximately corresponds to MC 6
What happened with IZ after oxidation?
Heat release?
Further corrosion?

## Slide 29: Vessel steel ablation during molten corium oxidation by steam (3)
Furnace schematics in MC-11
System of gas/steam supply and removal
1 – steam vent from the furnace; 2 – steam line; 3 – lid; 4- water-cooled cover; 5 – quartz tube; 6– water-cooled electromagnetic screen; 7 – crucible sections; 8 – inductor; 9 – melt; 10 – acoustic defect; 11 – thermal insulation of the specimen; 12 – top specimen calorimeter; 13 – bottom specimen calorimeter; 14 – US sensor.
1 – tanks with Ar, N2; 2 – steam generator; 3 – heated steam supply line; 4 – quartz tube for steam supply into the furnace; 5 – steam condenser; 6 – condensate collector; 7 – condensate drop catcher; 8 - ejector; 9 – large-area filter (LAF); 10 – silica gel drier; 11 – medium-area filter (MAF); 12 – electrochemical sensors of oxygen and hydrogen; 13 – vacuum receiver; 14 – mass-spectrometer; 15 – weight sensor 16 – hydro lock; 17 – vacuum gas burettes; 18 - medium-area filter (MAF).
Interaction at molten corium oxidation transients

## Slide 30
Interaction at molten corium oxidation transients
Corium surface oxidation influence on the heat fluxes into the vessel (1)
Methodology
Melt-induced thermal loads on the surface of water-cooled probe are determined during oxidation transient. Melt interaction with vessel steel is not examined
Oxidation rate is determined by on-line measurement of the gas flow-rates and compositions

## Slide 31
Interaction at molten corium oxidation transients
Corium surface oxidation influence on the heat fluxes into the vessel (2)
Measurements of sideward heat flux distribution during pool surface oxidation
1 –electromagnetic screen
2 – water-cooled probe
3 – cold crucible
4 –melt
5 – hyperthermocouple of differential type
6 –inductor
7 – bottom calorimeter
1
2
4
3
5
6
7
Calorimetry + calculation of heat flux profile from the measured temperature profile of water

## Slide 32: Interaction of molten corium with European vessel steel
Provisional GEMINI2 calculations of Russian and French steel mixtures with corium by C. Journeau, CEA
Conditions
GEMINI2 + NUCLEA04
no Mn, Mo, V, Cu and S in the database (were replaced by Fe)
MC8 corium (62.1 g U, 18.4g Zr, 16.6g O)
equal corium (97g) and steel (100g) mixtures
Results
Eutectic temperature :
1200 oC for 15Kh2NMFA steel
1100 oC for 16MND5 steel
Difference about 100 oC

## Slide 33: Interaction of molten corium with European vessel steel
Experimental conditions
Repetition of basic METCOR tests with specimens of vessel steel from European reactors
Proposals
Bottom-placed specimen with horizontal surface
Repetition of test conditions of MC 6 and MC 9
16MND5 steel

## Slide 34: Short-term plans
Activities for 1st and 2nd quarter:
  Pre-test calculations
  Design of new IMCC furnace for tests with vertical wall
  Manufacture of furnaces and specimens
  Pre-testing
Conceptual design of a new experimental installations, test procedures and type of European vessel steel will be discussed with collaborators at the METCOR-P project meeting, May 31, St Petersburg