## Slide 1: Progress Report on the ISTC project #3592 “Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel” (METCOR-P)
Presented by S. Bechta
12th CEG-SAM meeting
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
METCOR-P project general information
Objectives
Experimental matrix
Test results:
Test MCP-1
Test MC12
Test MCP-2
Short-term plans

## Slide 3: METCOR-P project general information
IRSN,
France
KAERI,
Korea
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZD, Germany
FORTUM, Finland

## Slide 4: Objectives of METCOR-P project
Interaction characteristics at the vertically positioned interface
Peculiarities of interaction with European vessel steel
Corium melt oxidation transients
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel focused on:

## Slide 5
Experimental matrix for the METCOR-P project
*In accordance with METCOR-P work group decision replaced by MCP2 test with UO2+x– ZrO2 corium in air and horizontal position of interface

## Slide 6: Interaction of molten corium with vertical cylindrical steel specimen: MCP-1 test
Objectives
Study of peculiarities of molten corium interaction with vessel steel at the vertical interface position
Test parameters are similar to MC6 test of METCOR-2:
C-30 corium
15Kh2NMFA vessel steel
Pure argon above the melt
10 h exposition

## Slide 7: Furnace design
1 – Water cooled
screen
2 – Cover
3 – Water-in
4 – Quartz tube
5 – Crucible sections
6 – Specimen
7 – Inductor
8 – Bottom calorimeter
9 – Welded crucible
sections
10 – SS support 11 – Water-out
12 –Electromagnetic
screen
13 – Crucible collector

## Slide 8: TC locations in the specimen
Coordinates of TC hot junctions

## Slide 9: Test procedure
Time, s | Operation mode
0-963 | Furnace deoxygenation by argon flow
963-3550 | Formation and homogenization of the molten pool. Increase of power in the melt to get 1400 oC on the specimen surface
3550-39874 | Keeping constant surface temperature and power extracted by water from the specimen by inductor voltage control
39875-42000 | Heating disconnection, melt solidification and ingot cooling in argon

## Slide 10: Furnace view in the test

## Slide 11: Test results: TC readings
Wrong readings of most thermocouples due to corrosion of wires (not junction!)

## Slide 12: Test results: TC readings (2)
Estimation of IZ progression from TC readings
Different lifetime of TCs in the mushy interaction zone
Not possible to estimate interaction kinetics
Short incubation period (or no incubation)

## Slide 13: Post test examination
Axial sections of ingot
Example of TC location
Corium upper crust is removed
Metal inclusions in corium ingot

## Slide 14: Post test examination (2)
Axial sections of specimen
MCP-1 (90º rotated)
MC 6
Corium
1st layer
2nd layer
Zone of thermal influence
Steel of initial structure
IZ
Steel

## Slide 15: Post test examination (3)
Shape of the boundary between IZ and steel
Initial volume of specimen: 35813 mm3
Volume of uncorroded steel : 25013 mm3
Volume of corroded steel: 10800 mm3

## Slide 16: Post test examination (4)
Temperature profile of the specimen (to be specified)
A – boundary of the thermal influence zone (760 C)
B – 2nd layer boundary (1050-1100 C)
C – 1st layer boundary (~1250 C)
1 – 700 C 5 – 1100 C
2 – 800 C 6 – 1200 C
3 – 900 C 7 – 1300 C
4 – 1000 C 8 – 1400 C
T, oC
90° rotated
Upper surface
bottom

## Slide 17
Higher content of U and Zr in IZ (40-50 and 13-20 mass %) in comparison with МС6 IZ (24 and 5 mass %)
High content of U and Zr in metal inclusion (58 and 24 mass %)
Post test examination (5)
Express XRF and chemical analysis
Average
sample of ingot upper part Cn≈40
Average
sample of
crust
Cn≈48
U=66.5
Zr=20.2
Fe=1.7
Cr=0.06
Ni=0.02
U=66.1
Zr=22.3
Fe=1.0
Cr=0.02
Ni=0.03
U=66.6
Zr=23.2
Fe=1.0
U=64.6
Zr=21.7
Fe=3.5
Cr=0.04
Ni=0.08
U=66.7
Zr=22.3
Fe=5.7
XRF,mass.%
ChA,mass.%
XRF
ChA
U=54.6
Zr=15.9
Fe=28.5
U=57.5
Zr=24.2
Fe=17.8
Cr=0.2
Ni=0.3
U=36.5
Zr=22.1
Fe=47.8
Cr=0.8
Ni=0.5
U=51.7
Zr=13.5
Fe=30.9
Cr=0.6
Ni=0.3
Average
sample of ingot lower part Cn≈32
29-31mm
23mm
25mm
U=66.8
Zr=22.3
Fe=2.1

## Slide 18: Comparison of МС and MASCA tests
Temperature boundary of the IZ final position coincides with its minimum value in MC tests, but it is smaller than in МС6 (at the horizontal interface orientation)
Component concentrations in the IZ are quite different from МС6 and close to MASCA

## Slide 19: MCP-1 concluding remarks*
New method and new IMCC furnace have been developed for studying corium melt/vessel steel interaction at the vertically positioned interface
Disadvantages of the experimental setup:
No US online measurements of corrosion kinetics
Limited pool depth (specimen height) and corium mass
Differences from MC6 with horizontal interface
In conditions:
Higher heat fluxes at similar interface temperatures
b) In results:
Shorter or absent incubation period
Metal inclusion in the corium ingot
Different macro and microstructure and composition of interaction zone (higher U and Zr content in IZ)
Lower temperature, which corresponds to the final position of IZ boundary (like in MC7 and MC9)
*) will be specified after the detailed analysis

## Slide 20: Interaction of molten corium and vessel steel in the oxidizing atmosphere. Tests MC12,MCP-2

## Slide 21: METCOR results for corium UO2+X-ZrO2-FeOY
0.001
0.01
0.1
1
10
0.65
0.75
0.85
0.95
1.05
MC1,2
MC11
МW
m
h
mm
,
q
W
2
T
1000
S
К
0.001
0.01
0.1
1
10
0.65
0.75
0.85
0.95
1.05
МW
m
h
mm
,
q
W
2
,
T
1000
S
1/
К
- air
- steam
Insufficient data in the Ts>1050C domain
No validated corrosion model at Ts>1050C, which can explain a bend in the curve “corrosion rate vs. Ts“

## Slide 22: METCOR results for corium UO2+X - ZrO2 – FeOY (2) Test MC12 (not funded by the ISTC)
Number of experimental points substantially increased
Insensitivity of corrosion rate to the composition of oxidizing atmosphere (steam, air) is confirmed for a wide range of temperatures
Absence of sharp bend in the curve “corrosion rate vs. Ts”

## Slide 23: Interaction zone structure MC12, Ts=1125C, q=1.09 MW/m2 (steam)
Average corrosion layer thickness   0.24 mm
steel
Fe1-xO
corium crust
melt

## Slide 24: Interaction zone (2) microstructure MC12, Ts=1125C
Grain boundary diffusion of corium components through the corrosion layer Fe1-xO is observed
Zone 1
Zone 3

## Slide 25: Interaction zone (3) microstructure MC12, Ts=1125C
Liquid phase exists on the boundary between the corrosion layer and corium

## Slide 26: Interaction zone (4)
h, mm
ТС
Temperature
Possible formation of liquid phase in the multi-component oxidic system within the corrosion layer
concentrations, mol%
Distribution of components

## Slide 27: Corrosion model
Corrosion rate depends on the intensity of diffusion processes in the corrosion layer
Two diffusion processes can be assumed to take place during the corium–steel interaction in the oxidizing atmosphere
 Fe2+ diffusion through the solid layer
 liquid-phase Fe2+ diffusion
The second process prevails at Тs>1050C

## Slide 28
Corium UO2+x – ZrO2 – FeOy
Summary of experimental data
Proposed semi-empirical correlation gives a good experimental data generalization at 1200  Тs  700C; 1.29  q  0.3 MW/m2

## Slide 29: Corium UO2+x – ZrO2 , MC10
Experimental data are insufficient for developing a correlation describing the wide temperature range
Decision on the additional test with corium UO2+x – ZrO2 taken at the first METCOR-P meeting

## Slide 30: Test MCP-2 Corium UO2+x – ZrO2
1 – Water-cooled pyrometer shaft 2 – Water-cooled lid 3 – Water-cooled electromagnetic screen 4 – Quartz tube 5 – Crucible section 6 – Inductor 7 – Melt 8 – Acoustic defect 9 – Molten ZrO2 (fianite) 10 – ZrO2 powder 11 – Vessel steel specimen 12 – Top calorimeter of the specimen 13 – Bottom calorimeter of the specimen 14 – Thermal insulation (mullite cotton) 15 – USS 16 – K-type thermocouples 17 – Crust 18 – Electromagnetic screen (welded crucible sections) 19 – Uncooled electromagnetic screen 20 – Cylindrical support of the specimen
Furnace schematics
Similar to METCOR tests

## Slide 31: TC readings
1
2
3
4
5
6
7
8
9
9 plateaus
Shorter plateaus are explained by a higher corrosion rate caused by Ts growth

## Slide 32: Axial section of the specimen top and profilogram

## Slide 33: Steel specimen corrosion kinetics
posttest measurement
on-line measurement
interpolation of on-line measurements
Time, s
h, mm

## Slide 34: Preliminary results
Not sensitive to the atmosphere composition (steam, air)
No corrosion intensification up to Ts  1350C can be explained by the solid crust maintenance due to the high Tsol  2450 C
Results will be generalized after the posttest analysis

## Slide 35: Short-term plans
Conclude posttest analysis of MCP-1, MCP-2 – Sept. 2007
Make a report of the interaction of corium UO2+x – ZrO2 – FeOy with vessel steel in the oxidizing atmosphere. Test MC12 - Sept. 2007
Make a report of the interaction of corium UO2+x – ZrO2 with with vessel steel in the oxidizing atmosphere. Test MCP-2 - Oct. 2007
Make a report of the interaction of corium С-30 with vessel steel at the vertical position of interaction interface. Test MCP-1 – Nov. 2007
Test MCP- 3 – Interaction of metallic melt of suboxidized corium with vessel steel at the vertical position of interaction interface - Dec. 2007