## Slide 1: Status of PRECOS ISTC project #3813: Phase relation in corium systems
ISTC
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
13th CEG-SAM Meeting

## Slide 2: Contents
  General information
  Project status
  Project focus
  Methodology
  PRECOS test matrix
  Conclusions

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
ISC RAS,
Russia
IHT RAS,
Russia
SPb Electrotechnical State University, Russia

## Slide 4: Status of the project
PRECOS test matrix has been finalized with collaborators at the 6th and 7th CORPHAD project meetings
The project was approved for funding by 44th ISTC MB in December 2007
Work Plan was prepared and sent to ROSATOM Export control in January 2008
The Work Plan was approved by the Export control in the end of February 2008. Export licensing is not necessary for PRECOS
The Work Plan will be distributed after the 13th CEG-SAM. Collaborators will be kindly requested to send letters of the Work Plan consent to ISTC
PRECOS has a chance to start in April 2008
Technical preparations for the project are in progress in NITI, IVTRAN and ISC

## Slide 5: PRECOS project focus
Project objective: Experimental study of phase diagrams of corium mixtures
Data application
  Liquidus and solidus temperatures versus component concentrations
  Temperature-concentration regions of the miscibility gap
  Coordinates of eutectic, dystectic and other characteristic points
  Final solubility in solid solution
Experimental data
  Thermodynamic database optimisation
  Thermodynamic code validation
  Corium behaviour modelling

## Slide 6: Experimental methods of phase diagram studies
Visual polythermal analysis in the cold crucible (VPA IMCC)
Differential thermal analysis (DTA) and differential scanning calorimetry (DSC)
Visual polythermal analysis in the Galakhov microfurnace (GM)
High-temperature microscopy (HTM)
Laser pulse heating (LP)
These methods have been used in the projects: COLOSS, METCOR, CIRMAT, CIT, ENTHALPY, ECOSTAR, OECD/MASCA and CORPHAD

## Slide 7: Methods of posttest analysis
Elemental analysis
 X-ray fluorescence analysis (XRF)
 Chemical analysis (СhA)
Phase analysis
 X-ray diffraction analysis (XRD)
 Energy-dispersive X-ray spectrometry (EDX)
Microstructure analysis
 Optical microscopy
 Scanning electron microscopy (SEM)
Oxygen determination
 Carbothermic reduction

## Slide 8: PRECOS test matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U-Zr-Fe-O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
2 | ZrO2 - FeOy | Air and pO2 contol | liquidus, solidus, solubility limits | 2 | 3
 | UO2 - SiO2 | Argon | liquidus, solidus, solubility limits, eutectic point | 1 | 7
 | CaO - UO2 |  |  | 1 | 7
3 | UO2 – FeO – SiO2 |  | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2 – FeO – CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by French partners (1 system), System (atmosphere) proposed by German partners (1 system), System (atmosphere) proposed by Russian partners (1 system) | 2 | 3
The matrix has been discussed and updated at the 6th and 7th CORPHAD Project meetings

## Slide 9: Quaternary system
U-Zr-Fe-O
U
?
Zr
Fe
O
2670°C
2515°C
Zr
Fe
mol %
20
40
60
80
40
60
80
20
40
60
80
O
20
2520°C
L1+L2
U
Fe
mol %
20
40
60
80
40
60
80
20
40
60
80
O
20
2600°C
L1+L2
CORPHAD DATA
Zr
O
mol %
20
40
60
80
40
60
80
20
40
60
80
U
20
L1+L2
2480°C
2370°C

## Slide 10: Binary oxidic systems (1)
ZrO2-FeOy
mass.%
Fe3O4
20
40
60
80
ZrO2
T, C
1200
2000
2400
2800
1600
1525
1434
Jones T.S.
Kimura Sh.
Muan A.
(1967)
~FeO1.3
mass.%
FeOx
20
40
60
80
ZrO2
T, C
1200
2000
2400
2800
1600
Petrov Yu.B.
Udalov Yu.P.
Slovak J.
Morozov Yu.G.
(2002)
Т, C
mol %
60
40
20
FeO1.5
10-7
10-5
10-3
10-1
101
103
air
Fe0.938O
500
700
900
1100
1300
1500
1700
FeO
80
10-1
101
10-7
10-5
10-3
10-1
103
10-3
105
105
air
Darken L.S. Gurry R.W.
(1945,1946)
FeO (mol %)
1300
1700
2100
2500
80
60
40
20
T, C
FeO
ZrO2
(1332±5)C
2900
Published
ZrO2
FeO
Fe2O3
Fe3O4
?
ss
CORPHAD

## Slide 11: Binary oxidic systems (2)
UO2-SiO2
?
?
Lungu S. (1962)
CORPHAD DATA

## Slide 12: Binary oxidic systems (3)
CaO-UO2
mol.%
CaO
20
40
60
80
UO2
T, C
1000
2200
2800
1600
1300
1900
2500
Alberman K.B.
Blakey R.C.
Anderson J.S.
(1951)
Amato I.
(1966)
Holc J.
Kolar D.
(1986)
Voronov N.M.
Sofronova R.M.
Ivanov O.S.
(1972)
Roche M.F.
Leibowitz L.
Fink J.K.
Backer Jr.
(1993)
300
600
900
1200
1500
1800
2100
2400
2700
3000
T, K
0
0.1
0.2
0.3
0.5
0.7
0.9
1
0.4
0.6
0.8
x (mol)
CaO-UO2
?
?
?

## Slide 13: Ternary oxidic systems (1)
UO2-FeO-SiO2
1300
1700
2100
2500
2900
UO2
20
40
60
80
FeO
FeO, mol %
T, °C
SS
L+SS
L
Allen W.C.
Snow R. B.
(1955)
Bowen N.L.
Schairer J. F.
(1932)
SiO2
FeO
UO2
?
CORPHAD
CORPHAD
Fe2SiO4
Published

## Slide 14: Ternary oxidic systems (2)
UO2-FeO-CaO
1300
1700
2100
2500
2900
UO2
20
40
60
80
FeO
FeO, mol %
T, °C
SS
L+SS
L
!
?
?
?
mol.%
CaO
20
40
60
80
UO2
T, C
1000
2200
2800
1600
1300
1900
2500
CaO
FeO
UO2
?
CORPHAD
Published
Allen W.C.
Snow R. B.
(1955)

## Slide 15: Ternary oxidic systems (3)
ZrO2-FeO-SiO2
FeO (mol %)
1300
1700
2100
2500
80
60
40
20
T, C
FeO
ZrO2
(1332±5)C
2900
Toropov N.A.
Galakhov F.Ya.
(1956)
Rosen E.
Muan A.
(1965)
Published
SiO2
FeO
ZrO2
?
CORPHAD
Allen W.C.
Snow R. B.
(1955)
Bowen N.L.
Schairer J. F.
(1932)
Fe2SiO4

## Slide 16: Ternary oxidic systems (4)
ZrO2-FeO-CaO
FeO (mol %)
1300
1700
2100
2500
80
60
40
20
T, C
FeO
ZrO2
(1332±5)C
2900
Published
Stubican V.C.
Ray S.P.
(1977)
CaO
FeO
ZrO2
?
CORPHAD
Allen W.C.
Snow R. B.
(1955)

## Slide 17: Concluding remarks
PRECOS project is in the initial phase, it can be officially started in the 2nd quarter 2008
Kick-off project meeting will be held in July 2008 in St. Petersburg
Compositions to be studied in 2008 will be discussed at the meeting