## Slide 1: Progress report on the ISTC project #3813: Phase relation in corium systems (PRECOS)
ISTC
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
15th CEG-SAM meeting
March 10-12, 2009, Villigen

## Slide 2: Contents
  General information
  Project objectives
  PRECOS test matrix
  Scope of work in the 2-3 quarters
  Test results:
  - U-Zr-O system
  - UO2-SiO2 system
  - UO2-CaO system
  - ZrO2 - FeOy system
  Conclusions

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
IHT RAS,
Russia
SPb Electrotechnical State University, Russia

## Slide 4: Project objectives
Experimental determination of:
liquidus – solidus temperatures
coordinates of reference points (eutectics, etc.)
solubility limits of a solid solutions
compositions of liquids coexisting in the miscibility gap

## Slide 5: PRECOS test matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U-Zr-Fe-O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
2 | ZrO2 - FeOy | Air and pO2 control | liquidus, solidus, solubility limits | 2 | 3
 | UO2 - SiO2 | Neutral | liquidus, solidus, solubility limits, eutectic point | 1 | 7
 | CaO - UO2 |  |  | 1 | 7
3 | UO2 – FeO – SiO2 |  | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2 – FeO – CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by: - French partners (1 system) German partners (1 system) - Russian partners (1 system) | 2 | 3
At the first meeting with collaborators it was decided for the 1st Task to carry out several tests in the U-ZrO2 section in order to determine tie-line directions and compositions of liquids in the miscibility gap

## Slide 6: Scope of work in quarters 2-3
For LPH study of the U-Zr-O system (U-ZrO2 section) NPO LUCH prepared specimens having the composition specified by collaborators
For analysis of samples of the UO2-SiO2 system the reference samples in a wide range of composition were synthesized in the Galakhov microfurnace to be used for the XRF
For study of the ZrO2-FeOy system specimens were prepared by mechanical mixing of powders, sol-gel method and hydrothermal synthesis
Experiments in the following systems have been performed:
  UO2-SiO2
  UO2-CaO
  ZrO2-FeOy

## Slide 7: Scope of work in quarters 2-3 (2)
PRS experiments were performed on the Rasplav-4 setup with 5.28 MHz frequency
GPRS experiments were performed in the Galakhov microfurnace
HPRS experiments were performed using a high-temperature microscope

## Slide 8
U-Zr-O system (UO2-Zr section)
Hydride technology of U and Zr preparation
Hydration in a high-purity hydrogen in a tungsten crucible
Charging into a tungsten tube
Sintering in pressurized container
Cutting of tungsten tube with a specimen
Electro-erosion cutting into pellets approx. 3 mm high
Surface polishing and ultrasonic cleaning
X-ray, micro and chemical analysis
1
2
3
4
5-6
Specimen synthesis and control of composition

## Slide 9
U-Zr-O system: specimen synthesis (2)
Characteristics of synthesized specimens
      Initial materials UO2 and ZrO2 of >99.85 % purity
50µm

## Slide 10
Test results on UO2-SiO2 system: GPRS 4-13
Experimental objectives
Annealing and quenching in Galakhov microfurnace
UO2 of >99.0 % purity, SiO2 of 99.99% purity, mass of the charge – 150 mg
SEM/EDX in progress
Determine a critical point
Determination of liquidus temperature at high UO2 content

## Slide 11
Test results on UO2-SiO2 system: PRS 2
Experimental objectives
Determine liquidus temperature at high UO2 content
VPA IMCC: Fragment of the experiment thermogram showing melt surface
Charge composition
Mol% 40UO2 + 60SiO2
    Tliq was measured three times: 2100 oC, 2085 and 2060oC  Tliq=2082±30°C

## Slide 12
Test results on UO2-SiO2 system: PRS 2 (2)
Melt surface cooling during VPA IMCC

## Slide 13
Test results on UO2-SiO2 system: PRS 3-1
Experimental objectives
Determine liquidus temperature at high UO2 content
VPA IMCC: Fragment of the experiment thermogram showing melt surface
Charge composition
Mol% 55.8UO2 + 44.2SiO2
    Tliq was measured two times: 2400oC and 2402oC  Tliq=2401±40oC

## Slide 14
Test results on UO2-SiO2 system: PRS 3-1 (2)
Microstructure of quenched sample
UO2 crystals
Phase spinodal decomposition
SQ mol%, 62.5UO2- 37.5SiO2
S. Lungu et al
Primary crystallization is suppressed at temperature below 2070°С
4.17µm
463µm
2.78µm

## Slide 15
Test results on UO2-SiO2 system: PRS 3-2
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured three times: 2487 oC, 2469 and 2492 oC  Tliq=2483±40oC
Charge composition
Mol% 66.7UO2 + 33.3SiO2

## Slide 16
Red lines – Lungu’ diagram
Blue lines and blue points –
results of our previous work
within the CORPHAD project
Green points – results of the
present work (compositions were measured by ChA, XRF in progress)
Test results on UO2-SiO2 system

## Slide 17
Test results on UO2 - CaO system: PRS 4
Experimental objectives
Determine liquidus temperature
Determine final solubility of components in the formed solid solutions
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured three times: 2188oC, 2195 and 2181oC  Tliq=2188±40oC
Charge composition
Mol% 50UO2 + 50CaO

## Slide 18
Test results on UO2 - CaO system: PRS 5
Experimental objectives
Determine liquidus temperature at very high CaO content (indirect determination of CaO melting point)
Charge composition
Mol% 1UO2 + 99CaO
Results
Startup heating was successful
Molten pool was not formed and measurements not taken due to low electric conductivity of the melt
RASPLAV-4 heating current frequency of 5.28MHz is insufficient to maintain the pool of this composition in a molten state
Decision is taken to increase the concentration of uranium oxide in the next experiment

## Slide 19
Test results on UO2 - CaO system: PRS 6-1
Experimental objectives
Determine liquidus temperature at high CaO content
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured two times: 2400oC and 2378oC  Tliq=2389±40oC
Charge composition
Mol% 17.2UO2 + 82.8CaO

## Slide 20
Test results on UO2 - CaO system: PRS 6-2
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured two times: 2583oC and 2537oC  Tliq=2560±50oC
Charge composition
Mol% 10.2UO2 + 89.8CaO

## Slide 21
Test results on UO2 - CaO system
The eutectics composition and solid solutions were synthesized by freezing the melt in close-to equilibrium conditions at slow (7.5 mm/h) and continuous change of crucible position versus the inductor
SEM/EDX in progress
Yellow dots– results of the
present work (Analysis of sample composition at Tliq measurements are in progress. Plotted dots represent charge composition)
Amato I.
(1966)
Alberman K.B.
Blakey R.C.
Anderson J.S.
(1951)
Holc J.
Kolar D.
(1986)
mol%
CaO
20
40
60
80
UO2
T, C
1000
2200
2800
1600
1300
1900
2500
?
?

## Slide 22
Test results on ZrO2 - FeOy system: HPRS1-3
Experimental objectives
Determine liquidus and solidus temperature
Methods of charge synthesis
mixing of components at the molecular level => Increase of the processes speed
oxidizing medium => iron state – mainly Fe3+solid solution ZrO2(FeOy) formation
Sol-gel technique
Hydrothermal synthesis

## Slide 23
Test results on ZrO2 - FeOysystem: HPRS1-3 (2)
Temperature of specimen shape degradation start – 1395C
Temperature, at which the active specimen spreading on holder starts – 1493С
Temperature of complete spreading – 1769С
VPA in HTM

## Slide 24
Test results on ZrO2 - FeOy system
Blue lines – Jones T.S., Kimura Sh., Muan A. Diagram
Red dots – results of the present work

## Slide 25: Conclusions
Experimental facilities have been prepared for PLH measurements. LUCH has prepared specimens. Documentation for radioactive specimen transport to IHT RAS is under preparation
4 points out of 7 have been determined in the UO2-SiO2 system. A large amount of new data enables to specify the phase diagram and crystallization peculiarities in the system
First experiments in the UO2-CaO system have been conducted. Liquidus temperatures have been determined; final solid solutions and eutectic nucleus have been synthesized
Studies in the ZrO2 – FeOy system have been started. DSC/TG is planned to specify solidus temperature and study thermal effects in detail