## Slide 1
Application of the SVECHA/QUENCH code to the simulation of the QUENCH bundle tests
Q-06 and Q-12
Presented by
A.V.Palagin
JRC-ITU
Topical Meeting on ISTC Projects 1648.2, 2916, 2936, 3194
Podolsk-Moscow, Russia
July 3-5, 2007

## Slide 2: Outline
Effective channel approach
Q-06 test simulation
  Processing of the Q-06 bundle test temperature data
  Q-06 test simulation
  Analysis of the results obtained
Q-12 test simulation
  Processing of the Q-12 bundle test temperature data
  Q-12 test simulation
  Analysis of the results obtained
Summary and conclusion

## Slide 3: Effective channel approach
Since the central rod of the bundle is not heated, its temperature evolution in the course of quench bundle test is completely determined by thermal-hydraulic boundary conditions: temperatures of the surrounding heated rods and shroud and characteristics of the coolant flow.
In the case of full-scale simulation of the bundle test the temperatures of the heated rods and shroud are calculated by specifying the electric power time evolution and thus, the boundary conditions for the central rod are determined by the code.
In the SVECHA/QUENCH code the thermal boundary conditions for the central rod are predetermined by specifying the temperatures of the “effective channel” inner wall on the basis of experimentally measured temperatures. The inner surface of the effective channel represents the surfaces of the heated rods surrounding the central rod.
From the viewpoint of the solution of the heat conduction problem inside the central rod both ways are equivalent. Specification of the boundary conditions on the basis of the experimentally measured temperatures even has certain advantages as it describes the thermal regime around the central rod very close to that in the experiment.

## Slide 4: Q-06 test simulation Processing of the TC experimental data
The numerical procedure of the TC data recalculation includes:
smoothening, averaging and interpolation of the temperature curves
Bundle temperature evolution at the elevation 1350 mm measured by thermocouples
TFS 2/17, TFS 5/17 and averaged temperature used in the calculations

## Slide 5: Q-06 test simulation Processing of the TC experimental data
Bundle temperature evolution at the elevation 1150 mm measured by thermocouples
TFS 2/15, TFS 5/15 and averaged temperature used in the calculations

## Slide 6: Q-06 test simulation Processing of the TC experimental data
Bundle temperature evolution at the elevation 950 mm measured by corner rod thermocouple TIT A/13, central rod thermocouple TCRC 13, and averaged temperature used in the calculations

## Slide 7: Q-06 test simulation Processing of the TC experimental data
Averaged and smoothed curves representing temperature evolution of the QUENCH-06 bundle at the elevations from 1350 to -250 mm

## Slide 8: Q-06 test simulation Numerical parameters
The bundle nodalization:
Heat conduction module
  The total nodes number in the radial direction: 35
  Pellet nodes number in the radial direction: 21
  External layer (oxide) nodes number: 7
  Total nodes number in the vertical direction: 197
Total number of axial meshes used by oxidation
and mechanical deformation modules: 98

## Slide 9: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 1350 mm: TFS2/17 data, TFS5/17 data and calculated temperature evolution of the central rod outer surface

## Slide 10: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 1250 mm: TFS3/16 data, TFS5/16 data and calculated temperature evolution of the central rod outer surface

## Slide 11: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 950 mm and calculated temperature evolution of the central rod outer surface

## Slide 12: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 850 mm and calculated temperature evolution of the central rod outer surface

## Slide 13: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 950 mm: TFS 4/13 data and calculated temperature evolution of the central rod outer surface.
Quenching phase of the test

## Slide 14: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 950 mm: TIT A/13 data, TCRC_13 data and calculated temperature evolution central rod pellet’s centre.
Quenching phase of the test

## Slide 15: Q-06 test simulation Results of calculations
The experimentally measured temperatures at the elevation 850 mm: TFS_3/12 data, TFS_5/12 data and calculated temperature evolution of the central rod outer surface. Quenching phase of the test

## Slide 16: Q-06 test simulation Results of calculations
Temperature at the elevation 850 mm: TIT D/12 data and calculated temperature evolution of the central rod pellet’s centre. Quenching phase of the test

## Slide 17: Q-06 test simulation Results of calculations
Temperature at the elevation 650 mm: TFS 3/10 data and calculated temperature evolution of the central rod outer surface. Quenching phase of the test

## Slide 18: Q-06 test simulation Results of calculations
Oxide layer thickness axial profile of corner rod B (withdrawn from the test bundle at 6620 sec.) compared to the calculated one of the central rod for the same time

## Slide 19: Q-06 test simulation Results of calculations
Measured oxide layer thickness profiles of the heated rods (average), of the corner rods and of shroud, all at final state, compared to the calculated oxide layer thickness profile of the central rod (final state).

## Slide 20: Q-06 test simulation Results of calculations
Measured oxide layer thickness profiles of the heated rods (average), of the corner rods and of shroud, all at final state, compared to the calculated oxide layer thickness profile of the central rod (final state).

## Slide 21: Q-06 test simulation Results of calculations
The experimentally measured temperature at the elevation 750 mm: TFS and TSH thermocouples data
“Thermocouples which are lead through the hot zone of the bundle may give wrong readings at high temperatures in the hot zone”

## Slide 22: Q-06 test simulation Results of calculations
Experimentally measured and calculated hydrogen production rate.
Total amount of released hydrogen: 36 g (exp); 29.6 g (calc.)

## Slide 23: Q-06 test simulation Results of calculations
Experimentally measured and calculated hydrogen production rate.
Quenching phase of the test.
Amount of hydrogen released during quenching: 4 g (exp); 4.4 g (calc.)

## Slide 24: Q-06 test simulation Analysis of the results obtained
  SVECHA/QUENCH code was applied to the simulation of the QUENCH bundle test Q-06. The simulation was performed within the framework of the ‘effective channel approach’.
  The calculations adequately reproduce temperature evolution of the central rod at different elevations during the whole test duration including quenching phase.
  The calculated oxide axial profile agrees quite well with the experimental data at the time moment 6620 s when the corner rod B was withdrawn from the bundle and at the end of the test.
  Oxide thickness at the elevation 750 mm calculated on the basis of ‘questionable TCs’ is overestimated; usage of protected shroud TCs data results in correct value of the oxide thickness. This fact confirmed the correctness of the supposition that thermocouples which are lead through the hot zone of the bundle may give wrong readings at high temperatures in the hot zone.
  The details of the experimentally measured time dependence of the hydrogen production rate as well as the total amount of the released hydrogen are well reproduced by the calculations

## Slide 25: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 1350 mm: TFC 18/4/17 data, TFSU 11/3/17 data and calculated temperature evolution of the central rod outer surface

## Slide 26: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 1250 mm: TFSH 30/5/16 data, TFC 13/3/16 data and calculated temperature evolution of the central rod outer surface

## Slide 27: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 950 mm: TFSH/TFSU/TFC/TIT data and calculated temperature evolution of the central rod outer surface

## Slide 28: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 1050 mm: TFSH/TFSU/TFC data and calculated temperature evolution of the central rod outer surface.
Quenching phase of the test

## Slide 29: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 750 mm: TFSH/TIT data and calculated temperature evolution of the central rod outer surface.
Quenching phase of the test

## Slide 30: Q-12 test simulation Results of calculations
The experimentally measured temperatures at the elevation 650 mm: TFSH/TFSU data and calculated temperature evolution of the central rod outer surface.
Quenching phase of the test

## Slide 31: Q-12 test simulation Analysis of the test conditions
  It was planned that QUENCH-12 test should have the same scenario as QUENCH-06. The two factors that differed from QUENCH-06 were:
    VVER materials
    Different geometry
  Third factor took place due to technical reasons: 18 heated rods from 31 (20 from 21 in QUENCH-06)
  This led to substantial temperature differences in radial direction of the bundle (100-150 K) non-typical for QUENCH-06.
  As a result, as the central rod was presumably kept at about 1200ºC (950 mm elevation) during preoxidation, a part of the bundle had rather lower temperatures at which break-away effect occurs.
  Thus, oxidation kinetics in a part of bundle in QUENCH-12 test was quite different from that of QUNCH-06 one.

## Slide 32: Q-12 test simulation Results of calculations
Oxide layer thickness axial profile of corner rod D (withdrawn from the test bundle
at 5972 sec.) compared to the calculated one of the central rod for the same time

## Slide 33: Q-12 test simulation Results of calculations
Oxide layer thickness axial profile of corner rod F (withdrawn from the test bundle
at 7158 sec.) compared to the calculated one of the central rod for the same time

## Slide 34: Q-12 test simulation Results of calculations
Measured oxide layer thickness profiles of the rod B (withdrawn from the bundle at the end of the test), central rod, averaged for 31 rods, all at final state, compared to the calculated oxide layer thickness profile of the central rod (final state).

## Slide 35: Q-06 and Q-12 test results comparison Results of calculations
Comparison of the calculated oxide thickness profiles for the Q-06 and Q-12 tests
(final state)

## Slide 36: Q-12 test simulation Results of calculations
Experimentally measured and calculated hydrogen production rate.
Total amount of released hydrogen: 58 g (exp); 32.5 g (calc.)

## Slide 37: Q-12 test simulation Results of calculations
Experimentally measured and calculated hydrogen production rate.
Quenching phase of the test.
Amount of hydrogen released during quenching: 24 g (exp); 9.9 g (calc.)

## Slide 38: Q-06 and Q-12 test results comparison Results of calculations
Comparison of the calculated hydrogen release rates for the Q-06 and Q-12 tests

## Slide 39: Q-12 test simulation Results of calculations
Comparison of the calculated hydrogen release rates for the Q-06 and Q-12 tests
Quenching phase of the test.

## Slide 40: Q-12 test simulation Analysis of the results obtained
  SVECHA/QUENCH code was applied to the simulation of the QUENCH bundle test Q-12. The calculations adequately reproduce temperature evolution of the central rod at different elevations during the whole test duration including quenching phase.
  The calculated oxide axial profile agrees quite well with the experimental data at the time moment 5972 s when the corner rod D was withdrawn from the bundle.
  The calculated oxide thickness agrees quite well with the experimental data at 940 mm but is significantly lower at 700 and 1120 mm at the time moment 7158 s when the corner rod F was withdrawn from the bundle. This fact may be explained by ‘break-away’ oxidation at relatively low temperatures.
  The calculated oxide thickness at the end of the test was significantly underestimated, especially at 950 mm. This fact may be explained by more intensive oxidation during transient and quenching phases through friable cracked oxide structure formed due to break-away oxidation previously
  The details of the experimentally measured time dependence of the hydrogen production rate are well reproduced by the calculations at the preoxidation and transient phases. Calculations underestimate hydrogen production rate at the end of transient and quenching phase of the test.

## Slide 41: Summary and conclusions
  SVECHA/QUENCH code was applied to the simulation of the QUENCH bundle tests Q-06 and Q-12.
  Performed calculations show adequate work of the code with respect to temperature evolution, oxide axial profile and hydrogen production rate.
  The difference between experimental data and calculation results in Q-12 test are due to break-away oxidation of the bundle. Model for break-away oxidation has not been yet developed and implemented in the SVECHA/QUENCH code.
  Comparison of the calculated oxide axial profile and hydrogen production rate of the Q-06 and Q-12 tests shows that two tests are quite similar to each other in terms of bundle temperature evolution: similarity in temperatures leads to similarity in oxide axial profiles and hydrogen production rates.