## Slide 1: Progress Report on the ISTC project #3592 “Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel” (METCOR-P)
A.P. Alexandrov Research Institute of Technology (Russia)
Presented by S. Bechta
16th CEG-SAM meeting
Moscow, Russia
September 08-09, 2009

## Slide 2: Contents
General information
Objectives of METCOR-P project
Experimental matrix for METCOR-P project
Interaction of molten corium with European vessel steel in oxidizing atmosphere – Test MCP- 4
- Objectives
- Installation
- Procedure
- Results
- Concluding remarks
Planning
Publications

## Slide 3: METCOR-P project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
SPb Electrotechnical State University, Russia
FORTUM, Finland

## Slide 4: Objectives of METCOR-P project
Interaction characteristics at the vertically positioned interface
Peculiarities of interaction with European vessel steel
Corium melt oxidation transients
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:

## Slide 5
Experimental matrix for METCOR-P project
*) replaced by MCP-2 test with UO2+x– ZrO2 corium in air and horizontal position of interface
**) was performed in air (instead of steam) and regimes with UO2+x - ZrO2 - FeOy corium were added

## Slide 6: МСР - 4 Objectives
Comparison of corrosion rates for the European and Russian vessel steels in oxidizing atmosphere

## Slide 7: Composition of 15Kh2NMFA and 20MnMoNi5-5 steels

## Slide 8: RASPLAV-3 Installation
1 –pyrometer shaft; 2 –cover; 3 –electromagnetic screen; 4 – quartz tube; 5 – crucible section; 6 – inductor; 7 –melt; 8 – acoustic defect; 9 – molten ZrO2; 10 –ZrO2 powder thermal insulation; 11 – vessel steel specimen; 12 –top calorimeter of the specimen; 13 – bottom calorimeter of the specimen; 14 – kaolin wool insulation; 15 –ultrasonic sensor; 16 –thermocouples; 17 – crust, 18 – electromagnetic screen; 19 – uncooled electromagnetic screen; 20 – cylindrical support of the specimen
Furnace schematics

## Slide 9: Air supply and evacuation diagram
1 - silica gel air drier; 2 - furnace; 3 – cyclone; 4 – Large Area Filters (LAF); 5 - vacuum pump; P1-P3 – pressure sensors; G1,2 – flow meters ; Т1-Т3 – thermocouples; Ox- electrochemical oxygen sensor

## Slide 10: Vessel Steel Specimen
Blank
Upper calorimeter
Lower calorimeter

## Slide 11: Location of K-type thermocouples in the specimen

## Slide 12: Experimental procedure
UO2+x-ZrO2 corium
UO2+x-ZrO2-FeOy corium

## Slide 13: Thermocouple readings
1, 2, 3 – UO2+x- ZrO2 corium
4, 5, 6 – UO2+x- ZrO2- FeOy corium

## Slide 14: Corrosion depth measurements
h, mm
t, s
1 2 3 4 5 6
US measurement data
The maximum corrosion depth was  6 mm (post test cross section is not ready yet)
1, 2, 3 – UO2+x - ZrO2
4, 5, 6 – UO2+x - ZrO2 - FeOy

## Slide 15: Posttest analysis
Ingot reconstruction
Steel specimen surface after the test

## Slide 16: Posttest analysis (2)
Numeric modeling of specimen temperature conditions, regime No.4
Temperature distribution along the specimen height
Temperature field in the specimen upper part
Т, С
h, mm
А – corrosion front position
ANSYS code was applied

## Slide 17: Posttest analysis (3)
Measured corrosion rate (W) versus calculated interface temperature (Tint)
and corium/steel heat flux (q)
Note: *- Measured and calculated data for these regimes will be specified

## Slide 18: Comparison of corrosion rates for the European and Russian vessel steels
O
O
O
 - 20MnMoNi5-5, UO2+x - ZrO2
O - 20MnMoNi5-5, UO2+x - ZrO2 - FeOy
Error bars for new data were not calculated yet
Corrosion rates of European and Russian steel agree within experimental error
Insufficient data of European steel corrosion for generalization
VVER steel correlations can be used for estimations
15Kh2NMFA :

## Slide 19: Conclusion remarks for MCP- 4 test
Posttest analysis is underway
VVER steel correlations are applicable for Europe steel corrosion estimations
Similarly to the VVER steel, intensification of 20MnMoNi5-5 steel corrosion occurs at the interaction with the fusible UO2+x-ZrO2-FeOy corium if the interface temperature exceeds some limiting value

## Slide 20: Planning
4 more tests are to be performed according to the Experimental Matrix of the Project
Participants’ proposals concerning the remaining tests concretization and possible corrections to the Experimental Matrix were discussed at the last, 3rd Meeting with collaborators
This discussion are continued by correspondence

## Slide 21: Reporting
According to Export Control decision, METCOR reports will be sent to JRC ITU only

## Slide 22: METCOR-P publications
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // Proceeding of ICAPP’08, Anaheim, CA USA, June 8-12, 2008, Paper 8052.
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Krushinov E.V., Kotova S.Yu., Kosarevsky R.A., Barrachin M., Bottomley D., Fischer M., Fichot F. Corium Phase Equilibria from MASCA, METCOR and CORPHAD Results // Nucl. Eng. and Design, 238, p. 2761-2771 (2008).
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. VVER Vessel Steel Corrosion at Interaction with Molten Corium in Oxidizing Atmosphere // Nucl. Eng. and Design, 239 (2009), p. 1103-1112.

## Slide 23: METCOR-P publications (2)
4. Bechta S.V., Granovsky V.S., Khabensky V.B. et.al. VVER Steel Corrosion during In-Vessel Retention of Corium Melt // Proceeding of the 3rd European Review Meeting on Severe Accident Research (ERMSAR 2008), Paper 2.7, Nesseber, Bulgaria, September 23-25 (2008).
5. Bechta S.V., Granovsky V.S., Khabensky V.B. et.al. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // J. Nucl. Technology (in press), Manuscript Number: 08110 (2008).