## Slide 1
Current results of the ISTC project #2916 (CHESS)
RRC “KI”

## Slide 2: DEVELOPMENT OF THE MODELS FOR NUCLEAR FUEL BEHAVIOR DURING ACTIVE PHASE OF CHERNOBYL ACCIDENT
RRC “KI”
This model will make it possible to:
explain current physical and chemical state as well as spatial location of fuel containing materials (FCM) and radioactive substances inside the damaged Unit;
evaluate possibilities of modeling and find out “bottle necks” within the existing computational programs while modeling Chernobyl type accidents;
determine directions of future research on the problem.

## Slide 3: Main Tasks of the project
RRC “KI”
Task 1. Review of available input information and appropriate abilities of existing models. Assessment of sufficiency and validity of the information.
Task 2. Identification of accidental processes (relevant to “lava” properties) able to be modeled.
Task 3. Measurements of uranium and zirconium concentration in metallic melts.
Task 4. Development of the model describing transformation of fuel in the core to the LFCM – in consistence with experimental results.

## Slide 4: Main Tasks of the project
RRC “KI”
Task 5. Development of the forecasts (based on the model) for LFCM properties which can not be defined experimentally (in inaccessible areas).
Task 6. Assessment of concrete degradation along the way of “lava” penetration.
Task 7. Comparison of of uranium and zirconium content in melted metal predicted by the model and measured experimentally.
Task 8. Assessment of adequacy of existing and development of models describing corium behavior recommendations that should be accounted for in the future.

## Slide 5: First year results
RRC “KI”

## Slide 6: Scenarios of reactor destruction and lava generation
RRC “KI”
First model presented to IAEA (1986)
“Flying reactor” model (1990)
More realistic models (1994-1996)
Model – 2006 ?

## Slide 7: Reactor structure transformation
RRC “KI”

## Slide 8: Layout of the under reactor room – view from East to West
RRC “KI”

## Slide 9: Approaches to assess balance of the materials involved in corium
RRC “KI”

## Slide 10: Approaches to assess balance of the materials involved in corium
RRC “KI”

## Slide 11: Modeling – first approximation
RRC “KI”
1- Concrete of the under-reactor plate;
2- Sand of the vault’s filling material;
3- Serpentine concrete (Mg6Si4O10)*(OH)8;
4- “Lava”;
5- Concrete of building constructions dropped into the vault from upper level marks;
6- Air.

## Slide 12: Materials participated
RRC “KI”
[1] Mass of graphite within RBMK-1000 – 1700 t

## Slide 13: Scenario suppositions
RRC “KI”
Initial time of calculation: 0.5 h and 1 d after accident.
Real curve for decay generation.
Burning out of carbon:
С+O2=CO2+390 kJ/mol C
Decomposition of serpentine at 500 К:
(Mg6Si4O10)*(OH)8=3Mg2SiO4+SiO2+4H2O
Burning out of zirconium:
Zr+H2O=ZrO2+H2+[7760+1,15*(T0-200)]J/g Zr
Effective heat transfer in air and the in melt by simulating convective processes and barbotage.
The modeling of burning out of carbon was simulated by means of input of oxygen with speed 0.7 and 1.26 m3/s in all volume (that corresponds to 4 and 7 days).

## Slide 14: Scenario 1 (one radian)
RRC “KI”
m
m
m
m
K
K
Volume of lava
Heat power
Burning out of zirconium
Burning out of carbon
Scenario 1: Burning out of carbon for 7 days. Start of calculation – 0.5 h after the accident

## Slide 15: 2D temperature fields and maps of the lava - 1
RRC “KI”
After 5 days
After 10 days
m
m
m
m
K
K

## Slide 16: Scenario 2 (one radian)
RRC “KI”
m
m
m
m
K
K
Volume of lava
Burning out of zirconium
Burning out of carbon
Scenario 2: Burning out carbon for 4 days. Start of calculation: 0.5 h after accident
Power
Burning out of zirconium
Heat power
Volume of lava
Burning out of carbon

## Slide 17: 2D temperature fields and maps of the lava - 2
RRC “KI”
After 5 days
After 10 days
m
m
K
m
m
K

## Slide 18: Scenario 3 (one radian)
RRC “KI”
K
Scenario 3: Burning out carbon for 7 days. Start of calculation: 1 d after accident
Volume of lava
Burning out of zirconium
Burning out of carbon
Heat power

## Slide 19: 2D temperature fields and maps of the lava - 3
RRC “KI”
After 5 days
After 10 days
m
K
m
m
K
m

## Slide 20: Calculation summary
RRC “KI”
Modeling has been performed for start of the process of 0.5 h and 1 day after the accident.
Oxygen consumption for carbon burn out was varied.
Preliminary assessment has demonstrated that existing input data and modeling approaches do not contradict that destruction of serpentine and sand filling was possible for the first ten days.

## Slide 21: Visible contradictions of “simple” scenario
RRC “KI”
  Asymmetrical lava formation and penetration.
  Different participation of “fuel rod”s and “channel” Zr in the melt.
  Half of all fuel in the corium but only quarter of the basement was melted; difficulties to explain all fuel location.
  Probable getting in the corium some materials dropped down after the accident.

## Slide 22: Development of the more adequate scenarios (example)
RRC “KI”
a) Upper part of active core was thrown out by explosion. Channel structure was partially conserved. South-Eastern upper part of the reactor basement plate (“OR”) was damaged by explosion, direct contact of fuel debris and serpentine has occurred.

## Slide 23: Development of the more adequate scenarios (example)
RRC “KI”
b) U-Zr-O eutectic in the channels begun to form, it flowed down. Upper part of channels and graphite burnt out, fuel containing mixture has been “denser” from viewpoint of fuel content, S-E quarter of “OR” begun to melt through.

## Slide 24: Development of the more adequate scenarios (example)
RRC “KI”
c) Process b) continued. U-Zr-O eutectic flowed into the funnel at the place of “OR” melting through.

## Slide 25: Development of the more adequate scenarios (example)
RRC “KI”
d) View at present – about 50% of fuel and Zr from fuel rods flowed down having formed corium. About 70-80% of graphite and “channel” Zr has burnt off.

## Slide 26: Conclusion
RRC “KI”
  Project #2916 implementation corresponds to schedule.
  A lot of initial information has been accumulated, but its further recognition is required.
  Preliminary assessment has demonstrated that existing input data and modeling approaches do not contradict that destruction of serpentine and sand filling was possible for the first ten days.
  Ongoing activities have to develop and quantitatively assess more adequate scenarios.