## Slide 1: Progress report on the UO2 – CaO system
A.P. Alexandrov Research Institute of Technology
Presented by E. Krushinov
2nd PRECOS Project Meeting
May 26, 2009, St. Petersburg
International Science and Technology Center

## Slide 2
Contents
Available binary diagrams
Test results on UO2 - CaO system
Plans for further research
Conclusions

## Slide 3: Available binary diagrams (UO2 – CaO system)
Alberman K.B., Blakey R.C.,
Anderson J.S.
(1951)
Amato I.
(1966)
Teut =2080±20 °C
(eut) – 55%mol.CaO
UO2(ss) – 47%mol.CaO

## Slide 4: Available binary diagrams (UO2 – CaO system)
Holc J., Kolar D.
(1986)
Teut =1850±20 °C
eut – 63%mol.CaO
UO2(ss) – 30%mol.CaO
CaO (ss) – 0.35%mol.UO2

## Slide 5
Test results on UO2 - CaO system: PRS 4
Experimental objectives
Determine liquidus temperature
Determine final solubility of components in the formed solid solutions
Charge composition
Mol% 50UO2 + 50CaO
Samples
Tliq
The regime of molten pool formation and Tliq measurements
Two melt samples were taken and Tliq was measured 3 times by VPA IMCC

## Slide 6
Test results on UO2 - CaO system: PRS 4
1941°С
1915°С
1861°С
1629°С
The regime of the eutectic core formation in the ingot
From 6040 s, the pool was pulled out from inductor at 7.5 mm/h for 7 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
The temperature of the beginning of crystallization at the molten pool surface is below 1920°С

## Slide 7
Test results on UO2 - CaO system: PRS 4
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured three times: 2188oC, 2195 and 2181oC  Tliq=2188±40oC
sample | Cha | XRF | EDX
 | UO2 mol.% |  | 
№1 | 49.8 |  | 38.6
№2 | 48.7 | 51.4 | 38.1
Melt samples composition

## Slide 8
Test results on UO2 - CaO system: PRS 4
Eutectic nucleus
1875°С
1859°С
1882°С
1890°С
1899°С
Differential method results
Tsol
Visual polythermal analysis in the Galakhov microfurnace Tsol=1870С; Tliq=1900С
An analysis of a sample from the crystallized ingot has shown its composition to be close to eutectic
Tliq and Tsol determination in Galakhov microfurnace

## Slide 9
Test results on UO2 - CaO system: PRS 4
SEM/EDX analysis
 | UO2 | CaO
 | mol.% | 
SQ1 | 31.1 | 68.9
SQ2 |  | 
P1 | 53.1 | 46.9
Quenched
sample
UO2 ss
Dendritic microstructure of the melt sample
SQ1,2 – eutectic microstructure in the ingot
P1- the UO2(CaO) solid solution in the eutectic region of the ingot
1 cm

## Slide 10
Test results on UO2 - CaO system: PRS 5
Experimental objectives
Determine liquidus temperature at very high CaO content (indirect determination of CaO melting point)
Charge composition
Mol% 1UO2 + 99CaO
Results
Startup heating was successful
Molten pool was not formed and measurements not taken due to low electric conductivity of the melt
RASPLAV-4 heating current frequency of 5.28MHz is insufficient to maintain the pool of this composition in a molten state
Decision is taken to increase the concentration of uranium oxide in the next experiment

## Slide 11
Test results on UO2 - CaO system: PRS 6
Experimental objectives
Determine liquidus temperature at high CaO content
Samples
Tliq
Sample
Tliq
Two melt compositions have been realized within one melting cycle
3 melt samples were taken and Tliq was measured 4 times by VPA IMCC
Charge composition
Mol% 17.2UO2 + 82.8CaO

## Slide 12
Test results on UO2 - CaO system: PRS 6-1
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured two times: 2400oC and 2378oC  Tliq=2389±40oC
sample | Cha | XRF | EDX
 | UO2 mol.% |  | 
№1 | 26.1 | 26.0 | 17.2
№2 | 26.0 | 26.5 | 18.7
Melt samples composition

## Slide 13
Test results on UO2 - CaO system: PRS 6-2
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured two times: 2583oC and 2537oC  Tliq=2560±50oC
Charge composition (after CaO addition in to the melt)
Mol% 10.2UO2 + 89.8CaO
Sample | Cha | XRF | EDX
 | UO2 mol.% |  | 
№3 | 17.7 | 17.0 | 12.0
Melt samples composition

## Slide 14
Test results on UO2 - CaO system: PRS 6
SEM/EDX analysis
1 cm
Quenched
sample
CaO
CaO
Dendritic microstructure of the melt sample
Crust on the ingot

## Slide 15
Test results on UO2 - CaO system
Possible reasons of discrepancy between the results of Cha, XRF and EDX
Considerable hygroscopic property of samples
Only dry preparation of polished sections for SEM/EDX, possible CaO crumbling and filling of all possible depressions in the polished section surface

## Slide 16
Test results on UO2 - CaO system
The eutectics composition and solid solutions were synthesized by slow freezing
SEM/EDX in progress, compositions of the eutectics and solid solutions are not given
Yellow dots – temperatures determined by VPA IMCC, while compositions obtained by chemical analysis and XRF
Amato I.
(1966)
Alberman K.B.
Blakey R.C.
Anderson J.S.
(1951)
Holc J.
Kolar D.
(1986)
mol%
UO2
CaO
20
40
60
80
T, C
1000
2200
2800
1600
1300
1900
2500
?
?

## Slide 17
To specify the eutectic temperature, samples from the eutectic nucleus from PRS4 will be subjected to DTA
CaO-oriented VPA IMCC and equilibrium crystallization of the ingot to form an ultimately solid CaO-based solid solution
UO2-oriented VPA IMCC for three compositions
Results processing and generalizing
Final report preparation
Plans for further research

## Slide 18: Conclusions
First experiments in the UO2-CaO system have been conducted. Liquidus temperatures have been determined; final solid solutions and eutectic nucleus have been synthesized
The eutectic temperature evaluation by VPA in the Galakhov microfurnace has shown it to practically coincide with the data of Holc J.