## Slide 1
Material investigations of the SF1 fuel assembly.
Posttest appearance of the SF2 fuel assembly.
Presented by D.Ignatyev
Topical meeteng
Podolsk 3-6 July, 2007
FSUE SRI SIA “LUCH”
IBRAE RAS
FSUE EDO “GIDROPRESS”
ISTC

## Slide 2
Objective
Analysis of model fuel assemblies VVER-1000 appearance after severe accident tests with TOP and TOP&BOTTOM flooding
Main tasks
Analysis of oxidation scale, structure, chemical and phase composition of the bundle elements;
Determination of UO2 pellets dissolution degree and fuel distribution on height of assembly;
Estimation of melt distribution and blockage formation in the bundle.

## Slide 3
Schematic model of PARAMETER-SF1 assembly
after test
Total amount of cross sections - 18

## Slide 4: Cross section of the bundle at Z = 536 mm (top)
The assembly has no essential damages, the thickness of oxide scale on the surface of zirconium elements does not exceed 10 microns;
Two drips of a melt are detected between rods;

## Slide 5: Structure and composition of the melt (Z = 536 mm)
Ceramic phase content – 24 %
Dark phase
Metallic phase
Grey phase
Light phase
Ceramic phase

## Slide 6: Cross section of the bundle at Z = 652 mm (top)
Eutectic Zr - SS
(U,Zr,O) melt
The melt between rods flew off on rod surface warming up them and diluting claddings;
- Composition of the melt - (U,Zr,O) or eutectic Zr – SS.

## Slide 7
Zr
Melt (Zr, U, O, Fe, Cr, Ni)
a – Zr(O) + (U,Zr)
UO2
Zr – UO2 interaction (Z =652 mm)
3.4
2.4
UO2
a – Zr(O)
(U,Zr)
a – Zr(O)+ (U,Zr)
- There was the melt In the cladding-fuel gaps, which was ‘liquefied’ fuel and claddings;
- In case of cladding-fuel contact the eutectic interaction occured with formation of phases, known to be typical for Zr-UO2 interaction

## Slide 8: Cross section of the bundle at Z = 699 mm (top)
(U,Zr,O) melt
2.4
- The essential damage of claddings and shroud is noted, that testifies reaching at the given level of melting point of metal Zr-1%Nb (~1870 C).
- The form of claddings was saved by the external oxide layer.

## Slide 9: Cross section of the bundle at Z = 723 mm (top)
Once molten and relocated masses have formed an almost compact blockage (bottom of the blockage); - The structure of melt at this cross section is quite homogeneous; - Claddings and shroud were completely dissolved.
(U,Zr,O) melt
2.6

## Slide 10: Cross section of the bundle at Z = 745 mm (top)
There is no molten material between rods; - Fuel pellets are essentially dissolved; - There is a ceramic (Zr,U)O2 on the surface of the dissolved pellets.
3.1
2.1

## Slide 11: Cross section of the bundle at Z = 793 mm (top)
3.4
2.1
There is a relocated mass of melt at this level (top of the blockage); - This mass of melt is not homogeneous – there are local variations in the brightness of the colour; - Fuel pellets are essentially dissolved.

## Slide 12
(Zr,U)O2 + ZrO2
a – Zr(O) + (Zr,U)O2 + (U,Zr)O2
a – Zr(O) + (Zr,U)O2 + (U,Zr)O2
Microstructures of the melt at 793 mm

## Slide 13: Cross sections of the bundle at 800…1100 mm
Z = 839 mm
Z = 1021 mm
There are no claddings, shroud and molten material at this region; - We can see remains of oxide scale on the rods; - Fuel pellets are essentially dissolved.

## Slide 14: Strong fuel dissolution by relocated melt
Z = 839 mm
Z = 886 mm
Z = 930 mm
Z = 1021 mm
2.3
3.9
2.2
2.3

## Slide 15: Fuel fragmentation
Z = 1066 mm
Z = 1091 mm
- Only on these levels fragmentation of fuel was found out, but relocation of fuel does not significant.

## Slide 16: Cross section of the bundle at Z = 1263 mm (top)
Zr
UO2
(U, Zr)
 - Zr(O) + (U, Zr)
Zr
ZrO2
Claddings has through-wall cracks, which faces does not oxidized; - In places of cladding-fuel contact were founded the tracers of eutectic interaction.

## Slide 17
UO2 distribution, melt relocation
and blockage formation in PARAMETER-SF1 bundle

## Slide 18: Posttest appearance of SF2 fuel assembly
Shroud kept its integrity and leak tightness;
There is a thin oxide layer on its outer surface;

## Slide 19: Sampling for material analysis
Z = 1100 mm
Z = 1250 mm
Z = 1300 mm
- Fuel rod claddings were oxidized considerably and partially fragmented;
- There is no melt in the space between fuel rods.

## Slide 20: CONCLUSION (1)
The top flooding of overheated up to 2000C bundle resulted in expanded degradation of fuel rods (Z = 700…1100 mm), formation of melt, melt relocation and blockage formation. The integrity of assembly was saved only at the expense of heaters, which one played a role of a hull in the given experiment;
According to the plan of the project ISTC #3194 material investigations of fuel assemly PARAMETER - SF1 were carried out. The obtained date include:
- thicknesses of ZrO2 layers on cladding and shroud;
- thicknesses of oxide phase on melt surface;
- axial UO2 distribution on the bundle hight;
- distribution of relocated masses and blockage in the bundle;
- srtucrure an composition of melt ar different cross sections;
- thicknesses of the layers, formed in consequence of eutectic interaction Zr – UO2;

## Slide 21: CONCLUSION (2)
The top&bottom flooding of overheated up to 1500 C bundle resulted in fragmentation of fuel rods without melt relocation and blockage formation;
According to the plan of the project ISTC #3194 fuel assembly PARAMETER – SF2 was filled by epoxy and cut on cross sections.