## Slide 1
Post-test assessment of the top-flooding test PARAMETER-SF1
September 5-8, 2006, Kurchatov, Kazakhstan
FSUE SRI SIA “LUCH”
IBRAE RAS
FSUE EDO “GIDROPRESS”
Presented by A.Kiselev
(ISTC Project # 3194)

## Slide 2: Codes verification against SF1 test
Pre-test runs
Assessment of SF1 test Peculiarities - heat balances
Post-test modeling

## Slide 3: SF1 assessment – participants
PARAMETER-SF1
Russia:
NPO LUCH
GIDROPRESS
IBRAE RAS
RRC KI
France:
EdF
IRSN
Germany:
GRS
FzK

## Slide 4: Pre-test runs
RATEG/SVECHA - IBRAE RAS, RRC KI
ICARE/CATHARE – RRC KI
MAAP4 – EdF
ATHLET - GRS
RELAP - OKB “Gidropress”, RRC KI
MELCOR 1.8.5 - OKB “Gidropress”, IBRAE
PARAM TG + RAPTA-5 – NPO “LUCH”

## Slide 5: Temperatures: level 1250 mm (second ring of bundle)

## Slide 6: Temperatures: level 1100 mm

## Slide 7: Temperatures: level 900 mm

## Slide 8: Temperatures: level 700 mm

## Slide 9: Power vs time

## Slide 10: Released Energy - averaged

## Slide 11: Results of estimations
Pre-test el. power: 6 kWt or 20 MJ
Averaged experimental el. power: 3.83 kWt or 13.4 МJ
Overheat of steam (450-1200 K): 3.2кWt or 11.2 МJ
Heat loses: 9 MJ
(20-9)/(13.4-9)=2.5 (1.74)
Steam flux: 1.3-2 g/s

## Slide 12: Possible reasons
Steam condensation after switching on water cooled jacket
Steam-argon bypasses in technological slots:
  Test section body – SS insulation shroud
  SS insulation shroud-fiber ZrO2 insulation (breakaway of thermal insulation bottom cover plate )

## Slide 13: Volume of condensed water in lower plenum, l, versus time (RATEG-SVECHA)

## Slide 14: Modeling assumptions
Self consistent modeling of condensation
Bypass for steam-argon mixture:
  Initially: 200 mm2 - technological
  After 11500 s – 1000 mm2 - breakaway

## Slide 15: Volume of condensed water in lower plenum, l, versus time (RATEG-SVECHA)
Rate: 1.5 - 2 g/s

## Slide 16: Post-test runs (presented to 1.09.2006)
IBRAE RAS – RATEG/SVECHA
OKB “Gidropress” – RELAP
RNC KI – ICARE/CATHARE
EDF – MAAP4

## Slide 17: Electrical power

## Slide 18: Volume of condensed water in lower plenum, l, versus time (RATEG-SVECHA)
Rate: 1.5 - 2 g/s

## Slide 19: Consistent modeling of steam flow rate through the bundle

## Slide 20: Cladding temperature for second radial group at elevation 600mm versus time

## Slide 21: Cladding temperature for second radial group at elevation 1250mm versus time

## Slide 22: Shroud temperature at elevation 900mm versus time

## Slide 23: Hydrogen Production

## Slide 24: Phenomena for verification
Condensation in presence of noncondensable
Heat loses through shroud
Escalation
Quench front propagation
UO2 dissolution
Metallic and oxide melt relocation
Oxidation of melt in course of relocation
Melt solidification

## Slide 25: Conclusions
Results of post-test runs:
    Acceptable simulation of thermal and hydraulical bundle behavior
Future steps:
    Improvements of oxidation modeling in the course of top flooding
    Improvements of melt relocation modeling under quench conditions
Looking for:
    SF1 Post test material investigations;
    Additional data from SF2 and future (?) tests;
    Account for results of ISTC projects 1648.2 (VVER-QUENCH), 2936 (Melt relocation).