## Slide 1: Status of the ISTC project #3592 (METCOR-P)
Presented by V. Khabensky
3rd METCOR-P project meeting
May 27, 2009, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: METCOR-P project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
SPb Technological University, Russia
SPb Electrotechnical State University, Russia
FORTUM, Finland
Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel (#3592 METCOR-P)

## Slide 3
Objectives of METCOR-P project
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:
Interaction at the vertical position of vessel steel specimen surface
European vessel steel specimen behavior
Oxidation effects

## Slide 4: Experimental matrix for the METCOR-P project

## Slide 5: Decisions of the 1st meeting (May 30, 2007, St. Petersburg) on the update of METCOR-P Work Plan matrix and test sequence
Task 1: to replace reference test with experiment “Interaction of molten corium UO2+x-ZrO2 with vessel steel in the oxidizing above-melt atmosphere. Test МСР-2»
Task 1: to conduct experiment “Interaction of molten corium Fe-U-Zr-Gr-Ni-O with vertically positioned vessel steel specimen in the argon atmosphere” after the МСР-1 posttest analysis, improvement of the corrosion kinetics measuring system and completion of МСР-2 and МСР-3 tests
Test МСР-2 to be followed by Task 2 test “Steam oxidation effect on the interaction zone of C-32 corium with vessel steel: МСР-3 test”
In order to prepare Task 3 implementation with the European vessel steel specimens to send a request with specimen dimensions and grade of steel*
* specimens have been shipped to the ISTC

## Slide 6: METCOR-P experimental matrix

## Slide 7: Decisions of the 2nd METCOR-P meeting, 9 July 2008, St. Petersburg
Suspend the implementation of experimental program until the export control commission permits METCOR-P implementation
Prepare reports on МСР-1, МСР-2 experiments
Complete МСР-3 posttest analyses
Prepare test facility for the planned experiments
On getting the permission of export control commission to communicate by e-mail and make a decision about the next experiment within the Project *
* The permission was received in April 2009

## Slide 8: Tests completed within METCOR-P
Test | Name | Stage | Deliverables
МСР-1 | Interaction of molten corium with vertically positioned vessel steel specimen in the neutral atmosphere | Completed | Report
МСР-2 | Interaction of molten corium UO2+x-ZrO2 with horizontally positioned vessel steel specimen in the steam atmosphere (Instead of reference test) | Completed | Report
МСР-3 | Interaction of suboxidized corium melt with steel at the replacement of neutral atmosphere with steel | Completed | Report

## Slide 9: Preparation of test facility for the experiments planned within the Project
Generator has been upgraded to increase power in the melt
Adjustment test has been made. A 30 % increase of power deposition in the melt has been registered
Furnace and cooling systems have been adjusted for experiments with vertically positioned vessel steel specimen
Specimen design has been modified to host the embedded ultrasonic sensor. The specimen has been fabricated and subjected to cold testing

## Slide 10: METCOR publications
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental Study of Oxides Corium Interaction with Reactor Vessel Steel Samples // RASPLAV Seminar 2000, Munich, Germany, 14-15 Nov., 2000.
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental studies of oxidic molten corium – vessel steel interaction / Nucl. Eng. Design 210, (2001) 193-224.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Gornet G., Kymalainen O. New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel // Proceeding of ICAPP’04, Pittsburgh, P.A. USA, June 13-17, 2004, Paper 4114.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Fischer M., Bottomley D., Tromm W., Barrachin M., Altstadt E., Piluso P., Fichot F., Hellmann S., Defoort F. CORPHAD and METCOR ISTC projects // The first European Review Meeting on Severe Accident Research (ERMSAR-2005), Aix-en-Provence, France, 14-16 November, 2005.

## Slide 11: METCOR publications (2)
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 1: Experimental // Nucl. Eng. Des., 236 (2006) 1810-1829.
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 2: Model development // Nucl. Eng. Des., 236 (2006) 1362-1370.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Piluso P., Miassoedov A., Altstadt E., Willschufz H.G., Fichot F. Experimental Study of Interaction Between Suboxidized Corium and Reactor Vessel Steel // Proceeding of ICAPP’06, Reno, P.A. USA, June 4-6, 2006, Paper 6054.

## Slide 12: Publications during METCOR-P
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // Proceeding of ICAPP’08, Anaheim, CA USA, June 8-12, 2008, Paper 8052.
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Krushinov E.V., Kotova S.Yu., Kosarevsky R.A., Barrachin M., Bottomley D., Fischer M., Fichot F. Corium Phase Equilibria from MASCA, METCOR and CORPHAD Results // Nucl. Eng. and Design, 238, p. 2761-2771 (2008).
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. VVER Vessel Steel Corrosion at Interaction with Molten Corium in Oxidizing Atmosphere // NED, (in press), Manuscript Number: 5248, Corrected Proof, http://dx.doi.org/10.1016/j.nucengdes.2008.12.009)

## Slide 13: Publications during METCOR-P (2)
4. Bechta S.V., Granovsky V.S., Khabensky V.B. et.al. VVR Steel Corrosion during I-Vessel Retention of Corium Melt // Proceeding of the 3rd European Review Meeting on Severe Accident Research (ERMSAR 2008), Paper 2.7, Nesseber, Bulgaria, September 23-25 (2008).
5. Bechta S.V., Granovsky V.S., Khabensky V.B. et.al. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // J. Nucl. Technology (in press), Manuscript Number: 08110 (2008).

## Slide 14: Current situation with METCOR-P
Within 2 years of the Project ~ 40 % of the work foreseen by its Work plan has been completed
The delayed Work plan implementation is explained by the absence of export control permission
The remaining experimental part (5 experiments) will be completed in accordance with the updated Work plan during the third (last) year of the project
Analysis of experimental data and delivery of reports are planned for the 6-month period after the formal Project completion
In order to get most relevant information on the studied phenomena it is recommended to update the experimental matrix using results of new tests