## Slide 1: Progress Report on the ISTC project #833.2 “Investigation of corium melt interaction with NPP reactor vessel steel” (METCOR-2)
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
9th CEG-SAM Meeting

## Slide 2: Contents
METCOR project general information
Experimental matrix
Tests with suboxidized corium
Conclusions on tests with suboxidized corium
Tests with oxidized corium in air and steam
Conclusions on tests with oxidized corium
Reporting
Publications
Plans for concluding of the project
Proposals for studies continued within a new project
Conclusions

## Slide 3: METCOR project general information
Qualification and quantification of physicochemical phenomena of corium melt interactions with reactor vessel steel
Experimental data application:
Analysis of in-vessel corium retention (IVR)
Analysis of ex-vessel retention (EVR) in the core catcher of a cold crucible type
Project objectives:

## Slide 4: METCOR project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatome ANP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZR, Germany
FORTUM, Finland
*) Should be finished in May 2006

## Slide 5: Experimental matrix of METCOR
Phase 1: Tests with fully oxidized melts

## Slide 6: Experimental matrix of METCOR
Phase 2: Tests with suboxidized corium and tests with oxidized corium in steam

## Slide 7: Tests with suboxidized corium
1 – pyrometer shaft; 2 – cover; 3, 18, 19 – electromagnetic screens; 4 – quartz tube; 5 – crucible sections; 6 – inductor; 7 –melt; 8 – acoustic defect; 9 – fused ZrO2 grains; 10 – ZrO2 powder insulation; 11 – vessel steel specimen; 12 – top specimen calorimeter; 13 – bottom specimen calorimeter; 14 – kaolin wool insulation; 15 –ultrasonic sensor; 16 – thermocouples; 17 – crust; 20 – cylindrical support of the specimen
Technology of the induction melting in a cold crucible
Atmosphere – high-purity argon
Long-term expositions in a stationary regime
On-line measurements:
specimen temperature
melt surface temperature
specimen ablation depth
electric parameters
power in the furnace components
Experimental methodology: Furnace section

## Slide 8: Tests with suboxidized corium (continued)
Experimental methodology: Methods of posttest analyses
Calculation of the whole electromagnetic system
Power deposition in the melt and its electric resistivity are determined Measured electric parameters of the system and power deposited into the furnace components are used in the numeric modeling.
Integrated calculation of the electromagnetic system and melt thermohydrodynamics
Radial heat flux distribution in the specimen top is determined. Calculations of the whole electromagnetic system and boundary conditions on the crucible and specimen surfaces are used.
Calculation of the specimen temperature conditions
Results of previous calculations, boundary conditions on the crucible surface and specimen calorimeters are used. The adequate agreement between calculations and thermocouple measurements is achieved by varying heat flux into the specimen and thermal resistance of the specimen side insulation.
Physicochemical analysis of the ingot, specimen and interaction zone
XRF; SEM/EDX; optical microscopy; chemical analyses. Elemental and mass balances, initial and final compositions of the system and its components are determined.

## Slide 9: Tests with suboxidized corium (continued)
Corrosion kinetics and final depth
Axial sections of specimens
Corrosion depth vs. time
MC6
MC7
MC8
MC9
Shrinkage cavity
Chip
Acoustic defect
EDX images of interaction zone
500 µm
100 µm
10 µm
Teut~1090ºC (DTA)

## Slide 10: Tests with suboxidized corium (continued)
Characteristics of Interaction zone
B – interaction zone boundary;
1 - 800C, 2 – 900°C, 3 – 1000°C, 4 – 1100°C, 5 – 1200°C, 6 – 1300°C, 7 – 1400°C
Temperature field in the specimens

## Slide 11: Tests with suboxidized corium (continued)
Empirical correlation for ablation kinetics
3 periods of ablation: incubation, fast ablation, transition (the last one is neglected in the model)
fast ablation resulting in saturation
, mm/s
1090  Tint  1440C – temperature on the ablation front
incubation period - oxidic melt tinc=8000+200 (70-Cn), s
30  Cn  70
- metallic melt
tinc=0
Kinetics of specimen corrosion

## Slide 12: Tests with suboxidized corium (continued)
Mass of ablated vessel steel vs. time
Lower head region after 20 h
Blue: calculation 1, red calculation 2
a) ablation depth of the lower head from the сalculation 2, grey: ablated steel b) temperature conditions of the vessel
the evaluated thickness of undamaged vessel wall is much smaller, if the vessel steel ablation is taken into account
vessel strength calculations are in progress
Example of plant application [E. Altstadt and H.G. Willschütz, 2006]:
For VVER-1000 – type reactor, low pressure scenario, homogeneous molten pool, initial temperature of corium is 1500K. Calculation 1 – without physicochemical interactions Calculation 2 – the interactions have been evaluated by the empirical correlations

## Slide 13: Conclusions on tests with suboxidized corium
The depth of eutectic melting (dissolution) of steel is limited by the position of isotherm  1090 C
The proposed empirical correlation enables to calculate the approximate corrosion rate, which decreases as the steel temperature on the interaction front is reduced, and to evaluate the thickness of unaffected vessel wall
First evaluations show the effect of corium/steel physicochemical interaction on the mass of ablated steel, vessel wall thickness and temperature

## Slide 14: Tests with oxidized corium in air and steam
Methodology
Furnace schematics
Gas-aerosol sampling system
1 – steam vent from the furnace; 2 – steam line; 3 – lid; 4- water-cooled cover; 5 – quartz tube; 6– water-cooled electromagnetic screen; 7 – crucible sections; 8 – inductor; 9 – melt; 10 – acoustic defect; 11 – thermal insulation of the specimen; 12 – top specimen calorimeter; 13 – bottom specimen calorimeter; 14 – US sensor.
1 – tanks with Ar,N2; 2 – steam generator; 3 – heated steam supply line; 4 – quartz tube for steam supply into the furnace; 5 – steam condenser; 6 – condensate collector; 7 – condensate drop catcher; 8 - ejector; 9 – large-area filter (LAF); 10 – silica gel drier; 11 – medium-area filter (MAF); 12 – electrochemical sensors of oxygen and hydrogen; 13 – vacuum receiver; 14 – mass-spectrometer; 15 – weight sensor 16 – hydro lock; 17 – vacuum gas burettes; 18 - medium-area filter (MAF).

## Slide 15: Tests with oxidized corium in air and steam (continued)
Methodological peculiarities of experiments in steam:
furnace design has been changed in order to minimize steam condensation on cool surfaces
superheated steam is supplied from electricity-heated steam generator
mass-spectrometer is used for determining the steam- gas composition at the furnace exit
temperature measurements of the melt surface are made discretely during the short-term replacement of steam with air

## Slide 16: Tests with oxidized corium in air and steam (continued)
– – - boundaries of regimes
within one regime the corrosion rate is practically constant (just like in air)
during a temperature increase on the specimen surface the corrosion rate grows
Kinetics and final depth of specimen ablation in MC 11
1– initial position of the specimen surface
2 – final position of the specimen surface
average ablation depth in the sighting spot of the US sensor – 3.7 mm – practically coincides with direct US measurements during the test completion
~100m
FeOy corrosion layer
40m
Bulk corium
FeOy
40m
U1-xZrxO2+yss

## Slide 17: Tests with oxidized corium in air and steam (continued)
Specimen temperature conditions in MC11
Т, С
h, mm
Regime №2

## Slide 18: Tests with oxidized corium in air and steam (continued)
In all experiments the corrosion kinetics is controlled by the diffusion of Fe ions through the corrosion layer of Fe oxides having thickness ; and it can be described by the Tamman equation
where Ea – activation energy; R – universal gas constant; A – numerical coefficient; q – heat flux from corium to steel; λ – heat conductivity of corrosion layer; ΔT – temperature difference of the corrosion layer of FeOy
Summary of experimental results in air and steam

## Slide 19: Tests with oxidized corium in air and steam (continued)
Two different types of corrosion kinetics depending on the interaction conditions and crust morphology
Corrosion layer and corium layer are solid
Eutectic melting of corrosion layer on the interface with corium
Corium Melt
Corium Crust
Corrosion Layer of FeOy
Vessel Steel Cooled from Outside
Tsol
H
δ
Tsurf
T<Teut (1340 oC)
1.1 UO2+x-ZrO2-FeOy corium: Tsurf<1050C
1.2 C-100 (UO2+x-ZrO2) corium: Tsurf<1200C
Corium Melt
Corrosion Layer of FeOy
Vessel Steel Cooled from Outside
δ=H
Tsurf
T=Teut (1340 oC)
2.1 UO2+x-ZrO2-FeOy corium: Tsurf≥1050C
2.2 C-100 corium: Tsurf≥1200C
H
Corium Melt
Corium Crust
Corrosion Layer of FeOy
Vessel Steel Cooled from Outside
δ
Tsurf
T=Teut (1340 oC)
Liquid sublayer
CORPHAD data:
- Teut=1339oC in UO2+x-FeOy-ZrO2 system in air

## Slide 20: Tests with oxidized corium in air and steam (continued)
Arrhenius plot for corrosion rate
Segments of straight lines having a large angle of slope are shown conditionally in order to determine the temperature, at which the corrosion regime is changed
The activation energy for the 1st corrosion regime is approx. 70 kJ/mol, and it is the same for air or steam atmosphere. The corrosion rate for corium C-100 is approx. two times higher than for UO2+x- ZrO2- FeOy
W/q,
(mm/h)/(MW/m2)
1000/Tsurf, 1/K
Corrosion kinetics for case 1

## Slide 21: Tests with oxidized corium in air and steam (continued)
Corrosion rate vs. inverse corrosion layer thickness
Corrosion rate practically does not depend on changes in the diffusion coefficient in the corrosion layer
Corrosion rate for corium C-100 is lower than for UO2+x-ZrO2-FeOy
Corrosion kinetics for case 2
Where: Tsurf – temperature on the steel surface; Teut – eutectic temperature in the UO2+x-ZrO2-FeOy system;
C – coefficient

## Slide 22: Conclusions on tests with oxidized corium
It has been established that corrosion characteristics are very sensitive to corium composition and not so sensitive to the replacement of air by steam above the melt
Two different corrosion regimes are possible depending on the interaction conditions
First of them is described by the Arrhenius equation
Second regime is controlled by the eutectic melting of corrosion layer on its interface with corium. The corrosion rate is linearly dependent on the inverse corrosion layer thickness
Produced results enable to refine the methodology of vessel steel corrosion calculations for the IVR conditions in the studied range of parameters

## Slide 23: Reporting: 2nd phase

## Slide 24: Publications
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol,
V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer,
G. Cognet, O. Kymäläinen.
New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel //Proceedings of ICAPP’04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4114
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky,
D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm,
D. Bottomley, H. Tuomisto.
Corrosion of vessel steel during its interaction with molten corium
Part 1: Experimental // to be published in Nucl. Eng. Des., reg. LO/NED#679,2005
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky,D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm, D. Bottomley, H. Tuomisto. Corrosion of vessel steel during its interaction with molten corium
Part 2: Model development // to be published in Nucl. Eng. Des., reg. LO/NED#680,2005
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol,
V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer,
P. Piluso, A. Miassoedov, E. Altstadt, H.G. Willschütz, F. Fichot.
Experimental Study of Interactions Between Suboxidized Corium and Reactor Vessel Steel //to be published in Proceedings of ICAPP’06, Reno, NV USA, June 4-8, 2006, Paper 6054

## Slide 25: Plans for concluding of the project
Complete MC 11 analyses
Deadline: Mart 2006
Release MC10&11 reports
Deadline: April 2006
Release METCOR.2 annual report (3rd year)
Deadline: May 2006
Release METCOR.2 final report
Deadline: July 2006
Finish METCOR paper preparation
Deadline: 2006
Final project meeting combined with kick-off meeting of the next project
June 2006, St Petersburg

## Slide 26: Experimental matrix* for a new project
*)To be included into Work Plan of a new project for the period of 01.07.2006 - 30.06.2009

## Slide 27: Conclusions
VVER steel corrosion mechanisms have been clarified
The developed correlations can be used in the analyses of IVR with oxidized and suboxidized coria under different above-melt atmospheres
Finalization of corrosion studies requires the following experiments
- for oxidized corium: in the temperature range of the specimen surface exceeding 1200 oC,
- for suboxidized corium: at the vertical orientation of the specimen surface
- for vessel steel used in European reactors