## Slide 1: Thermal and mechanical analyses of the VVER-1000 RPV in an IVR scenario considering corrosion effects
Eberhard Altstadt
2nd METCOR-P Meeting, St. Petersburg, July 9, 2008

## Slide 2: Corium pool configurations
Configuration 1: suboxidized pool
  melt segregation (metal and oxide layer)
  oxide mass: 64 t, metal mass: 116 t
  pool height 2.2 m (1 m + 1.2 m)
Configuration 2: fully oxidized pool
  homogeneous melt
  mass: 210 t
  pool height: 3.1 m

## Slide 3: Internal heat fluxes (calc. by Russian colleagues)

## Slide 4: Decrease of the internal heat flux

## Slide 5: External thermal boundary condition
Tw,e = f (q, Twater)

## Slide 6: Temperatures and heat fluxes
segregated pool
homogeneous pool

## Slide 7: Analysis of four scenarios
A: segregated pool without corrosion
B: segregated pool with corrosion
C: homogeneous pool without corrosion
D: homogeneous pool with corrosion

## Slide 8: Outer temperatures vs. time
Scenario A
Scenario B

## Slide 9: Outer temperatures vs. time
Scenario C
Scenario D

## Slide 10: Final ablation
B
A
C
D

## Slide 11: Ablation kinetics

## Slide 12: Mechanical calculations
Elastic-plastic material behaviour
Material configuration: final ablation state
Temperature field from t = 300 s
Weight of vessel and melt pool
Increasing internal pressure until vessel failure
Failure criterion: allowable stress max (T)

## Slide 13: Allowable stress

## Slide 14: Stress at failure pressure (segregated pool)
A
B

## Slide 15: Stress at failure pressure (homogeneous pool)
C
D

## Slide 16: Main results - overview
Scenario | A | B | C | D
Pool configuration | segregated | segregated | homogeneous | homogeneous
Corrosion | no | suboxidized | no | oxidized
ablated steel mass | 32.3 t | 36.5 t | 25.5 t | 35.5 t
Tmax,out | 400 K | 400 K | 393 K | 393 K
min. wall thickness | 60 mm | 50 mm | 100 mm | 70 mm
pFailure | 13.81 MPa | 13.80 MPa | 19.33 MPa | 19.11 MPa

## Slide 17: Allowable stress and characteristic temperatures
Tallow,cr
TB
Tliq

## Slide 18: Conclusions
Corrosion leads to significantly higher ablation
Corrosion effect more pronounced in the homogeneous (oxidized) pool
Due to the higher peak heat flux the segregated pool configuration is more critical
The vessel strength is almost not influenced by the corrosion
  load is carried by the cold outer region of the vessel wall

## Slide 19: Model of corrosion damage
NITI correlation for fast corrosion stage
interface
hel
T1
T2
T3
Element killed if Dcorr  1