## Slide 1: Progress report on the ISTC project #3813: Phase relation in corium systems (PRECOS)
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
19th CEG-SAM meeting
Pisa, Italy
March 14-16, 2011
ETU
Saint-Petersburg
SPbSIT (TU)

## Slide 2: Contents
  General information
  Project objectives
  PRECOS test matrix
  Scope of work in quarters 10 - 11
  Test results:
  UO2-SiO2- FeO system
  UO2-CaO- FeO system
  Concluding remarks
  ! IVTAN test results will be presented separately by Prof. M. Sheindlin

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
IVTAN,
Russia
SPb State Electrotechnical University,
Russia
SPb State
Technological University, Russia

## Slide 4: Project objectives
Experimental determination of:
liquidus – solidus temperatures
coordinates of reference points (eutectics, etc.)
solubility limits of solid solutions
compositions of liquids coexisting in the miscibility gap

## Slide 5: PRECOS test matrix
Task | Composition | Atm | Experimental data | Priority level | Number of tests scheduled /carried out
1 | U-Zr-Fe-O | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6/81
2 | ZrO2 - FeOy | Air and pO2 control | liquidus, solidus, solubility limits | 2 | 3/32
 | UO2 - SiO2 | Neutral | liquidus, solidus, solubility limits, eutectic point | 1 | 7/(53+404)
 | CaO - UO2 |  |  | 1 | 7/73
3 | UO2 – FeO – SiO2 |  | liquidus, solidus, solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10/(23+94)
 | UO2 – FeO – CaO |  | liquidus, solidus, solubility limits, ternary eutectic point | 1 | 10/(23+14)
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2/0
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2/0
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by: - French partners (1 system) German partners (1 system) - Russian partners (1 system) | 2 | 3/0
Notes: 1-LPH (Zr-O), 2- HTM, 3- VPA IMCC, 4- VPA in Galahov microfurnace
According to the 3rd Project meeting decisions these systems will be excluded from the test matrix for a more detailed study of systems having higher priority

## Slide 6: Scope of work in quarters #10-11

## Slide 7
UO2 – FeO – SiO2 system: PRS 13 test results
Experimental objectives
Charge composition
mol.% 30.00 UO2 + 46.67 FeO +23.33 SiO2
Tliq was measured 4 times by VPA IMCC with melt sampling
Eutectic core was synthesized by slow melt crystallization
Test procedure
Tliq determination by VPA IMCC
Determination of the ternary eutectic composition

## Slide 8
UO2 – FeO – SiO2 system: PRS 13 test results (2)
Measured liquidus temperature and compositions of melt samples

## Slide 9
SEM/EDX of eutectic core
UO2–FeO–SiO2 system: PRS 13 test results (3)
Inclusions of UO2 base solid solution were identified in the eutectic core
Eutectic compositions were determined in 14 ss-free regions and the data were averaged
The sample cut out from the eutectic core had unknown content of the ss
Eutectic |  | UO2 | FeO | SiO2
14 fields | mass % | 10.3  1.2 | 63.3  3.0 | 26.4  2.5
 | mol% | 2.8  0.3 | 64.9  3.1 | 32.3  3.0
6 m
SS

## Slide 10
Teut determination in the Galakhov microfurnace
Tsol= 1191С≈Teut
Tliq=1545С
UO2 –FeO-SiO2 system: PRS 13 test results (4)
Sample cut out from the eutectic core of the ingot
1179C
1545C
1191C
1528C
1264C

## Slide 11
UO2-FeO-SiO2 system: test results (5)
e1 composition was determined by SEM/EDX
e2 and e3 ternary eutectics are expected in the system
e2 eutectic core was synthesized in PRS16 tests
Next test will be objected on e3 determination
UO2
Eutectic points
Fe2SiO4
e1
e2?
e3?

## Slide 12
UO2 – FeO – SiO2 system: PRS 16 test results (6)
Experimental objectives
Charge composition
mol.% 10 UO2 + 70 FeO +20 SiO2
Tliq was measure 3 times by VPA IMCC with melt sampling
The pool was pulled out from the inductor at 9 mm/h for 4.5 hours starting at 4646 s. This has ensured close to equilibrium crystallization and eutectic core formation in the ingot upper part
Tliq determination by VPA IMCC
Determination of the e2 ternary eutectic composition

## Slide 13
UO2 – FeO – SiO2 system: PRS 16 test results (7)
VPA IMCC: Example of thermogram #1 showing melt surface
    First solid phase was not detected at the melt surface. Consequently Tliq was not determined
    Melt samples were used for VPA GM

## Slide 14
Tsol and Tlig determination in the Galakhov microfurnace
Tsol= 1194С
Tliq=1627С
Close temperatures for other samples
UO2 –FeO-SiO2 system: PRS 16 test results (8)
Sample #3
1158C
1627C (complete spreading)
1194C (deformation start)
1620C
1231C

## Slide 15
Experimental objectives
Annealing, melting and quenching in the Galakhov microfurnace
Test | Content, mol.% |  |  | Tempera-ture, С | Exposure time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS59 | 5.0 | 77.0 | 18.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS60 | 5.0 | 77.0 | 18.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
GPRS61 | 10.0 | 78.0 | 12.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS62 | 10.0 | 78.0 | 12.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
GPRS63 | 15.0 | 79.0 | 6.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS64 | 15.0 | 79.0 | 6.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
Study of tie lines and miscibility gap boundaries
UO2 of >99.0 % purity, SiO2 of 99.99% purity, FeO of >99.0 % purity, charge mass – 150 mg, molybdenum crucibles  6 mm
SEM/EDX in progress
UO2-FeO-SiO2 system: GPRS #59-64 test results (9)

## Slide 16
UO2-FeO-SiO2 system: test results (10)
Eutectic point e1 has been determined to belong to UO2-Fe2SiO4 section of the diagram.
e2 and e3 ternary eutectics are expected in the system
Tliq of PRS 13 composition has been measured by VPA IMCC. Tliq of PRS 16 composition has been determined by VPA GM and will be checked by DTA
The performed annealing tests confirm miscibility gap in a fairly narrow region adjacent to the SiO2 corner of the diagram

## Slide 17
UO2 – FeO – CaO system: PRS 14 test results
Experimental objectives
Charge composition
mol.% 6UO2 + 75FeO +19CaO
Tliq determination by VPA IMCC
Determination of eutectic composition
Tliq was measured 3 times by VPA IMCC with melt sampling
Eutectic core was formed in the ingot
Test procedure

## Slide 18
UO2 – FeO – CaO system: PRS 14 test results (2)
Liquidus temperatures and compositions of melt samples measured by XRF and ChA
* - determined from residue
Tliq was measured 3 times by VPA IMCC but video record of one measurement was not interpreted.
The results of corium samples XRF and chemical analysis were found to differ significantly
XRF results are believed to be more accurate, since the content of CaO was not determined by chemical analysis, but calculated from the residue

## Slide 19
40 m
Sample 1
20 m
Sample 2
60 m
200 m
40 m
Sample 3
Composition |  | UO2 | FeO | CaO
Averaged | mass % | 13.31.0 | 73.00.9 | 13.70.4
 | mol% | 3.80.3 | 77.50.5 | 18.70.4
SEM/EDX of the melt samples
UO2 – FeO – CaO system: PRS 14 test results (3)
Local composition (averaging square about 1000 m)
The results of SEM/EDX on Ca content confirm the XRF results

## Slide 20
1 sm
ingot
250 m
6 m
6 m
15 m
CaUO3
FeO
CaO2FeO
Eutectic |  | UO2 | FeO | CaO
Average of 8 sections | mass % | 10.4  0.3 | 62.5  0.6 | 27.1  0.7
 | mol% | 2.8  0.1 | 62.5  0.7 | 34.7  0.8
SEM/EDX of the eutectic core
UO2 – FeO – CaO system: PRS 14 test results (4)

## Slide 21
UO2 – FeO – CaO system: PRS 15 test results(5)
Experimental objectives
Charge composition
mol.% 13UO2 + 50FeO +37CaO
Tliq was measured 3 times by VPA IMCC with melt sampling
From 4575 s, the pool was pulled out from the inductor at 9 mm/h for 4.5 hours. This has ensured close to equilibrium crystallization and the eutectic core formation in the ingot upper part
Tliq determination by VPA IMCC
Confirmation of eutectic composition

## Slide 22
UO2–FeO–CaO system: PRS 15 test results (6)
VPA IMCC: Example of thermogram 1 from the test showing melt surface
    Results of Tliq measurements: 1516, 1516, 1511oC

## Slide 23
UO2 – FeO – CaO system: PRS 15 test results (7)
Liquidus temperatures and compositions of melt samples measured by XRF and ChA
* - determined from residue
XRF result seems more accurate since the content of CaO was directly measured and confirmed by SEM/EDX

## Slide 24
100 m
Sample 1
20 m
Sample 2
15 m
40 m
Sample 3
Composition |  | UO2 | FeO | CaO
Averaged for 3 section | mass % | 30.62.2 | 45.72.9 | 23.60.9
 | mol% | 9.70.8 | 54.32.6 | 36.01.8
UO2 – FeO – CaO system: PRS 15 test results (8)
SEM/EDX of melt samples
Notes: Слава. Если известно буллит о фазе первичной кристаллизации и микроструктуре пробы

## Slide 25
1 cm
ingot
50 m
6 m
10 m
FeO
Eutectic |  | UO2 | FeO | CaO
9 sections averaged | mass % | 11.3  2.0 | 59.6  2.7 | 29.1  1.3
 | mol% | 3.0  0.6 | 59.7  2.2 | 37.3  1.8
CaFeO2
UO2 – FeO – CaO system: PRS 15 test results (9)
SEM/EDX of eutectic core

## Slide 26
UO2 – FeO – CaO system: PRS 15 test results (10)
Eutectic |  | UO2 | FeO | CaO
 | mass % | 10.9  2.3 | 61.1  3.3 | 28.1  2.0
 | mol% | 2.9  0.7 | 61.1  2.9 | 36.0  2.6
Averaged eutectic composition in PRS 14 and 15 tests
CaO2FeO
0.2
0.4
0.6
0.8
FeO
0.8
0.6
0.4
0.2
0.8
0.6
0.4
0.2
1
3
3
5
±
5
1
1
0
8
1
8
7
8
±
3
0
CaO
UO2
PRS14
CaUO3
PRS15
CaFeO2
PRS14
PRS14
5
Eutectic point

## Slide 27
Experimental objectives
Annealing, melting and crystallization in the Galakhov microfurnace
UO2 of >99.0 % purity, SiO2 of 99.99% purity, FeO of >99.0 % purity, charge mass – 150 mg, molybdenum crucibles  6 mm
SEM/EDX in progress
UO2-FeO-CaO system: GPRS 66 test results (11)
Validation of eutectic composition
Charge composition
mol.% 15UO2 + 80FeO +5CaO

## Slide 28
UO2-FeO-CaO system: test results (12)
Tliq of PRS 14 and 15 compositions has been determined by VPA IMCC
Single eutectic point has been found. Its composition has been determined. It will be checked by SEM/EDX of GPRS 66 ingot section
Measurements of Tsol and final solubility are in progress

## Slide 29: Joint publication with collaborators within the reported quarters
V.I. Almiashev et al, Ternary eutectics in the systems FeO–UO2–ZrO2 and Fe2O3–U3O8–ZrO2 // Radiochemistry, 2011, V. 53, N 1, P. 13–18

## Slide 30: Concluding remarks
The Project has been prolonged for 6 months without additional funding
Work scope for quarters # 12 - 13
Complete study of the next systems: ZrO2-FeOy (by LPH in IVT RAN) UO2-SiO2-FeO CaO-UO2-FeO U-Zr-O systems (by LPH in IVT RAN)
Start eutectic composition measurement of a realistic complex corium mixture
Collaborators are kindly requested to provide German and French partner compositions of complex corium mixtures