## Slide 1: Progress Report on the ISTC project #1950.2 “Phase Diagrams for Multicomponent Systems Containing Corium and Products of its Interaction with NPP Materials” (CORPHAD.2)
Presented by S. Bechta
10th CEG-SAM Meeting
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
Project general information
Experimental matrix of CORPHAD Project
Scope of work in the 12-13 quarters
Zr-Fe-O system
UO2-SiO2 system
Complex corium mixture
Papers
Plans for the final period of the Project
Conclusions

## Slide 3: CORPHAD project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatome ANP, Germany
ISC RAS,
Russia
RRC Kurchatov Institute, Russia
SPb Electrotechnical State University, Russia
*) Should be finished in November 2006

## Slide 4: Experimental matrix of CORPHAD Project
    *) On agreement with collaborators the test was replaced by two experiments in the Zr-O-Fe system

## Slide 5: Scope of work in the 12-13 quarters

## Slide 6: Zr-Fe-O system: CORD44
VPA IMCC Fragment of the experimental thermogram showing the melt surface
    Tliq was measured three times: 1770 oC, 1780 oC and 1790 oC  Tliq=1780 oC
Tliq
Experimental objectives Determine liquidus temperature
Notes: In accordance wit the CORD33 posttest analysis the miscibility gap area is smaler than the calculated one, and the determined tie-line is on the boundary edge. For this reason it was decided to shift the CORD39 initial charge composition deeper into the gap.

## Slide 7: Zr-Fe-O system: CORD44
SEM/EDX
1cm
10 m
Cation composition of the melt quenched from liquidus temperature
30 m
Co-crystallization of refractory phases
 | Zr | Fe
mol. MeOx% | 80.7 | 19.3
 | Zr | Fe
mol. MeOx% | 66.3 | 33.7

## Slide 8: Zr-Fe-O system: CORD45
Experimental objectives Determine liquidus temperature
VPA IMCC Fragment of the experimental thermogram showing the melt surface
    Tliq was measured two times: 2505 oC and 2535 oC  Tliq=2520 oC
Tliq
Notes: In accordance wit the CORD33 posttest analysis the miscibility gap area is smaler than the calculated one, and the determined tie-line is on the boundary edge. For this reason it was decided to shift the CORD39 initial charge composition deeper into the gap.

## Slide 9: Zr-Fe-O system: CORD45
SEM/EDX
1cm
30 m
 | Zr | Fe
mol. MeOx% | 26.1 | 73.9
0.5 mm
ZrO2
ZrFe3(O)
Uniform ingot structure, Fe/Zr cation ratio - 1:3
The presence of ZrO2 globules concentrated in the samples rapidly quenched during melting indicates melt immiscibility
10 m
Melt sample

## Slide 10
Concluding remarks
Zr-Fe-O system
Tie line (Tmelt=2773K)
Tie line (Tmelt=2693K)
Miscibility gap was observed in CORD33 and CORD39 tests
Tliq=2655K (at.% 48.7 Zr – 19.7 Fe – 30.6 O)
Tliq=2763K (at.% 45.4 Zr – 25.8 Fe – 28.8 O)
CORD39
heavy “metallic” liquid, at.% 45.1Zr –31.5Fe –23.4O light “oxidic” liquid , at.% 44.4Zr –7.1Fe –48.5O
CORD33
light “metallic” liquid, at.% 51.5 Zr –24.3 Fe –24.2 O heavy “oxidic” liquid, at.% 47.9 Zr –4.9 Fe –47.2 O
Tliq=2793K (at.% 29.9 Zr – 61.1 Fe - 9 O)
CORD35
Depending on position of the figurative point in the miscibility gap, relation between the densities of oxidic and metallic liquids may differ (in CORD33, oxide density was higher than that of metal)
Compositions of liquids coexisting in the miscibility gap of CORD39 indicate that the gap is narrower than calculated using GEMINI-2/NUCLEA-05
2773K
CORD45
Tliq=2637K (at.% 48.7 Zr – 19.7 Fe - 30.6 O)
CORD44
Tliq=2053K (at.% 62.8 Zr – 18.6 Fe - 18.6 O)
Notes: In comparison with thermodynamic calculation the miscibility gap is a little narrower.

## Slide 11
Test objectives
UO2-SiO2 system
Published phase diagrams
1650
SiO2
80
60
40
20
UO2
1800
mol % SiO2
UO2 + SiO2
1400
1600
2000
2200
UO2 + L
L
SiO2
+
L
T, C
UO2 – SiO2 phase diagram by S.M. Lang et al., Nat. Bur. Stand., Circular 568. 1956
mol % SiO2
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2070±10
Phase diagram by Lungu S., Romanian J. of Physics. 1962. V. 7. N 4. P. 419
  Define whether the miscibility gap exists in the system or not
  Determine the miscibility gap boundary
  Evaluate monotectic temperature

## Slide 12
UO2-SiO2 system
  1 – pyrometer;
  2 – video cameras;
  3 – W heating tube;
  4 – Mo crucible
  Atmosphere – Ar + H2(4 vol. %)
  Total gas pressure – up to 3 atm
  Mass of the samples – 50-150 mg
  Stepwise heating
  Heating rate – 1-8C/min
  Exposure time – 1 min
  The error of pyrometer temperature
measurements is ±1 relative %
Experimental setup:
Galakhov microfurnace
Sample quenching
SEM/EDX analysis

## Slide 13
UO2-SiO2 system
Charge composition
Composition of all samples, % | UO2 | SiO2
mass | 50.7 | 49.3
mol | 18.62 | 81.38
Test characteristics

## Slide 14
UO2-SiO2 system
Macrostructure of quenched ingots
2000C
2080C
2140C
2140C
2200C
No quenching
GCORD 1-5
Stratification in the system above 2000°C

## Slide 15
UO2-SiO2 system
Microstructure of GCORD3 ingot
No interaction with Mo crucible in accordance with EDX data
Large quantity of gas pores in the layer corresponding to light liquid
Presence of heavy liquid globules in the light liquid
3 m
Heavy
liquid
Light
liquid
Mo crucible
1mm

## Slide 16
UO2-SiO2 system
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2080
mol % SiO2
2140
Initial composition
2070±10
First results
The miscibility gap was found to exist in the UO2 – SiO2 system
The miscibility gap boundary was estimated
The monotectic temperature was found to be in the 2000-2080C temperature range

## Slide 17
Complex corium mixture
Experimental objectives
Mass %, 54.2UO2 – 17.9ZrO2 – 13.7SiO2 – 7.6FeO – 3.8CaO – 1.5Cr2O3 – 1.3Al2O3
Charge composition
Determine liquidus temperature
VPA IMCC Fragment of the experimental thermogram showing the melt surface
Tliq = 2020 °C
Posttest analysis of samples and ingot is underway
Tliq

## Slide 18: Complex corium mixture
SEM/EDX
1cm
5 m
0.3 mm
 | UO2 | ZrO2 | SiO2 | CaO | AlO1.5 | FeO | CrO1.5
mass.% | 45.81 | 12.65 | 22.00 | 6.23 | 2.70 | 8.62 | 1.99
mol.% | 17.88 | 10.82 | 38.60 | 11.71 | 5.58 | 12.64 | 2.76

## Slide 19: CORPHAD Papers
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Defoort F., Gusarov V.V. Phase diagram of the ZrO2–FeO system. // J. Nucl. Mater. Vol. 348, p.p. 114-121 (2006)
Mezentseva L.P., Popova V.F., Almjashev V.I., Lomanova N.A., Ugolkov V.L., Bechta S.V., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V.V. Phase diagrams of the SiO2–Fe2O3(Fe3O4) systems in different gas atmosphere. // J. Europ. Ceram. Soc., prepared for publication
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Gusarov V.V. UO2–FeO phase diagram. // J. Nucl. Mater., 2006. in press
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V. V. Phase relations in the ZrO2--FeO system. // Russian J. Inorg. Chem. 2006. V. 51. N 2. P. 325-331. (Eng.)
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V. V. Phase and chemical transformations in the SiO2–Fe2O3(Fe3O4) systems at various oxygen partial pressure. // Russian J. Inorg. Chem. 2006. V. 51. N 1. P. 125-133. (Eng.)

## Slide 20: Plans for the final period of the Project
Completion of posttest analysis
Report on the U-Zr-O system including CORD41 (U-O system)
Report on the Zr-Fe-O system
Report on the U-Fe-O system
Report on the UO2-SiO2 system
Report on the complex corium mixture
Final report with the attachments
Deadline: March 2007

## Slide 21: Conclusions
Experimental part of the project is in progress
The Zr-Fe-O system was found to have a narrower miscibility gap than calculated using GEMINI2+NUCLEA05
Stratification in the UO2 – SiO2 system has been established, the first data confirm the diagram version of Lungu S. and Romanian J., 1962. The estimate of monotectic temperature and miscibility gap boundaries has been made
Liquidus temperature of the prototypic multi-component corium has been determined
The produced systematic data characterize the crystallization pattern of oxidic and metal-oxidic systems