## Slide 1: CORPHAD Programme Status
Presented by S. Bechta
5th CEG-CM Meeting
A.P. Alexandrov Research Institute of Technology
ISTC CORPHAD Project
#1950

## Slide 2: ISTC PROJECT # 1950.2
Phase Diagrams for Multicomponent Systems Containing Corium and Products of its Interaction with NPP Materials
( CORPHAD )
PHASE 1: 1 August 2001 - 30 April 2002
PHASE 2: 1 July 2003 - 30 June 2006

## Slide 3: CORPHAD project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatom ANP, Germany
ISC RAS,
Russia
RRC Kurchatov Institute, Russia
SPb Electrotechnical State University, Russia

## Slide 4: CORPHAD project focus
Project objective: Experimental study of phase diagrams of corium/NPP material mixtures
Reactor application
  Liquidus and solidus temperatures versus components concentration
  Temperature-concentration regions of the miscibility gap
  Coordinates of eutectic, dystectic and other characteristic points
  Solubility limits
Experimental data output
  Thermodynamic database optimisation
  Thermodynamic code validation
  Corium behaviour modelling

## Slide 5: CORPHAD phase 2 test matrix
Task | Composition | Temperature range, °C | Atmosphere | Measurement method | Priority level
 | UO2- FeO 4),5) | Up to 3000 | Argon |  | High
 | UO2X - FeOy 4),5) | Up to 3000 | Air | Galakhov | Middle-Low
 | ZrO2 – FeO 4) | Up to 3000 | Argon | Microfurnace | High
1 | UO2 – Cr2O3 5) | Higher than 2400 | Argon | IMCC VPA1) | Middle
 | SiO2– Fe2O3 | Up to 2000 | Air/Oxygen | DTA2) HTM3) | Middle
 | UO2– SiO2 | Up to 2500 | Argon |  | Middle-Low
 | (BaO,SrO) - UO2 4) | Up to 3000 | Argon |  | Low
 | Eutectic composition 4)5) of UO2– ZrO2-FeO |  | Argon |  | High
 | Eutectic composition5) of UO2+x – ZrO2-FeOy |  | Air | HTM | Middle
2 | U-O-Fe | Up to 2500 | Argon | IMCC VPA | High
 | Zr-O-Fe |  | Argon | DTA | High
 | U-O-Zr |  | Argon | Galakhov | High
 | UO2 – ZrO2-SiO2 (CaO)7) |  | Argon | Microfurnace | Middle
3 | Quaternary system Different composition in U-Zr-Fe-O system | Up to 2600 | Argon | IMCC VPA, Galakhov by air HTM | High
 | Corium oxidation kinetic test6): C-32 (U-Zr-O) | Up to 2600 | Argon replacement | IMCC | High
4 | Corium oxidation kinetic test: 90%C-32 + 10%Fe |  | by air |  | 
5 | Eutectic composition measurement of a prototype complex corium mixture | Up to 2500 | Argon | IMCC VPA DTA, Galakhov Mkrofurnace HTM | High
Notes: 1.Induction Melting in a Cold Crucible with Visual Polythermal Analysis; 2. Differential Thermal Analysis; 3. High Temperature Microscopy; 4. Determination of the solubility limit; 5.Determination of the eutectic composition and temperature; 6.Decision concerning these tests will be taken upon completing first three stages of the project; 7.For tests with CaO the decision will be based on ENTHALPY project results.
In progress
finished
proposed to cancel

## Slide 6: Work per each test
IMCC test preparation and carrying out; primary analysis of findings
Physico-chemical posttest analysis of samples
Samples preparation for the analyses by other methods, e.g. Galakhov furnace, HTM, DTA and DSC
Pre- and posttest calculations using thermodynamic codes
Integrated analysis and experimental data finalization

## Slide 7: Current list of activities
Task 1 – Investigation of binary systems
  ZrO2 – FeO system phase diagram
  UO2 – FeO system phase diagram
  SiO2 – Fe2O3 system phase diagram
Task 2 – Investigation of ternary systems
  First results of Tliq measurements for the system U – Zr – O

## Slide 8: Scope of the technical work during the 1st and 2nd quarter
New IMCC furnace designed for UO2 – FeO system has been built
High temperature thermoanalyser for simultaneous DTA/DCC has been installed:
  -SETSYS Evolution TAG 24 (up to 2400 C in inert atmosphere)
More sensitive XRF analyzer has been installed:
  - SPECTROSKAN MAKS – GV (elements from Na to U)
TIGEL facility has been modernized in RRC KI

## Slide 9: The scope of studies carried out during the 1st and 2nd quarters of CORPHAD Project

## Slide 10: 3rd CORPHAD Project Meeting
List of presentations:
Project status
Phase diagram of the ZrO2 – FeO system
Phase diagram of the UO2 – FeO system
Measurement results of liquidus temperature in the U-Zr-O system
Phase diagram of the SiO2 – Fe2O3 system
Experimental matrix proposals for the period until next meeting
Preliminary melting point measurements of the U-Zr-O system using a modified set-up with Laser Heating

## Slide 11: Phase diagram of the ZrO2 – FeO system
T, С
FeO 20 40 60 80 ZrO2
mass %
1300
1500
1700
1900
2100
2300
2500
2700
1300
1500
1700
1900
2100
2300
2500
2700
1100
1100
1172
2347
2710
1377
IVTANTHERMO
DTA
<1172
>1800
SEM/EDX
W.A.Fischer, A.Hoffman, Archiv Eisenhüttenw.,
28 №739, 1957
Liquid
Galakhov microfurnace
CCVPA
t-ZrO2
c-ZrO2
m-ZrO2
CCVPA New technique

## Slide 12: Phase diagram of the UO2 – FeO system
The error of pyrometer temperature measurements is ±1 relative %
The error of FeO concentration measurements is ±3 relative %
FeO/UO2 ss
FeO/UO2 ss +liquid
liquid

## Slide 13: Phase diagram of the SiO2 – FeOy system
FeO
10
Fe2O3
SiO2
20
30
40
50
60
80
90
10
20
30
40
50
60
70
80
90
10
20
30
40
50
60
80
90
mass %
eutectic composition:
79.55 mass% Fe3O4 according Muan diagram
86.50 mass% Fe3O4 according present investigation
hematite
magnetite
wustite
fayalite
FeOFe2O3
cristobalite
iron
2 FeOSiO2
1500
1400
1300
1200
2
4
12
13
14
2
2 – 92 mass% Fe2O3
4 – 90 mass% Fe2O3
12 – 89 mass% Fe2O3
13 – 88 mass% Fe2O3
14 – 87 mass% Fe2O3
– air
– oxygen

## Slide 14: Phase diagram of the SiO2 – Fe2O3 system
Eutectic point:
1470C
89 mass% Fe2O3
1440C
88 mass% Fe2O3
1500
1600
1800
1400
1700
T, С
Fe2O3 20 40 60 80 SiO2
mass %
1500
1600
1800
1400
1700
1723
1539
Liquid
(Fe3O4)
1470
1535
Experimental error - 25C
HTM
DTA
1440
1375
6 Fe2O3  4 Fe3O4 + O2
DTA (decomposition)
IVTANTHERMO
New compositions

## Slide 15: Fusion diagram of Fe3O4-SiO2 system
IVTANTHERMO
New compositions
1400
1500
1700
1300
1600
T, С
Fe3O4 20 40 60 80 SiO2
mass %
1400
1500
1700
1300
1600
1723
Two
liquids
1430
1550
1597
Quenching

## Slide 16: Results of liquidus temperature in the U-Zr-O system

## Slide 17: Future plans
Concussions and recommendations of the 3rd CORPHAD Project Meeting
1) Concerning Task 1 it was agreed to delete the low and middle priority systems UO2+-x –FeOy , UO2-Cr3O3 and (Ba, SrO)-UO2 from the test matrix. This was accepted as it had been agreed previously that the high-priority systems should be studied in a more profound and detailed manner.
2) As regards the UO2-SiO2 system, it was convened to keep it for the time being, check the available phase diagram information and their quality before making a final decision. It will be decided at the next meeting whether some tests are valuable to be carried out, possibly in the UO2-rich domain.
3) Possible investigations of the “ternary” systems of Task2 (UO2-ZrO2-SiO2), UO2-ZrO2-CaO) will be discussed and decided after the completion of Task 1.

## Slide 18: Future plans
To complete the prossesing of experimental data for the UO2 – FeO system
Deadline: October 2004
To perform 2 IMCC tests for the ZrO2 – FeO system Deadline: October 2004
To perform 2 tests for the U - O – Zr system in RRC KI Deadline: October 2004
To prepare reports on the diagrams of UO2 – FeO; ZrO2 – FeO; SiO2 – Fe2O3 Deadline: October 2004
To perform a test on determining eutectics composition of the UO2 - ZrO2 – FeO system
Deadline: end of 2004
To prepare tests in the U – O – Fe system
Deadline: end of 2004