## Slide 1: Concretes for MCCI Christophe JOURNEAU

## Slide 2: Summary of the VULCANO 2D Tests

## Slide 3: Summary of CCI 1,2,3
Test
CCI
-
1
CCI
-
2
CCI
-
3
Corium load
composition
61 wt.% UO
2
, 25% ZrO
2
,
6.4%
SiO
2
, 1.2% CaO,
0.4%
Al
2
O
3
, 0.1%
MgO,
5.9%
Cr(evaporating).
60.6 wt.% UO
2
, 24.9
% ZrO
2
,
3.4%
SiO
2
, 3.1% CaO,
0.4%
Al
2
O
3
, 1.1%
MgO,
6.4%
Cr(evaporating).
56 wt.% UO
2
, 23% ZrO
2
,
11.1%
SiO
2
2.2% CaO,
0.6%
Al
2
O
3
, 0.1%
MgO,
6.4%
Cr(evaporating).
Corium mass
400 kg
400 kg
400 kg
Concrete
chemical
composition
(major
constituents,
after dry
ing)
69 wt. % SiO
2
13.5 % CaO
4% Al
2
O
3
,
0.7% MgO
4.2% CO
2
3.7% H
2
O
28.3 wt. % SiO
2
26 % CaO
3.5% Al
2
O
3
,
9.6% MgO
21.4% CO
2
6.1% H
2
O
61 wt. % SiO
2
17 % CaO
3.6 % Al
2
O
3
,
0.9 % MgO
10 % CO
2
3.8% H
2
O
Initial
Temperature
~2325 K
~2200 K
~2225 K
Test Duration
(before
flooding)
2 hrs
5 hrs
2 hrs
Ratio of
horizontal to
vertical
ablation
Large lateral ablation bursts
~ 1:1
~7:1

## Slide 4: Recommendations for VNIIEF
“CEG-SAM members have proposed to use Limestone-Common Sand concrete for the preliminary test (since this type of concrete is linked to isotropic ablation, any artifact in the heat flux distribution will be detected) and siliceous concrete (for which it must be verified that the observed ablation anisotropy is not an artifact due to experiment size or heating system).”

## Slide 5: Composition recommended for pretest
        Limestone concrete for medium-scale pre-test