## Slide 1: EVAN ISTC Project # 3345: Source Term Assessment at Ex-Vessel Stage of Severe Accident Task 2: Experimental study of FP release from molten corium pool
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
Progress meeting of EVAN ISTC project
Budapest, Hungary, March 4, 2008

## Slide 2: Contents
Objectives
Test matrix
Methodology of evaporation study and post test analysis
Installation:
- Induction furnace
- Gas-aerosol sampling system
EVAN-1FP test procedure
EVAN-1FP test results:
- Pyrometer readings and melt surface temperature during the 1st part of the test
- Pyrometer readings and melt surface temperature during the 2nd part of the test
- Evolution of corium oxidation index
- Crucible and ingot after the test
- Mass balance of corium
- Composition of aerosol samples in comparison with melt composition
- Aerosol transport losses
- Aerosol mass release rates - Element specific release rates
- Temperature dependence of release rates at C 70 and C 85
- Influence of oxidation index on the release rates
- Aerosol phase composition
- Aerosol size distribution
- Uranium species partial pressure
Thermodynamic modeling by Gemini2/NUCLEAiv-07_1
Conclusions

## Slide 3: Objectives
Determination of release rates of FP and corium components at different melt surface temperatures and corium oxidation indexes Cn
FP simulants: Ba, Sr, Ce, La, Mo, Ru
Corium components: U, Zr
Сn=100(MZr, - MZr,met)/ MZr, % MZr, – integral mass of Zr in oxidized and free form;
MZr,met – mass of Zr-free

## Slide 4: Test matrix
Pr1-EV1: pretest carried out for facility functional check and determination of melt oxidation rate
Pr2-EV1: pretest carried out for preparation of the crucible charge of high density (m=1390 g, grading 200-300 µm)
EVAN-1FP: main test
BaO and SrO were added in the form of their zirconates

## Slide 5: Method of evaporation study
Mass transfer (dynamic) method: saturation of carrier gas by the vapour of the studied substance at constant temperature and gas flow rate
Carrier gas in
Gas\aerosol mixture out
Substance
T const
Flow reactor
Methods of transferred mass determination:
Weighting
Radiotraces
Chemical analysis of solid depositions
…

## Slide 6: Methods of post test study of samples (1)
XRF, EDX, Chemical analysis
(U+4, U+6 and Zrfree)
ICP MS
Errors of measurements (rel. %):
XRF - 5%
ChA - 5%
ICP MS -10%(Sr, Ba) and 50% (Ce, La, Ru, Mo)
EDX - 3- 5 %
Analysis of solid depositions and corium ingot

## Slide 7: Methods of post test study of samples (2)
XRD → phase composition
(qualitative)
Small angle light scattering → aerosol size distribution
(Error: 2 rel. %)
MICROSIZER-201A setup
Range of detectable aerosols: 0.2-300 µm
Laser wave length: 0.63 µm
Detector: diode target array
Registration channels: 38
Sample preparation: ultrasonic dispersion
Dispersion cell volume: 150-1000 ml
Ultrasonic frequency: 50 kHz
Power of ultrasonic pulser: up to 200 W
PC
Ultrasonic disperser
Pump
Mixer
Optical cell
Lens
He
-
Ne
Laser
Sensor array
Amplifier

## Slide 8: Methods of post test study of samples (3)
High temperature Knudsen MS → partial pressures of species in vacuum
(Error: 10 rel. %)
Knudsen cell
1 – Lid
2 – Cathodes
3 – Vessel
4 – Support bar
5 – Ports for pyrometry

## Slide 9: Induction furnace for the EVAN-1FP test (1)
1
2
3
4
5
6
7
8
9
1 - Lid 2 - Pyrometer shaft 3 - Quartz partition 4 - Quartz vessel 5 - Cold crucible 6 - Corium melt 7 - Inductor coil 8 - Corium crust 9– Bottom calorimeter
Reduction of aerosol transport losses:
Molten pool is placed in the top of cold crucible for reduction of cold surface area
Quartz partition is separating above the melt area from the furnace internals
Pyrometer shaft was moved out from the furnace during sampling (only short-term temperature measurements at the beginning and the end of every regime)

## Slide 10: Induction furnace for the EVAN-1FP test (2)
Pretest DNS of gas flow structure: Q = 10 l/min, Ar:O2=80:20
Gas temperature and velocity vectors:
No quartz partition With quartz partition
Effective aerosol capture by axial upward gas flow
Reduction of recycling zone and area of furnace cold surfaces, which are in contact with hot gas-aerosol flow

## Slide 11: Gas-aerosol sampling system
1 - Gas canisters 2 - Gas flow regulators 3 - Gas mixing unit 4 - Electrochemical oxygen sensors 5 - Induction furnace 6 - F2: large exposition aerosol filter (replaceable) 7 - F1: small exposition analytical filter (replaceable) 8 - Bubblers 9 - Gas flow meter 10 - Fun 11 - Vibrator 12 - Main line (electrochemically polished copper tube)
13 -Three-way valve
F1 filters were often replaced, while F2 filters were continuously used during every regime
Electromechanical vibrator was installed for reduction of aerosol depositions in the main line
Two bubblers (the first one with 0.1mol K2S2O8 solution and the second – with 1mol KOH) were used for adsorption of RuO4

## Slide 12: General procedure of EVAN-1FP test (1)
Molten pool formation in argon, power in the melt control in order to reach specific melt surface temperature
Melt sampling
Short-term temperature measurements
Exposition of the molten pool in steady-state with continuous aerosol sampling
Change of melt surface temperature, it’s measurements and repetition of aerosol sampling
Sampling from bubblers
Supply of Ar/O2 mixture into the furnace and corium oxidation up to specific Cn
Control of melt surface temperature
Repetition of melt, aerosol and bubblers sampling
Heating disconnection, melt crystallization and ingot cooling in argon
! It was not possible to maintain equal melt surface temperature at different Cn, because it’s increase resulted in higher liquidus temperature of corium

## Slide 13: General procedure of EVAN-1FP test (2)
Steady-state( ) and transient ( ) regimes
Aerosols were collected at different melt surface temperatures of C 70 and C 100 corium

## Slide 14: EVAN-1FP test results (1)
Pyrometer readings and melt surface temperature during the 1st part of the test
EVAN-1FP
(1st part)

## Slide 15: EVAN-1FP test results (2)
Pyrometer readings and melt surface temperature during the 2nd part of the test
EVAN-1FP
(2nd part)

## Slide 16: EVAN-1FP test results (3)
Mass of adsorbed oxygen and evolution of corium oxidation index
Pr1-EV1
EV1-1
EV1-2
Pr1-EV1
1st phase: 9.3 ±0.3 (О2 mg) /s
2nd phase: 7.3 ±0.2 (О2 mg) /s
EV1
15.0 ±0.8 (О2 mg) /s
Different melt oxidation rate in EV1 and Pr1-EV1 due to the change of furnace hydrodynamics (quartz partition installation)
Different melt oxidation rate in the 1st and the 2nd phase of Pr1-EV1 due to the change of furnace hydrodynamics (pyrometer shaft was moved down in the 2nd phase)
Kinetics of melt oxidation is controlled by the supply of oxidizer to the pool surface

## Slide 17: EVAN-1FP test results (4)
Ingot surface
Aerosol depositions inside the lid and partition
Aerosol depositions on the cold crucible
Crust above the melt
Crucible and ingot after the test
Metal inclusion in the oxidic ingot
Mass: 5.1г
Composition, mass % (XRF): 88.8 - Ru; 11.0 - Mo; 0.2 – Zr
Liquid immiscibility indication for the final C 100 composition
What was in C 70 and C 85 melt?
Shrinkage pore
1 cm

## Slide 18: EVAN-1FP test results (5)
Mass debalance corresponds to the mass of absorbed oxygen
Element specific debalance does not exceed 1.5 rel.% for U, 4.5% for Zr, 4.0% for Sr, 1.9% for Ba, 3.5% for Ce, 5.9% for La, 0.2% for Ru and 0.4% for Mo
*-ZrO2 used for Ba and Sr zirconate preparation and for the cold crucible insulation
Mass balance of corium

## Slide 19: EVAN-1FP test results (6)
Composition of aerosol samples in comparison with melt composition
Aerosols are enriched in U and depleted in Zr in comparison to the melt composition
Reduction of Sr/Ba and increase of Mo releases following Cn increase
No indication of RuO4 release according to results of ICP MS of samples taken from the bubblers

## Slide 20: EVAN-1FP test results (7)
Aerosol transport losses
Total aerosol mass of 64.38 g
Significant transport losses 60%
The transport losses were taken into account by the coefficient:
        where mMAF, mAAF and MoΣ are masses of aerosols collected in F1, F2 filters and integral aerosol mass, respectively
Main line
Three-way valve
F1 filters
F2 filters
Cold crucible
Quartz partition and vessel
Aerosol mass (g) collected in
Thus the transport losses were assumed to be proportional to integral aerosol mass.
Aerosol mass release rates were calculated as:
        where Δτα and S are exposition of a-regime and melt surface area

## Slide 21: EVAN-1FP test results (8)
Aerosol mass release rates
Significant increase of aerosol release rate at elevated temperatures
Influence of oxidation index is suppressed by temperature effect

## Slide 22: EVAN-1FP test results (9)
Element specific release rates
Increase of aerosol release rate at elevated temperatures
Influence of oxidation index is suppressed by temperature effect
Uranium
Sr, Ba, Mo, Zr
La, Ce, Ru

## Slide 23: EVAN-1FP test results (10)
Temperature dependence of release rates at C 70 and C 85
Uranium
Strontium
Barium
Molybdenum

## Slide 24: EVAN-1FP test results (11)
Influence of oxidation index on the release rates at 2652oC
Significant reduction of U, Zr and FP release rates following corium oxidation (except Mo)
Ruthenium release rate was not sensitive to melt oxidation index in the range C 70…100
Uranium
Sr, Ba, La, Ce
Ru, Mo

## Slide 25: EVAN-1FP test results (12)
#F1
С70
С85
С100
С85-100
С70-85
18
21
50
56
62
40
35
24
9
30
35
40
45
50
55
60
65
70
75
Aerosol phase composition
2Θ
UO2(ASTM: 73-1715) UO2(ASTM:13-225) UO3(ASTM:31-1416) U3O8(ASTM:31-1425)
SrUO4(ASTM: 75-1946)
Phases identified by XRD: - UO2 - based solid solution in the aerosols released in inert conditions
- UO3, U3O8, UO2 and SrUO4 phases (the last two in small quantities) in the aerosols released in oxidizing condition

## Slide 26: EVAN-1FP test results (13)
F1 №5
(I regime), Tmelt=2595C, C 70
F1 №9
(II regime), Tmelt=2535C, C 70
F1 №9
(II regime), Tmelt=2535C, C 70
F1 №64
(VIII regime), Tmelt=2652C, C 100
Aerosol size distribution
4 main ranges of aerosol sizes: <1 µm, 1.59-3.63 µm, 3.63-5.49 µm, 9.54-12.6 µm
Temperature effect
Influence of oxidation index
Increase of fine particle fraction and reduction of agglomerate fraction with temperature increase
Increase of agglomerate fraction (9.54- 12.6 µm) after melt oxidation

## Slide 27: EVAN-1FP test results (14)
Effect of atmosphere
Significant increase of fine aerosol fraction in oxidizing atmosphere
Practically no agglomeration of particles in oxidizing atmosphere
Aerosol size distribution
F1 #35 (V regime), Ar
F1 #50 (VII regime), Ar/O2

## Slide 28: EVAN-1FP test results (15)
Integral partial pressure of uranium species determined by HT MS
About the same effect of Cn in vacuum: higher values of integral partial pressures of U at smaller Cn
Conditions of HT MS of corium samples:
Sample mass  20 mg
Error of sample weighting ±0.1 mg
Reference sample for
pressure calibration gold
High vacuum
Integral pressure of
all species less than 13 Pa
- Exposition at every temperature 60 min

## Slide 29: Thermodynamic modeling by Gemini2/NUCLEAiv-07_1 (1)
Comparison of release data of the I regime of the test
Volume of gas to be in local equilibrium with the melt was determine from oxidation régimes (as the volume of gas, from which all oxygen was absorbed)
Reasonable agreement in U, Zr, Ba releases, but discrepancy in Ru (liquid immiscibility?) and Sr (salting-out?)
Tmelt=2595C, C 70

## Slide 30: Thermodynamic modeling by Gemini2/NUCLEAiv-07_1 (2)
Evolution of phase composition versus temperature
No miscibility gap at 2850-2950 К. Solid HCP Ru-containing phase forms during crystallization of the last remaining liquid. Contradiction with metal inclusion location
Final C 100 corium

## Slide 31: Conclusions (1)
The following qualitative effects have been detected:
Decrease of the evaporation rate of melt components and fission products, excluding molybdenum, after the increase of the corium oxidation index. Therefore, melt oxidation in the catcher has in general a positive influence on the radiation situation in the containment
Strong adhesion of the chemically prototypic corium aerosols, especially to cold metallic surfaces. This also reduces the release of aerosols into atmosphere of the containment, but may influence efficiency of such safety systems as SPOT GO/PG (Passive Heat Removal System from Containment/Steam Generator), hydrogen catalytic recombiners, etc.
Kinetics of melt oxidation is controlled by the supply of oxidizer to the pool surface, i.e., depends on characteristics of the steam-gas mixture natural convection in the reactor at the in-vessel stage of a severe accident, or in the reactor pit at the ex-vessel stage

## Slide 32: Conclusions (2)
Qualitative effects (2):
The submicron particles fraction in the release is noticeable. Their inertia and gravitational deposition are weak. This fraction keeps increasing during the melt surface oxidation. Characteristics of the aerosol release during melt oxidation at its interaction with sacrificial material have not been determined yet
There exists evidence that ruthenium and a part of molybdenum, which concentrate in the metallic melt, stratify in molten corium C 100. Under conditions of the test, no release of gaseous RuO4 was measured until free zirconium in the melt has oxidized completely

## Slide 33: Conclusions (3)
The obtained quantitative results can be used for the development and verification of models and codes which describe the release of FP during a severe accident.
These results include:
Correlations of the element release rates with the melt temperature and oxidation index
Aerosols chemical and phase composition
Dispersion and masses of aerosols collected along the facility duct at different distances from the release source
For verification use of the data, the report offers the facility’s design and geometry, in particular, of its gas-aerosol duct, as well as characteristics of the gas-aerosol flow