## Slide 1: EXPERIMENTAL STUDY OF AEROSOLS DEPOSITION AND RESUSPENSION IN THE PRIMARY CIRCUIT EQUIPMENT Mikhail Lebedev (JSC «NPO CKTI») EVAN ISTC Project Progress meeting
March 04 2008
Budapest, Hungary
WP3
TASK 4

## Slide 2: Contents
The goal of the experimental study
Experimental set-up
Measurement technology
Results (liquid and solid particles)
Summary
WP3
TASK 4

## Slide 3: Matrix of performed experiments for phase №1 and №2
Test | Velocity for deposition phase, m/s | Velocity for resuspension phase, m/s | Particle size d, mkm | Temperature, K | Test Purpose | Aerosol particles parameters | Orientation and surface parameters of working section
EVAN–№3345 AT 1.1 | 33,8 | None | 0.2 – 5 | 300 | Investigation of transport and deposition rate of liquid aerosol particles from gas flow towards the wall | Liquid JEM PRO-SMOKE high density (SP MIX) | Vertical pipe with 98 mm diameter, height ~6 m (upwards flow), steel 10ХСНД
EVAN–№3345 AT 1.2.1 | 39,6 | None | 0.2 – 28 | 300 |  |  | 
EVAN–№3345 AT 1.2.2 | 33,8 |  |  |  |  |  | 
EVAN–№3345 AT 1.2.3 | 24,8 |  |  |  |  |  | 
EVAN–№3345 AT 1.2.4 | 6,5 |  |  |  |  |  | 
EVAN–№3345 AT 2.1 | 20 | 65 | 0.3 – 10 | 320 | Investigation of deposition and resuspension of solid aerosol particles (prototype and preliminary tests) | Solid aerosol particles of NH4Cl | Vertical pipe from stainless steel with diameter 50mm, height ~5 m,
 |  | 105 |  |  |  |  | 
EVAN–№3345 AT 2.2 | 30 | 75 |  |  |  |  | 
 |  | 105 |  |  |  |  | 
EVAN–№3345 AT 2.3 | 38 | 75 |  |  |  |  | 
 |  | 105 |  |  |  |  | 

## Slide 4: Aerosol test facility ATF1

## Slide 5: Aerosol test facility ATF2

## Slide 6: Aerosol test facility ATF3

## Slide 7: Aerosol test facility ATF4

## Slide 8: Aerosol test facility ATF5

## Slide 9
General view of the test structure

## Slide 10: Measurement techniques (1)
Velocity related parameters of the carrying media and disperse phase of the flow
Hot-wire anemometer
Laser Doppler anemometer
Spectral transparency (extinction) method
Forward scattering (Fraunhofer diffraction) method
Particle counter
Size and concentration of the disperse phase
(liquid aerosol)

## Slide 11: Measurement techniques (2)
Size and concentration of the disperse phase
(solid aerosol)
Chemical
analysis
Weighting
of trials
Micro
Photography

## Slide 12: Hot-wire anemometer probe
General view
Sensors: 5 mm gilded wolfram wires

## Slide 13
TRAVERSING SYSTEM
Doppler
signal
processor
Sending
optics
Laser
PC
Receiving
module
Aperture
v
Single-component Laser Doppler Anemometer (LDA)

## Slide 14
Workbench of LDA system
Running of the profile measurement procedure
Resulting profile of measured velocity and turbulence intensity

## Slide 15: Spectral transparency method: realization
Analog to digital
converter
Sending
optics
Laser
PC
Receiver
(PM tube)

## Slide 16
Forward scattering method
- first-order Bessel function of the first kind
1. Light source
2. Jet
3. Objective
4. Optical fiber
5. Light register
6. Indicating gage
7. Power unit

## Slide 17
Pulse amplitude
analyzer
Sending
optics
Laser
PC
Receiving
module
Individual particle counter (sizer)

## Slide 18
Axial velocity profile
Root-mean-square pulsations of the axial velocity profile
1 – level 3, Uav=33.8 m/s, EVAN-№3345АТ1.2.2;
2 – level 3, Uav=39.6 m/s, EVAN-№3345АТ1.2.1;
3 – level 3; Uav=26.9 m/s,
4 – level 3, Uav=33.0 m/s.
Measurement with the hot-wire anemometer (ATF3)

## Slide 19
Axial flow velocity = 24.6 m/s, level 2, EVAN–№3345 AT 1.2.3 | 
Mean axial velocity profile | Turbulence intensity profile
LDA measurements: axial air velocity (ATF3)

## Slide 20
Air/drop velocity comparison (ATF2)
Axial flow velocity  6 m/s, level 1
Axial flow velocity  6 m/s, level 3
0
1
2
3
4
5
6
7
0
10
20
30
40
50
60
70
80
90
100
Gaging point, mm
Mean velocity value, m/s
ROSCO
PRO ULF 1037
drop
air
0
1
2
3
4
5
6
0
10
20
30
40
50
60
70
80
90
100
Gaging point, mm
Mean velocity value,
m/s
PRO ULF 1037
ROSCO
drop
air

## Slide 21: Velocity pulsation (ATF3)

## Slide 22: Aerosol transport process: measurement results

## Slide 23: Aerosol transport process: measurement results
Distribution of counting concentration, surface and volume of liquid particles

## Slide 24: Aerosol transport process: measurement results
0
0,4
0,8
1,2
1,6
2
2,4
0
10
20
30
40
50
60
70
80
90
Gaging point, mm
Relative particles rate
Level 1
Level 3
Simmetrical
values
Level 3
Measurements
Concentration profiles comparison

## Slide 25: Aerosol transport process: measurement results
0,101
0,103
2,10
2,40
4,50
5,5
6,5
EVAN–№3345
AT 1.2.4
0,110
0,112
0,600
0,500
1,10
5,5
24,8
EVAN–№3345
AT 1.2.3
0,141
0,143
0,480
0,250
0,730
5,5
39,6
EVAN–№3345
AT 1.2.1
0,195
0,198
0,750
0,750
1,50
5,5
33,8
EVAN–№3345
AT 1.2.2
0,182
0,185
0,700
4,10
4,80
0,52
33,8
EVAN–№3345
AT 1.1
g/(m2s)
g/s
g/m3
g/m3
g/m3
mkm
m/s
F
M
C1-C2
С2
С1
Particle size
Um
Test
3,03E-02
1,21E-01
2,63E-01
1,50E-01
3,42E-02
m/s
Vd

## Slide 26: Solid particles study: test section
1 ÷ 6 – test section elements; 7 – dotted precipitators; 8 – static pressure taps;
9 – connection clip

## Slide 27: Solid particles study: test section
Connection clip

## Slide 28: Solid particles study: test section
Dotted precipitator

## Slide 29: Solid particles study: test section
Element for optical measurements
At the top - optical windows, at the bottom – points of optical fibers installation

## Slide 30: Solid particles study: test section
Measuring section

## Slide 31: Solid particles study: generator
Generator of sal ammonia design

## Slide 32: Solid particles study: generator

## Slide 33: Solid particles study: generator

## Slide 34: Solid particles study: generator

## Slide 35: Solid particles study: measurement techniques
. Block diagram of 3-cascade impactor
BASE PLATE-1 BASE PLATE-2 BASE PLATE-3
Aerosol from the volume under investigation

## Slide 36: Measurement with the hot-wire anemometer (ATF4)
Results of velocity profiles measurements
1 – wav =56,27 m/s; 1 – wav =47,74 m/s;
3 – wav =20,12 m/s (EVAN-№3345 AT 2.1);
4 – wav =8,52 m/s; 5 – wav =29,98 m/s (EVAN-№3345 AT 2.2)

## Slide 37: Optical measurements
0,00
0,20
0,40
0,60
0,80
1,00
1,20
1,40
0:00:00
0:14:24
0:28:48
0:43:12
Time from generator starting
Mass concentration , g/m3
Measured value
Corrected value
Mass sal ammonia particles concentration
EVAN–№3345 AT 2.2.4

## Slide 38: Impactor measurement
Aerosol powder. Test EVAN–№3345 AT 2.1

## Slide 39: Impactor and filter measurements
Time dependence of aerosol concentration, EVAN–№3345 AT 2.3

## Slide 40: Chemical measurement
Surface density of sal ammonia layer
Overall diagram of deposition tests
Tests AT 2.2.1, AT 2.2.2, AT 2.2.3

## Slide 41: Mass balance
Regime
Balance
value,
g
Loading of generator
g
20 m/s
501,20
529,57
30 m/s
531,50
559,54
38 m/s
451,72
489,88
Mass of aerosol, fed in the test section

## Slide 42: Microphotography
Aerosol structure on the base plate of stainless steel, 1-t cascade of impactor
(regime АТ 2.2.3)

## Slide 43: Microphotography
Aerosol structure on the base plate of stainless steel, 2-d cascade of impactor
(regime АТ 2.2.3)

## Slide 44: Microphotography
Aerosol structure on the base plate of stainless steel, 3-d cascade of impactor
(regime АТ 2.2.3)

## Slide 45: Microphotography
Deposit structure on precipitators

## Slide 46
WP3 Summary TASK 4
All experiments according to the matrix have been executed
Deposition velocities of liquid aerosol size of 0,2 … 14 microns in the cylindrical vertical channel in a range of Reynolds numbers from 10000 to 240000 have been obtained
Parameters of carrier gas flow (average velocity, velocity fluctuations and fluctuation frequencies) in the cylindrical vertical channel in diameter of 98 mm have been obtained
Particle size spectra and particle concentrations along the channel (D=98 мм) are obtained
A novel experimental setup for investigation of aerosol deposition and resuspension has been constructed
The design of the ammonium chloride aerosol generator based on use of reversible chemical reaction (dissociation - recombination) has been developed
Deposition intensities of ammonium chloride aerosol in size of 0,15 to 5 microns in the vertical channel in diameter of 50 mm have been obtained under air velocity from 20 to 38 m/s. It has been found out that deposition intensities depend on two simultaneous processes – deposition and resuspension
Resuspension velocities of ammonium chloride aerosol in the vertical channel in diameter of 50 mm have been obtained under air velocities from 65 to 105 m/s

## Slide 47: THANK YOU FOR THE ATTENTION!
Presentation is over

## Slide 48: Измерительная система ЛДА

## Slide 49
Дифференциальная схема ЛДА с ячейкой Брэгга и расширителем пучков лазера
1 - лазер; 2,4 - разделитель пучков; 3 - ячейка Брэгга; 5 - расширитель пучков;
6 - фронтальная линза; 7 – рабочий участок; 8 - приемная линза ФП; 9 - ФЭУ.

## Slide 50
OPTICAL METHODS FOR THE FRACTIONAL ANALYSYS
Extinction method
Particle counter method (PCM)

## Slide 51
В работе реализованы три оптических метода исследования фракционного состава двухфазного потока:
- - метод спектральной прозрачности (СП) для исследования капель тумана (со средним размером капель порядка микрона);
- - метод «малых углов» (МУ) для исследования фракционного состава крупных капель (средний размер капель более одного микрона);
- - счетный метод для измерения размеров и профиля концентрации частиц.
ОПТИЧЕСКИЕ МЕТОДЫ ФРАКЦИОННОГО АНАЛИЗА

## Slide 52
Схема компоновки комплекса измерения фракционного состава потока

## Slide 53
Отработка конфигурации входной части канала. Расход воздуха через канал 0,04 м3/с
Измерения термоанемометром
Профиль продольной скорости
Среднеквадратичные пульсации продольной скорости
1 – уровень 2, цилиндрическое входное устройство;
2 - уровень 2, без входного устройства;
3 - уровень 3, соосно с каналом установлена входная камера с тороидальным коллектором;
4 - уровень 3, отсутствие соосности входной камеры с каналом;
5 - уровень 3, соосно с каналом установлена входная камера без тороидального коллектора;
6 – уровень 3, то же, что и в случае 3.

## Slide 54
Режим 1,5 м/c | 
Результаты измерений на уровне 1 | 
профиль средней осевой скорости | профили интенсивности турбулентности
Результаты измерений на уровне 2 | 
Измерение кинематических характеристик потока с использованием
в качестве трассеров частиц дымогенератора размерами 1мкм(схема № 1)

## Slide 55
Измерение кинематических характеристик потока с использованием
в качестве трассеров частиц от генератора тумана ROSCO 1500 (схема № 1)
Режим 1,5 м/c | 
Результаты измерений на уровне 1 | 
профиль средней осевой скорости | профили интенсивности турбулентности
Результаты измерений на уровне 2 | 

## Slide 56
Измерение кинематических характеристик потока с использованием в качестве трассеров частиц от генератора тумана ROSCO 1500 (схема № 1)
Режим 6 м/c | 
Результаты измерений на уровне 1 | 
профиль средней осевой скорости | профили интенсивности турбулентности
Результаты измерений на уровне 2 | 

## Slide 57
Наложение эпюр скорости потока для двух видов частиц: тумана, генерируемого ROSCO, с диаметром капель порядка 1 мкм, и аэрозоли, созданной генератором аэрозольных частиц
PRO ULF 1037, с диаметром капель порядка 12 мкм (схема № 2)
Режим 6 м/c
Результаты измерений на уровне 1
Результаты измерений на уровне 3
0
1
2
3
4
5
6
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Среднее значение скорости,
м/с
PRO ULF 1037
ROSCO
0
1
2
3
4
5
6
7
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Среднее значение скорости, м/с
ROSCO
PRO ULF 1037

## Slide 58
Измерение осевой и тангенциальной составляющих скорости на уровне 2. В качестве трассеров использовались частицы тумана
Режим 6 м/c. Параметры осевой скорости | 
Параметры тангенциальной составляющей скорости | 
профили средней осевой скорости | профили интенсивности турбулентности

## Slide 59
Режим 6 м/c | 
Результаты измерений на уровне 1 | 
профиль средней осевой скорости | профили интенсивности турбулентности
Результаты измерений на уровне 3 | 
0
1
2
3
4
5
6
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Среднее значение скорости,
м/с
0
1
2
3
4
5
6
7
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Среднее значение скорости,
м/с
0
10
20
30
40
50
60
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Интенсивность
турбулентности, %
0
2
4
6
8
10
12
0
10
20
30
40
50
60
70
80
90
100
Координата измерения, мм
Интенсивность турбулентности,
%
Parameters of the Скорость дисперсной фазы (стенд по варианту 2)

## Slide 60
Измерение размеров аэрозоля – режим 1
Скорость несущей среды (м/с) | Массовая концентрация дисперсной фазы (г/м3)
6,5 | 6,5

## Slide 61
Измерение размеров аэрозоля– режим 3
Скорость несущей среды (м/с) | Массовая концентрация дисперсной фазы (г/м3)
1,5 | 6,0

## Slide 62
Массовая концентрация аэрозоля – режим 3
Скорость несущей среды (м/с) | Массовая концентрация дисперсной фазы (г/м3)
1,5 | 6,0

## Slide 63
Изменение дисперсности по высоте канала
Скорость V=6.5м/с, массовая концентрация m=9г/м3)

## Slide 64
Velocity of deposition
Оценка скорости осаждения по результатам измерения концентрации

## Slide 65
Light extinction law (Bouguer law)
Angular distribution of scattered light
Particle sizing through light scattering

## Slide 66
Computed relationship for particle sizing
(n=1,4135, r1=0.42 mм, r2=0,66 mм)
Spectral transparency method: basics

## Slide 67
Measurement of aerosol mass concentration (R1)
Air velocity [meter/s] | Mass concentration of liquid [g/m3]
6,5 | 6,5

## Slide 68
Axial flow velocity  3 m/s, level 2 | 
Mean axial velocity profile | Turbulence intensity profile
LDA measurements: seeding particles comparison
Smoke
Fog
Smoke
Fog

## Slide 69
Measurement of aerosol mass concentration (R4)
Air velocity [meter/s] | Mass concentration of liquid [g/m3]
42 | 1,5

## Slide 70: WP3 Perspectives for stage 2 TASK 4
Mounting of the new channel and the measurement equipment
Experiments
Data processing and analyses
Final report
September 2007
October 2007
November 2007
December 2007

## Slide 71: WP3: EXPERIMENTAL STUDY OF AEROSOLS TRANSPORT PROCESS IN THE PRIMARY CIRCUIT EQUIPMENT (Task4)
Test | Velocity for deposition phase, m/s | Velocity for resuspension phase, m/s | Particle size d, mkm | Temperature, K | Test Purpose | Aerosol particles parameters | Orientation and surface parameters of working section
EVAN–№3345 AT 1.1 | 33,8 | None | 0.2 – 5 | 300 | Investigation of transport and deposition rate of liquid aerosol particles from gas flow towards the wall | Liquid JEM PRO-SMOKE high density (SP MIX) | Vertical pipe with 98 mm diameter, height ~6 m (upwards flow), steel 10ХСНД
EVAN–№3345 AT 1.2.1 | 39,6 | None | 0.2 – 28 | 300 |  |  | 
EVAN–№3345 AT 1.2.2 | 33,8 |  |  |  |  |  | 
EVAN–№3345 AT 1.2.3 | 24,8 |  |  |  |  |  | 
EVAN–№3345 AT 1.2.4 | 6,5 |  |  |  |  |  | 
EVAN–№3345 AT 2.1 | 20 | 65 | 0.3 – 10 | 320 | Investigation of deposition and resuspension of solid aerosol particles (prototype and preliminary tests) | Solid aerosol particles of NH4Cl | Vetrtical pipe from stainless steel with diameter ~50mm, height ~5 m,
 |  | 105 |  |  |  |  | 
EVAN–№3345 AT 2.2 | 30 | 75 |  |  |  |  | 
 |  | 105 |  |  |  |  | 
EVAN–№3345 AT 2.3 | 38 | 75 |  |  |  |  | 
 |  | 105 |  |  |  |  | 
Matrix of experiments for phase №1 and phase №2

## Slide 72
Test | Um | Particle size | С1 | С2 | C1-C2 | M | F
 | m/s | mkm | g/m3 | g/m3 | g/m3 | g/s | g/(m2s)
EVAN–№3345 AT 1.1 | 33,8 | 0,52 | 4,80 | 4,10 | 0,700 | 0,185 | 0,182
EVAN–№3345 AT 1.2.2 | 33,8 | 5,5 | 1,50 | 0,750 | 0,750 | 0,198 | 0,195
EVAN–№3345 AT 1.2.1 | 39,6 | 5,5 | 0,730 | 0,250 | 0,480 | 0,143 | 0,141
EVAN–№3345 AT 1.2.3 | 24,8 | 5,5 | 1,10 | 0,500 | 0,600 | 0,112 | 0,110
EVAN–№3345 AT 1.2.4 | 6,5 | 5,5 | 4,50 | 2,40 | 2,10 | 0,103 | 0,101
WP3: EXPERIMENTAL STUDY OF AEROSOLS TRANSPORT PROCESS IN THE PRIMARY CIRCUIT EQUIPMENT (Task4)
The experimental results for phase 1
Particle spectrum for AT 1.2
Particle spectrum for AT 2.1
0.0
0.5
1.0
1.5
2.0
2.5
3.0
3.5
0.0
0.2
0.4
0.6
0.8
1.0
diameter
[
mkm
]
Relative frequency
[
-
]
эксперимент
“
а
”
эксперимент
“
б
”
аппроксимация.
experiment
“
а
”
experiment
“
b
”
approximation

## Slide 73: WP3: EXPERIMENTAL STUDY OF AEROSOLS TRANSPORT PROCESS IN THE PRIMARY CIRCUIT EQUIPMENT (Task4)
The experimental results for phase 2
Particle spectrum for AT 2.2.1
Particle spectrum for AT 2.1

## Slide 74
Выполнены все опыты в соответствии с матрицей экспериментов.
Получены количественные данные для оценки скорости осаждения жидкого аэрозоля размером от 0,5 до 15 мкм в цилиндрическом вертикальном канале в диапазоне чисел Рейнольдса от 10000 до 240000.
Получены количественные данные по кинематическим характеристикам несущей среды (средние скорости, пульсационные составляющие скоростей, частоты пульсаций) в цилиндрическом вертикальном канале диаметром 98 мм.
Получены количественные данные по характеристикам дисперсной структуры потока, включая распределение капель по размерам, изменение концентраций и размеров капель в поперечном сечении и вдоль по потоку в цилиндрическом вертикальном канале диаметром 98 мм.
Создана новая экспериментальная установка, предназначенная для исследования процессов осаждения и уноса твердых аэрозолей в цилиндрических каналах.
Разработана конструкция генератора аэрозоля хлорида аммония, основанная на использовании обратимой химической реакции диссоциации-рекомбинации хлорида аммония.
Получены количественные данные интенсивности осаждения аэрозоля хлористого аммония размером от 0,5 до 10 мкм в вертикальном канале диаметром 50 мм при скоростях потока от 20 до 38 м/с. Экспериментально определенная масса осаждений является результирующей величиной двух явлений – осаждения и уноса.
Получены количественные данные интенсивности уноса предварительно осажденного аэрозоля хлористого аммония в вертикальном канале диаметром 50 мм при скоростях потока от 65 до 105 м/с.
WP3: EXPERIMENTAL STUDY OF AEROSOLS TRANSPORT PROCESS IN THE PRIMARY CIRCUIT EQUIPMENT (Task4)
Conclusion:

## Slide 75
Regime | Air velocity, m/s | Measured parameters |  |  | 
 |  | Mean drop diameter mm | Mass concentration of the disperse phase, g/m3 | Relative drop enlargement, % (level to level) | Relative decrease of mass concentration, % (level to level)
R1 | 6.5 | 0.55 | 6.5 | 5 | 14±2
R2 | 6.5 | 0.53 | 9.5 | 6 | 14±2
R3 | 34.0 | 0.48 | 1.5 | 6 | 4±2
R4 | 42.0 | 0.48 | 1.5 | 6 | 4±2
Aerosol transport process: measurement results