## Slide 1
Institute of Physics and Power Engineering
ISTC CEG-SAM 6-th Meeting
September 14-17, 2004, Dimitrovgrad, Russia
Revised proposal presented by Alexander Lukyanov
Determination of parameters of fission product
release from VVER irradiated fuel under
beyond design basis accident conditions

## Slide 2: Institute of Physics and Power Engineering
Proposal Content

## Slide 3: FP Aerosol Source Term Experimental Definition
Institute of Physics and Power Engineering
1 - High temperature furnace
2 - Filters set
3 - Bubble condenser
4 - Heater
5 - Flow meter
6 - Ventilation
7 - Steam supply
8 - Gas supply
9 - Kr detector
10 - Gas sampler

## Slide 4: Test Procedure
Institute of Physics and Power Engineering
1 - Specimen preparation:
- γ-scanning
- cutting
- weighing
- dissolution and radiochemical analysis of the witness
- porosity determination by electron microscopy
2 - Heating up in furnace:
- isothermal mode
- controlled rate of the temperature rise
3 - Isotope balance determination (0.1 – 2%)
+ elution of the deposited material from communications
+ bubbler content and gas phase analysis

## Slide 5
Source Term Definition for VVER Irradiated Fuel
Institute of Physics and Power Engineering

## Slide 6
Conditions Of Performed Experiments With Irradiated Fuel
Nuclide | Fuel Specimen Parameters |  |  | Conditions |  | 
 | Mass, g | Burn up, MW*Day/ kg U | Activity, Bq | T, С | Carrier Gas | 
Cs-137 | 8 | 23 & 17 | 2.41073.4108 | 900,1000, 1100,1200 | Ar | 
Cs-137 | 8 | 23 & 17 | 4.01081.6109 | 900,1000, 1100,1200 | Аг - Steam | 
Cs-137 | 21 | 6.3 & 9.6 | 4.01081.7109 | 1200,1600 | He | 
Cs-137 | 24 | 8 & 17.6 | 2.61072.3108 | 1200,1600 | Ar - Steam | 
Ru-106 | 8 | 7 & 23 | 6.01051.2106 | 900,1000, 1100,1200 | Ar | 
Ru-106 | 8 | 17 & 23 | 2.01062.5106 | 1100,1200 | Ar-Steam | 
Ru-106 | 21 | 6.3 & 9.6 | l.0l045.0104 | 1200,1600 | He | 
Institute of Physics and Power Engineering

## Slide 7: FP Aerosol Source Term Experimental Definition
Institute of Physics and Power Engineering
What is new:
Comparative measurements in inetr and steam containing atmosphere were conducted;
Oxygen partial pressure measurement in atmosphere is provided;
Furnace was tested for temperature range 1700 - 2100 oC;
Influence of the structure materials in hot zone (Zr, stainless steel) on FP aerosol formation is to be determined.

## Slide 8: Analytical activity
Institute of Physics and Power Engineering
pretest and posttest simulation by MELCOR code;
- development of FP aerosol formation, transport and depletion models

## Slide 9: Expected contribution Expected outcome
Institute of Physics and Power Engineering
extended data base on FP release from VVER fuel
- validation of FP behavior models, implemented in different codes
test matrix specification;
- analytical accompaniment of experimental efforts