## Slide 1
Post test analysis of PARAMETER-SF4
Jon Birchley and Leticia Fernandez-Moguel (PSI)
Presented by Salih Guentay,
CEG-SAM, 14-16 March, Pisa, Italy

## Slide 2
  SCDAP/Sim modelling
    background
    new air oxidation model
    SCDAP model for PARAMETER
    treatment of boundary conditions
  SF4 analysis
    pre-oxidation
    air phase
    reflood
  Conclusions and forward plans
Outline

## Slide 3
  Previous analysis (presented CEG-SAM 2010) made with standard versions of SCDAP/RELAP5 and SCDAP/Sim
    neither code contains full model for air oxidation
    new SCDAP/Sim version (Mod3.5) includes
      PSI air oxidation kinetic model
      oxygen as an active species; nitrogen as a catalyst species
      now provides correct gas composition (for flow rate, heat transfer)
      treatment of melt oxidation
  Present analysis concentrates on SCDAP/Sim/Mod3.5 calculations
  Oxidation kinetics based on standard correlations (Cathcart-Pawel/Urbanic-Heidrick, Sokolov...) plus
    breakaway treated by imposing an upper limit on effective oxide thickness
    criterion based on temperature and oxidising medium
SCDAP/Sim modelling

## Slide 4
  Define breakaway condition as an upper limit on effective oxide thickness
    cladding oxidation rate/area: R = ρZr d(δ)/dt ~ A exp(-B/T) / δ,eff
    where δ,eff = max (δ0 , min ( δ, δ* ) )
    δ0 is some tiny minimum (<<< δ* )
    and δ = true oxide thickness
  Separate values of δ* are defined for air and steam
    typically: δ, δ*air < δ*steam (i.e. breakaway possible in air, unlikely in steam)
  In general δ* is a function of temperature, material and possibly other factors
  We also define a criterion for onset of breakaway δ,crit ( ≥ δ*) and timescale τ over which the limit value δ* is applied
  Model parameters δ,crit, δ*, τ will be mostly based on results of recent and current separate-effects experiments
PSI oxidation model - 1

## Slide 5
Outline of model concept - 2
PSI oxidation model - 2
continued parabolic if no δ,crit

## Slide 6: Comparison with KIT thermal balance tests in O2 and air (T = 800 ºC)
Air alone
193 s O2
then air
390 s O2
then air
O2 alone
PSI oxidation model - 3

## Slide 7
SCDAP/RELAP5 noding
Same base model for SF2, SF3, SF4
28 axial nodes for test section (lower, central and upper sections)
Radial noding: 1/1/4 in lower/central/upper sections
Heater: 14 Ta, 2x6 Mo, 2x1 brass
Cooling jackets for central and upper sections
Shroud/insulation for central bundle; dummy insulation applied in lower and upper sections (forced by SCDAP limitation)
Except where stated, base model uses default or recommendations
Same external resistance in base case models (8.5 mΩ/rod)

## Slide 8
  Pre-oxidation (0 - 13886 s)
  - 2 g/s Ar; 3.5 g/s steam (start at 1716 s)
  - power staged increase to 7900 W
  Cooling phase (13886 - 16022 s)
  - power reduced to 4000 W
  Air ingress (16022 - 17511 s)
  - 0.48 g/s air (normal oxygen-nitrogen mixture)
  - 2 g/s Ar continued
  - power increased to 6000 W during this phase, tripped at 17412 s
  Reflood (17434 - 17908 s)
  - bottom injection: 80 g/s water (midway period at 40 g/s)
  - switch Ar injection to upper volume
SF4 boundary conditions

## Slide 9
  Temperatures
  Hydrogen generation
  Oxide scale buildup
SF4 preoxidation

## Slide 10
Minor underestimate of temperatures in highest elevations
Temperatures

## Slide 11
Minor underestimate of H2, may be related to slight underestimate of temperatures
No strong influence of PSI model of possibility of breakaway during steam oxidation
H2 generation

## Slide 12
PSI model can predict breakaway in steam
Slighly increased oxidation at some locations
For base case model we focus on cases without steam oxidation breakaway
Oxide thickness
no effect at highest elevation

## Slide 13
  Temperatures
    lower elevations
    upper elevations
  Effect of oxidation model
  Oxygen starvation
  Oxide scale buildup
SF4 air ingress phase

## Slide 14
Initial heat up due to reduced heat transfer
Accelerated heating at T > ca. 1400 K
Faster acceleration if already in breakaway
Early acceleration with Melcor kinetic parameters
Uneven escalation indicates progression of starvation front
Effect of oxidation model

## Slide 15
Initial heat up due to reduced heat transfer
Slow heatup at highest elevations
Maximum temperatures ca. 1800 K
Starvation occurs earliest at top of bundle and progresses downward
Temperatures (upper)
onset of starvation

## Slide 16
First acceleration in heatup not due to breakaway
Downward progression of starvation front
Calculated a bit early
Temperatures (lower)
progression of starvation

## Slide 17
SF4 data normalised to maximum
Base model comes closest to rate of consumption and no breakaway
Some effect of earlier breakaway in steam (if calculated)
MELCOR kinetic parameters strongly overestimate kinetics and calculate breakaway as well
Oxygen consumption

## Slide 18
Most oxidation in air ingress phase occurs at mid-elevations in bundle bundle (300 - 800 mm)
Further oxidation during reflood, mostly at same elevations
Oxide scale buildup
start of injection

## Slide 19
  Temperatures
  Hydrogen generation
  Effect of oxide scale failure (=> melt breakout)
Reflood phase

## Slide 20
High temperature and delayed cooling calculated at 200 - 500 m
Earlier cooling above and below
Behaviour due to melt oxidation
Absent if no melt breakout
Reflood temperature excursion

## Slide 21
SSim calculated high temperatures and delayed cooling in melt zone 200-500 mm
No thermal data for 200-300 mm but indicated at 600-700 mm
Bundle examinations showed extensive melting down to 260 mm
Temperatures in molten zone

## Slide 22
Significant H2 generation due to oxidation of metallic melt
Total amount about right but kinetics overestimated
May be reason for such high calculated temperatures
Reflood hydrogen generation

## Slide 23
  PARAMETER-SF4 analysed with new version of SCDAP/Sim
    full treatment of air oxidation
  Default air oxidation model largely based on default model in SCDAP (Cathcart-Pawel /Urbanic-Heidrick) plus possibility to calculate breakaway
    model can also calculate breakaway in steam
  Conclusion about air phase not very different from earlier analysis (using steam oxidation model with modified parameters)
    overestimation with Melcor kinetic parameters confirmed
    breakaway effects at most minor
  Large excursion during reflood linked to oxidation of metallic melt
    broadly consistent with experimental results
    suppressed by higher temperature criterion for melt breakout (2500 K instead of 2200K)
    low temperature melt breakout may have occurred due to earlier oxygen starvation
  New version still being assessed; analyses will continue
Conclusions and forward plans

## Slide 24
Thank you for your attention
Notes: Beispiel um die Schlussfolie als Danksagung zu nutzen