## Slide 1
Results of post-test examinations of SF2 fuel bundle and numerical simulations of the experiments PARAMETER-SF3 and -SF4
Presented by A.Kiselev
FSUE SRI SIA “LUCH”
IBRAE RAS
FSUE EDO “GIDROPRESS”
14th CEG-SAM Meeting, Kiev, Ukraine, September 9-11, 2008

## Slide 2: Contents
PARAMETER-SF2 bundle material investigations results
Post-test PARAMATER-SF2 numerical analysis results
Pre-test PARAMATER-SF3 calculations
Proposed PARAMATER-SF3 scenario

## Slide 3: Part 1: SF2 bundle material investigations Post-test appearance of the shroud
Shroud kept its integrity
Thin oxide scale on the outer surface
Z = 850-1050 mm
Z=1100-1300 mm

## Slide 4: Overview of sectioning map for metallographic examination
At 400-1300 mm
30 crosscuts were
made
12 cross-sections
were chosen for
studies
5 selected cross
section are considered
in detail
in the presentation

## Slide 5: Metallographic examination of the cross -section at Z=513 mm
Rod 2.1
Rod 2.3

## Slide 6: Metallographic examination of the cross section at Z=702 mm
Rod 1.1
Rod 2.1

## Slide 7: Layers structure at Z=702 mm
Rod 1.1
Rod 2.1

## Slide 8: Metallographic examination of the cross- section at Z=1033 mm
Through wall cracks on the claddings
A lot of oxide scale remnants between rods

## Slide 9: Layers structure at Z=1033 mm
Tmax ~1350◦C
Internal oxide of columnar
structure with multi-layer
spalling-off films
No oxidation of cracks

## Slide 10: Metallographic examination of the cross section at Z=1103 mm
Rod 1.1
Rod 2.5
Rod 3.9
Rod 2.6

## Slide 11: Layers structure at Z=1103 mm
Rod 2.2
Rod 2.5
Rod 2.4
Rod 3.5

## Slide 12: Metallographic examination of the cross section at Z=1250 mm

## Slide 13: Layers structure at Z=1250 mm
Tmax ~1500◦C
Columnar structure of inner
oxide and spalling-off
multi-layers
on the external surface
No oxidation of cracks

## Slide 14: Distribution of the compact dioxide zirconium thickness along heated zone

## Slide 15: Averaged cladding zirconium dioxide thickness*
* exhausted metal layer *1.56

## Slide 16: Hydrogen pickup
Applied method – X-ray analysis
No possibility for claddings investigations because of their brittleness
The shroud hydrogen pickup was measured for Z=250, 500, 900 and 1200 mm.

## Slide 17: X-ray analysis results

## Slide 18: Some outcomes from SF2 material investigations
Material investigations of the PARAMETER-SF2 bundle are completed.
  The fuel assembly was filled with epoxy and cut on the cross-section
  12 cross section were chosen for metallographic measurements
  5 cross section have been investigated and described in detail (Z=513, 702, 1033, 1103, 1250 mm)
There is no fuel relocation.
Pronounced oxidation of the claddings at Z=1000-1300 mm elevations have been revealed. No oxidation of through wall cracks.
ZrO2 oxide on the claddings surface includes inner compact one-layer dioxide zirconium with columnar structure on the metallic layer and external multi-layer spalling-off films.
Metallic layer thickness of the fuel rod claddings together with compact dioxide zirconium thickness were measured.
Shroud hydrogen pickup was investigated by X-ray analysis (Z=250, 500, 900, 1200 mm).
Maximum hydrogen pickup in the shroud was revealed at Z= 900 mm (23 at%)

## Slide 19: Part 2: SF2 post-test numerical analysis Used codes and participants
SOCRAT –IBRAE
ICARE/CATHARE - NSI RRC KI
ATHLET-CD – GRS
RELAP/SCDAPSIM MOD3.2 (RELAP) - FSUE EDO “GIDROPRESS”
PARAM-TG - FSUE SRI SIA “LUCH”

## Slide 20: Initial and boundary conditions PARAMETER-SF2 post-test analysis
ICARE/CATARE
Experimental thermoinsulation temperature used as boundary conditions

## Slide 21: Heat balance PARAMETER-SF2 post-test analysis
ATHLET

## Slide 22: Heat balance PARAMETER-SF2 post-test analysis
Pre-oxidation phase
Joel heating power ~ 7kW
Coolant heating power ~ 6kW
Before flooding onset
Joel heating power ~ 9.5kW
Coolant heating power ~ 9kW
Oxidation reaction power
Pre-oxidation phase - up to 1kW
Before flooding up to 2.3kW
Flooding phage up to 2.5 kW

## Slide 23: Claddings temperature evolution PARAMETER-SF2 post-test analysis

## Slide 24: Shroud temperature evolution PARAMETER-SF2 post-test analysis

## Slide 25: Hydrogen release PARAMETER-SF2 post-test analysis
Hydrogen release
Experimental ~28 g
ICARE ~ 25.5 g
ATHLET ~ 23 g
SOCRAT ~ 20 g

## Slide 26: Main outcomes from SF2 post-test calculations
Post-test calculations and experimental data on temperature evolution are in a good agreement except temperature “hump” at 12000 s
The most codes underestimate hydrogen total amount.
In the course of post-test SF2 calculations heat loss due to external resistance and heat loss through shroud were specified.

## Slide 27: Part 3 and 4: Proposed PARAMETER-SF3 test scenario and pre-test calculations results

## Slide 28: Initial and Boundary conditions
Electrical power
Pre-oxidation phase ~ 7.7 kW
Transient phase ~ 10.5 kW

## Slide 29: Used codes and participants
SOCRAT –IBRAE
ICARE/CATHARE - NSI RRC KI
ATHLET-CD – GRS
RELAP/SCDAPSIM MOD3.2 (RELAP) - FSUE EDO “GIDROPRESS”
PARAM-TG - FSUE SRI SIA “LUCH”
SCDAP/RELAP/IRS (RELAP/IRS) -PSI

## Slide 30: Heat balance PARAMETER-SF3 pre-test analysis

## Slide 31: Heat balance PARAMETER-SF3 pre-test analysis
Heat loss through shroud
at pre-oxidation phase
~15-20% of core power over 0-1275 mm

## Slide 32: Claddings temperature evolution - hottest zone PARAMETER-SF3 pre-test analysis

## Slide 33: Claddings temperature evolution: 700-1000 mm PARAMETER-SF3 pre-test analysis

## Slide 34: Shroud temperature evolution PARAMETER-SF3 pre-test analysis

## Slide 35: Temperature profile PARAMETER-SF3 pre-test analysis

## Slide 36: Oxide scale thickness PARAMETER-SF3 pre-test analysis

## Slide 37: Hydrogen release PARAMETER-SF3 pre-test analysis
Hydrogen release predicted ~ 22-27 g
No extra hydrogen release at the flooding stage

## Slide 38: Flooding Phase (SOCRAT calculations)

## Slide 39: Conclusions
SF2 post-test and SF3 pre-test runs have been performed by SOCRAT, ICARE/CATHARE, ATHLET-CD, RELAP, PARAM-TG codes
(IBRAE, RRC KI, GRS, PSI, GIDROPRESS, LUCH)
Scenario for SF3 test was numerically justified.
Predicted temperatures are similar.
Predicted hydrogen release is estimated as 22-27g