## Slide 1
Post-test Calculations of PARAMETER SF4 using ATHLET-CD
Thorsten Hollands, Christine Bals
Henrique Austregesilo, Wolfgang Luther
Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany
1

## Slide 2: Content
  Boundary conditions for PARAMETER SF4 experiment and simulation with ATHLET-CD
  Input model and options for ATHLET-CD post-test calculation
  Results of PARAMETER SF4 post-test calculations:
    Temperatures
    Quench fronts
    Oxygen consumption
    Hydrogen generation
  Conclusions
2

## Slide 3: PARAMETER SF4: Boundary Conditions and Simulation with ATHLET-CD (1)
Power supply – temperature:
cold bundle at start of test: 21 °C at 0 s
pre-oxidation phase: max. plateau temperature of ~ 1200 °C is reached at ~ 8000s with power increase to ~7 kW; temperature is kept until ~ 14000 s with power regulation between 7 and 8 kW;
at 14000 s power reduction to ~ 4 kW to reduce Tmax to ~ 900 °C before air injection is started at 16000s
again power increase to ~ 6 kW during air injection phase; power is switched off at 17412 s (max. temperature of 1740 °C is measured)
bottom injection of water is started at 17434 s; valve of air supply is closed at 17511 s
bottom flooding is finished at 17908 s when bundle is cooled down
3

## Slide 4: PARAMETER SF4: Boundary Conditions and Simulation with ATHLET-CD (2)
Argon inlet flow : - constant rate of 2.0 g/s - switch to upper injection after start of reflood - T ~ 280 °C
Steam inlet flow: - starts at 1716 s with flow rate of ~ 3.5 g/s until 16022 s when air injection is started, - T ~ 500 °C
Air inlet flow: - 0.5 g/s (0.1 g/s O2, 0.4 g/s N2 for simulation) - air injection starts at 16035 s - air injection is switched off at 17511 s (77s after opening the bottom flooding valve)
Bottom flooding : - initial water level of 450 mm below inlet pipe - is initiated at 17434 s (Tmax = 1740 °C is measured); - water flow rate: 80 - 30 - 80 g/s, water temperature: 25 °C - is finished at 17908 s (bundle is cooled down)
Bundle pressure: ~ 4 bar; constant boundary condition at outlet (PHCOROUT) for simulation
4

## Slide 5: Input model for PARAMETER calculations with ATHLET-CD
Flow Channels
    Central bundle (with rods) CORE2 85.7 %
    Outer bundle region CORE3 14.3 % connected to outlet OUTPIPE
    Cross connection
    Cooling Jacket
Structures
    Rods: ROD1 ( 1 unheated rod) ROD2 ( 6 heated rods) ROD3 (12 heated rods)
    Grids (6)
    Shroud / Insulation
    Cooling Jacket Wall
    Structures at top of bundle (upper plate, separation sheet)
Changes compared to previous calculations (SF2, SF3):
    Additional fills O2FILL, N2FILL for air injection
Changes compared to SF4 pre-test calculation:
    12 unheated peripheral rods considered → smaller bundle flow area, → oxidation: as shroud
5

## Slide 6
  Zr / steam oxidation model: Cathcart / Prater-Courtright correlation (IOXMOD = 15) was used instead of Leistikow / Prater-Courtright correlation (IOXMOD = 19) (SF2, SF4 pre-test calculation: IOXMOD = 19 was taken; SF3 post-test calculation: IOXMOD = 15 was used for better agreement of H2 data; Sokolov correlation (IOXMOD = 18) leads to underestimated oxidation)
  Zr / air oxidation model: Correlation derived for Ar / O2 mixture (AEKI, IOXAIR = 6) was used to calculate oxygen reaction (with Powers, IOXAIR = 1, taken for SF4 pre-test calc., temperature increase is too fast) ► reference post-test calculation without consideration of ZrN formation; ► further post-test calculation with new modeling which includes ZrN formation (Hollands, INITN2 = 1)
  External resistance increased from 1 mΩ/rod (used for pre-test calculation) to 3 mΩ/rod after pre-oxidation phase
  Hydraulic diameter in core region is DH at grid position (DH = 3.8·10-3 m, as used for pre-test calculation); bundle flow area reduced from 2.31·10-3 m2 to 2.16 ·10-3 m2 due to consideration of 12 peripheral rods;
  Candling velocity of melt : WSL= 5 mm/s (reference calc.), 2 mm/s(calc2); melting temperature of metallic Zr increased from 2033 K (ß-Zr) to 2250 K (α-Zr); unlimited oxidation in structures possible up to 2300 K (TCMLT1); limited oxidation up to 2600 K (TCMLT2)
  Default values for other models (e.g. interfacial friction model, quench model) are used
6
Options for ATHLET-CD post-test calculation of SF4 (1)

## Slide 7: Results of PARAMETER SF4 post-test calculation (reference)
7
Temperatures during pre-oxidation period (before air oxidation)
maximum temperature is calculated at 1250 mm elevation as in test
  given time function for power leads to a maximum plateau temperature of Tmax = 1155 °C which is slightly underestimated compared to data
  during temperature decrease between 14000 s and 16000 s a max. temperature of ~ 800 °C is achieved; lower than measured
Notes: 7

## Slide 8: Results of PARAMETER SF4 post-test calculation (reference)
8
Temperatures during air ingress period – lower and medium bundle heights –
due to oxygen starvation in the upper bundle region the higher air oxidation and therefore the stronger temperature excursion moves to lower elevations in agreement between measured data and calculation
  maximum temperature of 1740 °C is reached at 17412 s in test with highest temperatures at bundle elevations 500 - 800 mm; max. temperature in simulation at 17412 s is 1950 °C at 500 mm position
Notes: 8

## Slide 9: Results of PARAMETER SF4 post-test calculation (reference)
9
Temperatures during air ingress period – upper bundle heights –
  initial increase of temperatures is in good agreement with test data; for later phase of air ingress temperature increase is too fast
Notes: 9

## Slide 10: Results of PARAMETER SF4 post-test calculation (reference)
10
Oxygen starvation
after a time period of ~ 1200 s following the start of air injection (t = 16035 s) oxygen starvation can be observed at the elevations above ~ 600 mm
  resulting time period of oxygen starvation in upper bundle region (until start of injection): Δt ≈ 200 s (~ 17235 → 17434 s)
Notes: 10

## Slide 11: Results of PARAMETER SF4 post-test calculation (reference)
11
Oxygen starvation
  oxygen consumption is slightly underestimated in simulation compared to test data
Notes: 11

## Slide 12: Results of PARAMETER SF4 post-test calculation (reference)
12
Temperatures during quench period – medium and upper bundle heights –
after start of flooding considerable temperature increase between 500 and 900 mm bundle elevation
  max. rod temperature 2320 °C in outer ring (ROD3) at 600 mm elevation (t=17550 s); max. shroud temperature 2390 °C at 600 mm elevation
Notes: 12

## Slide 13: Results of PARAMETER SF4 post-test calculation (2 mm/s candling)
13
Temperatures during quench period – medium and upper bundle heights –
Simulation with lower candling velocity
simulates cooling behavior in better agreement with data, but shows no successful total quench due to too early stop of injection
Notes: 13

## Slide 14: Results of PARAMETER SF4 post-test calculation (ZrN model)
14
Oxygen starvation
in comparison to the reference calculation a better agreement of the oxygen consumption is calculated; time point of oxygen starvation is calculated in very good agreement with data
  oxygen starvation at ~ 17200 s leads to nitride formation and further temperature escalation due to additional exothermal heat
Notes: 14

## Slide 15: Results of PARAMETER SF4 post-test calculation
15
Hydrogen Generation
during pre-oxidation period: 20.8 g 21 g measured
→ good agreement with used correlation IOXMOD=15
→ improvement with consideration of 12 peripheral rods
Notes: 15

## Slide 16: Results of PARAMETER SF4 post-test calculation
16
Hydrogen Generation during quench phase
during quench phase: reference calc: 55.8 g (tot. 76.6 g) lower candl. vel.: 70.2 g (tot. 91.0 g) new ZrN model: 79.0 g (tot. 99.6 g) measured: 86 g (tot. 107 g)
→ temperature excursion / steam oxidation during flooding could be improved with use of more realistic input values for Zr melt temperature (α-Zr → 2250 K; transfer to higher values with increasing oxide layer → TCMLT2)
→ melt oxidation is underestimated
→ amount of hydrogen generation and melt production is improved by use of ZrN model
Notes: 16

## Slide 17: Conclusions
  ATHLET-CD calculates in good agreement the behavior within the pre-oxidation phase
  Air injection with a rate of 0.5 g/s leads to a oxygen starvation at the positions above ~ 600 mm after a time period of 1200 s (at ~ 17200 s, start of air injection at 16035 s); therefore the elevation of the maximum temperature moves to lower positions in agreement with test data
  Temperature increase during air oxidation phase is calculated in good agreement with test data with IOXAIR=6 (AEKI Ar/O2) instead of IOXAIR=1 (Powers); consideration of nitride formation leads to faster temperature increase due to more exothermal energy
  Temperature increase after start of reflood (steam oxidation) can be simulated up to bundle region of ~ 1000 mm; seems to be underestimated above
  Time needed for quenching: ~ 400 s; bundle is cooled down at ~ 17830 s; good agreement of temperature decrease for positions up to ~ 800 mm – positions in upper bundle region are cooled down too fast (ref. calc.)
  Total hydrogen generation is 76.6 g (ref. calc.) and 99.6 g for simulation with improved air oxidation modeling, lower than measured (107 g) → heat up at upper bundle positions and melt oxidation seem to be underestimated (ref. calc.)
  The results can be improved by implementing a first model to consider nitride formation during air ingress, but this model and its input parameters have to be further developed and validated
  For the evaluation of simulation results it could be helpful to know how many H2 was released by each component and how many O2 and N2 was consumed
17

## Slide 18: Acknowledgement
The development and the assessment of ATHLET-CD are sponsored by the German Federal Ministry of Economics and Technology.
18