## Slide 1: Interaction of suboxidized corium melt with a vertically-positioned specimen. Test МСР-1. Results of analysis
Presented by V. Granovsky
2nd METCOR-P project meeting
July 9, 2008, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
Experiment specifications
Results
Posttest analysis
Systematization of tests with suboxidized corium
Model of stabilized corrosion condition
Comparison with GEMINI / NUCLEA calculations
IVR application
Requirements to the test on the interface orientation relevance
Conclusions

## Slide 3: Objectives of the test
Comparison with results of MC6 test with horizontally positioned interface
Test parameters are similar to MC6 test of METCOR-2:
C-30 corium charge
15Kh2NMFA vessel steel
Pure argon above the melt
10 h exposition

## Slide 4: Furnace design
1 – Water-cooled screen
2 – Lid
3 – Water in
4 – Quartz tube
5 – Crucible sections
6 – Specimen
7 – Inductor
8 – Bottom calorimeter
9 – Welded crucible sections
– SS support
– Water out
12 – Electromagnetic screen
13 – Crucible collector

## Slide 5: TC locations in the specimen
Coordinates of TC hot junctions
Majority of TC were installed at H=50 mm elevation, where the maximum depth of specimen corrosion was expected according to the pretest calculations

## Slide 6: Test procedure
Time, s | Operation mode
0-963 | Furnace deoxygenation by argon flow
963-3550 | Formation and homogenization of the molten pool. Increase of power in the melt to get 1400 oC on the specimen surface
3550-39874 | Surface temperature and specimen - water power kept constant by inductor voltage control
39875-42000 | Heating disconnection, melt solidification and ingot cooling in argon

## Slide 7: Test results: TC readings (1)
Wrong readings of several thermocouples due to corrosion of wires below the hot junctions

## Slide 8: Test results: TC readings (2)
Estimation of IZ progression from TC readings
Different lifetime of TCs in the mushy interaction zone
Not possible to estimate interaction kinetics
Short incubation period (or no incubation)

## Slide 9: Posttest examination
Axial sections of ingot
Example of TC location
Corium upper crust is removed
Metal inclusions in corium ingot
Axial sections of ingot
Axial sections of ingot
The maximum depth of corrosion is in the middle section of the specimen (Н  30 mm) due to formation of a thick corium upper crust and decrease in the melt depth

## Slide 10: Posttest examination (2)
Axial sections of specimen
MCP-1 (90º rotated)
MC 6
Corium
1st layer
2nd layer
Zone of thermal influence
Steel of initial structure
IZ
Steel

## Slide 11: Posttest examination (3)
Temperature profile of the specimen
A – boundary of the thermal influence zone (lamellar pearlite structure indicating eutectic composition formation at 727 oC)
B – boundary of the 2nd layer (1000-1090 oC)
C – boundary of the 1st layer (1240-1300 oC)
1 – 700 oC 5 – 1100 oC
2 – 800 oC 6 – 1200 oC
3 – 900 oC 7 – 1300 oC
4 – 1000 oC 8 – 1400 oC
T, oC
90° rotated
Upper surface
bottom

## Slide 12
Reduction of Cn up to ≈17% (instead of 30) at the interaction start is explained by a high oxygen content in the upper crust
Higher content of U and Zr in IZ (40-50 and 13-14 mass %) in comparison with МС6 IZ (24 and 5 mass %)
High content of U and Zr in metal inclusion ( 58 and  24 mass %), as in MC6
Posttest examination (4)
XRF and chemical analysis
XRF,mass.%
ChA,mass.%
U=66.1
Zr=20.1
Fe=1.7
Cr=0.06
Ni=0.02
U=65.6
Zr=22.1
Fe=1.0
Cr=0.02
Ni=0.03
U=66.6
Zr=23.2
Fe=1.0
U=64.4
Zr=21.7
Fe=3.5
Cr=0.04
Ni=0.08
U=66.7
Zr=22.3
Fe=5.7
XRF
ChA
U=57.5
Zr=24.2
Fe=17.8
Cr=0.2
Ni=0.3
1st layer:
U=52.4
Zr=13.7
Fe=30.9
Cr=0.6
Ni=0.3
U=66.8
Zr=22.3
Fe=2.1
Average
sample of ingot upper part Cn≈40
Average
sample of
crust
Cn≈48
2nd layer:
U=36.4
Zr=14.3
Fe=47.8
Cr=0.8
Ni=0.5
Average
sample of ingot lower part Cn≈32
29-31mm
23mm
25mm

## Slide 13: Posttest examination (5)
SEM/EDX analysis
Steel
Crust
__________
U(Zr)O2
intermetalics
1st layer
__________
U(Zr)O2
Zr(U)Fe2
U6Fe
U(Zr)- Fe
eutectic
1 mm
Corium
____________
U(Zr)O2
-Zr(O)
2nd layer
_________
U(Zr)Fe2
Fe- U(Zr)
eutectic
UFe3
U(Zr)Fe3
No liquid in the crust
Small solid fraction in the 1st layer
Small liquid fraction in the 2nd layer (only in a thin layer contacted with steel)

## Slide 14: Comparison of MCP-1 and MC6 data
Conditions Results
Different conditions not only in the interface orientation, but also in corium oxidation index and heat flux
Reason of result differences?

## Slide 15: Discussion of results
Possible reason of shorter incubation period in МСР-1 in comparison with МС6:
- thinning of crust between melt and IZ caused by increased heat flux and surface temperature
Lower temperature of MCP-1 IZ final boundary in comparison with MC6 can be explained by :
- a significantly decreased Cn, i.e. increased content of Zr- free in the melt ?
- vertically- positioned interface ?

## Slide 16: Results of tests with suboxidized corium
Test | Corium oxidation index, Сn | Temperature on the IZ boundary, TB ,С | Mass fraction of interacting specimen steel, ,% | IZ composition, mass.% |  |  | Composition of the in-corium metallic body, mass.% |  | 
 |  |  |  | U | Zr | Fe | U | Zr | Fe
МС6 | С-30 | 1120 … 1200 | 3,4 | 25,6 | 5,4 | 64,4 | 55,0 | 25,0 | 15,0
МС7 | С-30 | 1030 … 1100 | 0,4 | 44,0 | 2,2 | 50,0 |  |  | 
МС8 | С-70 | 1200 | 2,9 | 22,0 | 6,1 | 68,2 |  |  | 
МС9 | С-30 | 1060 … 1100 | 9,2 | 33,3 | 8,3 | 53,0 |  |  | 
МСР-1 | С-17 | 1000 … 1090 | 7,1 | 44,0 | 14,0 | 40,0 | 57,0 | 24,0 | 18,0

## Slide 17: Peculiarities of METCOR tests
  Fe displaced by U and Zr from the IZ forms a metallic body in the oxidic melt. Other conditions being equal, it leads to the corium oxidation degree growth
  In МС9 200 g of SS is introduced. Absence of the melt surface crust leads to the Fe volatilization, therefore a metallic body is not formed in the oxidic melt.
  For metallic melt (1) CU and CZr is larger, and CFe – smaller than in case of metallic melt (2)
MASCA METCOR
MC6 … MC8, MCP-1 MC9
T1 = T2 T1 >> T2
Oxide melt
(U, Zr)2-x – FeO1-y
Metal melt (1)
U–Zr– Fe–(O)
T1
T2
Metal
melt (1)
Oxide melt
(U, Zr)2-x – FeO1-y
Metal melt (2)
U–Zr– Fe–(O)
(IZ)
T2
T1
Crust
Crust
Oxide melt
(U, Zr)2-x – FeO1-y
Metal melt (2)
U–Zr– Fe–(O)
(IZ)
T2
T1
Crust
Vessel steel
Vessel steel

## Slide 18: MASCA results
As and Сn grow, U and Zr concentrations decrease, and Fe concentration increases in the metallic part of the melt
U, Zr and Fe concentrations in the metallic ingot as a function of the introduced steel concentration
in the С-32 – С-45 range
in the С-60 – С-75 range

## Slide 19: Fe concentration in the IZ versus the mass fraction of interacting steel
  МС8 point is on a steeper curve than МС6, МС7 due to a higher oxidation index
  МСР-1 point is on a flatter curve than МС6, МС7 due to a lower oxidation index
  МС9 point is on a flatter curve than МС6, МС7 due to the absence of a metallic body, which is equivalent to a smaller oxidation index
, evaporation)

## Slide 20: Model of the stabilized system after corrosion stage completion
● Stabilized condition (corrosion completion) means chemical equilibrium between the oxidic liquid (corium) and metallic liquid (IZ) in the thermal gradient conditions. The equilibrium is provided by the repartitioning of components between liquids (like in MASCA)
● Low IZ temperature explains insignificant solubility of
oxygen in the metallic melt. Therefore, the IZ can be roughly analyzed using the U-Zr-Fe ternary diagram (without oxygen)
● Steel corrosion – its dissolution in the IZ metallic melt
● Specimen and IZ temperature are sensitive only to thermal boundary conditions

## Slide 21: Model of the stabilized system after corrosion stage completion (2)
Conventional phase diagram
Equilibrium concentration of Fe in the IZ versus steel mass fraction
Final position of the IZ boundary
Corium melt
Steel
U, Zr
Fe
T

## Slide 22: Comparison of GEMINI / NUCLEA calculations with experimental data
U/Zr variation range in the IZ compositions from 3.15 to 20.0
Mass Fraction
Zr
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1.0
MC7
MC8
MC9
MCP-1
1.0
0.9
0.8
0.7
0.6
0.5
0.4
0.3
0.2
0.1
0.0
1.0
0.9
0.8
0.7
0.6
0.5
0.4
0.3
0.2
0.1
0.0
Fe
U
0.0
MC6

## Slide 23: Comparison of GEMINI / NUCLEA calculations with experimental data (2)
  Minimum value exceeds
  The MC7 IZ composition is close to the eutectics. It corresponds to the
  SEM/EDX results – liquid phase is more than 80 mass.%
  Composition of the МС9, МСР-1 IZ is mushy. It corresponds to the
  SEM/EDX results
МС7 U/Zr=20.0 МС9 U/Zr=4.0 MCР-1 U/Zr=3.15
U, Zr
Mass.%
T,C
Fe
U, Zr
Mass.%
30
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
Fe
T,C
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
U, Zr
30
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
T,C
Mass.%
Fe

## Slide 24: Comparison of GEMINI / NUCLEA calculations with experimental data (3)
  IZ is liquid. It corresponds to the SEM/EDX results
MC6 U/Zr=4.75 MC8 U/Zr=3.62
U, Zr
U, Zr
Fe
Fe
Mass.%
Mass.%
T,C
T,C
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500

## Slide 25: Application for IVR VVER-1000
Stratified molten pool
1090°C
Metal melt
Oxide melt
1500°C
mstmax
Metal melt
Oxide melt
Fragment

## Slide 26: Application for IVR VVER-1000 (2)
- МС8
- VVER-1000

## Slide 27: Requirements to the test on checking the influence of interface orientation
      ● Prototype with a horizontal specimen positioning– МС8
  ● Exact thermometry of the specimen
  ● Melt oxidation index – С-30
  ● Added 12 mass% of steel  С-70 oxidation index
  ● Corium crust on the oxidic melt surface,
  ● Establishment of the specimen’s stationary temperature condition
  ● Numerical modeling to determine , at which
  ● Adjustment of stationary regime
  ● Regime duration – until corrosion front stabilizes

## Slide 28: Conclusions
      ● Completed analysis explains the МСР-1 results; the interface orientation is not taken into account
      ● If the corrosion of steel at its interaction with suboxidized corium melt depends only on the chemical equilibrium, the interface orientation assumably does not influence the final corrosion depth
      ● Experiments on checking the possible influence of interface orientation are to have identical conditions:
  - Сn
  -
  - presence of crust on the molten corium surface
      ● In order to verify the presented model it is advisable to make an experiment at the horizontal position of the interface with corium
      C-90 (С-95) or С-30 (С-70) and increased value of in comparison with с МС6, МС8 in order to get ТВ  1300 - 1350С