## Slide 1: Progress Report on the ISTC project #833.2 “Investigation of corium melt interaction with NPP reactor vessel steel” (METCOR-2)
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
10th CEG-SAM meeting

## Slide 2: Contents
METCOR project general information
Project meetings
Experimental matrixes
Experimental methodology
Tests with suboxidized corium
Tests with oxidized corium
Example of plant application
Reporting
Publications
Proposals for studies continued within a new project
Conclusions

## Slide 3: METCOR project general information
Qualification and quantification of physicochemical phenomena of corium melt interactions with reactor vessel steel
Experimental data application:
Analysis of in-vessel corium retention (IVR)
Analysis of ex-vessel retention (EVR) in the core catcher of a cold crucible type
Project objectives:

## Slide 4: METCOR project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatome ANP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZR, Germany
FORTUM, Finland

## Slide 5: Meetings of METCOR.2 projects
▼ 1st meeting of the Steering Committee, 3 October 2002, Karlsruhe, Germany
▼ 2nd meeting of the Steering Committee, 29 January 2003, Aix-en-Provence, France
▼ 3rd meeting of the Steering Committee, 16 September 2003, St. Petersburg, Russia
▼ 4th meeting of the Steering Committee, 10 February 2004, Paris, France
▼ 5th meeting of the Steering Committee, 14 September 2004, Dimitrovgrad, Russia
▼ 6th meeting of the Steering Committee, 12 July 2005, St. Petersburg, Russia
▼ 7th meeting of the Steering Committee, 14 June 2006, St. Petersburg, Russia

## Slide 6: Experimental matrix of METCOR
Phase 1: Tests with fully oxidized melts

## Slide 7: Experimental matrix of METCOR
Phase 2: Tests with suboxidized corium and tests with oxidized corium in steam

## Slide 8: Experimental methodology: Furnace section
1 – pyrometer shaft; 2 – cover; 3, 18, 19 – electromagnetic screens; 4 – quartz tube; 5 – crucible sections; 6 – inductor; 7 –melt; 8 – acoustic defect; 9 – fused ZrO2 grains; 10 – ZrO2 powder insulation; 11 – vessel steel specimen; 12 – top specimen calorimeter; 13 – bottom specimen calorimeter; 14 – kaolin wool insulation; 15 –ultrasonic sensor; 16 – thermocouples; 17 – crust; 20 – cylindrical support of the specimen
Technology of the induction melting in a cold crucible
Atmosphere – high-purity argon
Long-term expositions in a stationary regime
On-line measurements:
specimen temperature
melt surface temperature
specimen ablation depth
electric parameters
power in the furnace components

## Slide 9: Experimental methodology: Posttest analyses
Calculation of the whole electromagnetic system
Power deposition in the melt and its electric resistivity are determined Measured electric parameters of the system and power deposited into the furnace components are used in the numeric modeling
Integrated calculation of the electromagnetic system and melt thermohydrodynamics
Radial heat flux distribution in the specimen top is determined. Calculations of the whole electromagnetic system and boundary conditions on the crucible and specimen surfaces are used
Calculation of the specimen temperature conditions
Results of previous calculations, boundary conditions on the crucible surface and specimen calorimeters are used. The adequate agreement between calculations and thermocouple measurements is achieved by varying heat flux into the specimen and thermal resistance of the specimen side insulation
Physicochemical analysis of the ingot, specimen and interaction zone
XRF; SEM/EDX; optical microscopy; chemical analyses. Elemental and mass balances, initial and final compositions of the system and its components are determined

## Slide 10: Tests with suboxidized corium
Identified phenomenon of steel corrosion: U, Zr, O partitioning and partial eutectic melting (dissolution) of the vessel steel , IZ depth is limited by position of isotherm 1090 oC
Axial sections of specimens
МС6
МС7
МС8
МС9
Shrinkage cavity
Chip
Acoustic defect
EDX images of Interaction Zone
10 µm
500 µm
100 µm
Teut~1090ºC (DTA)
DTA of IZ in MC-8

## Slide 11: Tests with suboxidized corium (continued)
Model of ablation kinetics
2 main periods of ablation: incubation and fast ablation
fast ablation resulting in saturation
, mm/s
Tint – current temperature of steel surface 1090  Тint  1440C
TB – final temperature of steel surface after interaction termination (1090 oC for reactor application)
Incubation period: - oxidic melt tinc=8000+200 (70-Cn), s
30  Cn  70
- metallic melt
tinc=0

## Slide 12: Tests with suboxidized corium (continued)
Cn  30%
Analogous results for solid/liquid and liquid/liquid interactions obtained in METCOR and MASCA projects
Due to thermal gradient U and Zr concentrations in the interaction zone (METCOR) are lower than in the metallic melt (MASCA)
Thermal gradient Influence on chemical equilibrium:
Final concentrations of elements in metallic melt vs. steel mass fraction and Cn

## Slide 13: Tests with oxidized corium
Elemental phase composition
Element/ Phase 1 Phase 2
oxide w% w%
U M - 83.78
Zr K - 0.243
Fe K 70.00 3.85
O 29.00 12.11
UO2 - 95.00
ZrO2 0.30 0.40
Fe2O3 99.70 4.6
Identified phenomenon of steel corrosion: Surface oxidation of vessel steel; corrosion layer thickness and
stability is effected by corium composition and crust temperature
Example of Interaction Zone structure in MC-2

## Slide 14
Tests with oxidized corium (continued) IZ structures at different temperatures and corium compositions
UO2+x- ZrO2 - FeOy corium
UO2+x- ZrO2 (С-100 corium)
melt
melt
crust
crust
corrosion layer
corrosion layer
T
sol
T
sol
T
d
T
eut
T
s
<1230
°
C
T
s
³
1230
°
C
liquification
T
d
=T
eut
steel
steel
d
d
D
D

## Slide 15: Tests with oxidized corium (continued)
Corrosion model
Corrosion rates in air and in steam are similar
Decrease of corrosion rate following increase of iron oxides content in corium melt
Intensification of corrosion after reaching eutectic temperature of the interface between corrosion layer and corium
0.001
0.01
0.1
1
10
0.65
0.75
0.85
0.95
1.05
Corium B, air
Corium A, steam
Corium B, steam
W/q,
1/K
0
1
2
3
4
5
6
7
3
5
7
9
11
1230
°
С
1050
°
С
W/q
,
МW
m
h
mm
2
,
T
1613
1000
S
-
1/K
No eutectic interaction between corium and corrosion layer
Eutectic thinning of corrosion layer

## Slide 16
Tests with oxidized corium (continued) Corrosion model: modified Tamman equation for:
1) UO2+x- ZrO2 - FeOy corium
FeOy=20…30%, U/Zr=0.11…1.05
Ts <10500C
1340>Ts >10500C
Ts <12300C
2) UO2+x- ZrO2 (С-100 corium),
U/Zr  1.0
1340>Ts >12300C
Ts=720…12000C
q =0.30…1.29MW/m2
Ts = 1035…12350C
q = 0.95…1.1MW/m2
W – mm/h; q - MW/m2 ; T - K

## Slide 17: Example of plant application
Mass of ablated vessel steel vs. time
Lower head region after 20 h
Blue: calculation 1, red calculation 2
a) ablation depth of the lower head from the сalculation 2, grey: ablated steel b) temperature conditions of the vessel
the evaluated thickness of undamaged vessel wall is much smaller, if the vessel steel ablation is taken into account
vessel strength calculations are in progress
For suboxidised corium, VVER-1000 – type reactor, low pressure scenario, homogeneous molten pool, initial temperature of corium is 1500ºК. Calculation 1 – without physicochemical interactions Calculation 2 – the interactions have been evaluated by the empirical correlations

## Slide 18: Reporting

## Slide 19: Published papers
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, D.B. Lopukh, Yu.B. Petrov, A.Yu. Petchenkov, I.V. Kulagin, V.S. Granovsky, S.V. Kovtunova, V.V. Martinov, V.V. Gusarov. Experimental studies of oxidic molten corium – vessel steel interaction // Nucl. Eng. Design 210 (2001) 193-224.
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer, G. Cognet, O. Kymäläinen. New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel // Proceedings of ICAPP’04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4114
S.V. Bechta, V. B. Khabensky, V.S. Granovsky, E.V. Kroushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, L.P. Mezentseva, Yu.B. Petrov, D.B. Lopukh, M. Fischer, D. Bottomley, W. Tromm, M. Barrachin, E. Altstadt, P. Piluso, F. Fichot, S. Hellmann, F Defoort. CORPHAD and METCOR ISTC projects / Proc. of the first European Review Meeting on Severe Accident Research (ERMSAR-2005), Aix-en-Provence, France, 14-16 November 2005
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky, D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm, D. Bottomley, H. Tuomisto. Corrosion of vessel steel during its interaction with molten corium. Part 1: Experimental // NED, vol.236, 2006, pp 1810-1829
S.V. Bechta, V.B. Khabensky, S.A. Vitol, E.V. Krushinov, V.S. Granovsky,D.B. Lopukh, V.V. Gusarov, A.P. Martinov, V.V. Martinov, G. Fieg, W. Tromm, D. Bottomley, H. Tuomisto. Corrosion of vessel steel during its interaction with molten corium. Part 2: Model development // NED, vol.236, 2006, issue 13, pp 1362-1370,
S.V. Bechta, V.B. Khabensky, V.S. Granovsky, E.V. Krushinov, S.A. Vitol, V.V. Gusarov, V.I. Almiashev, D.B. Lopukh, W. Tromm, D. Bottomley, M. Fischer, P. Piluso, A. Miassoedov, E. Altstadt, H.G. Willschütz, F. Fichot. Experimental Study of Interactions Between Suboxidized Corium and Reactor Vessel Steel //Proceedings of ICAPP’06, Reno, NV USA, June 4-8, 2006, Paper 6054

## Slide 20: Papers in preparation Tentative titles:
Interactions of oxidized corium melt with vessel steel of VVER reactor (Analysis of the tests done in air and steam )
Corrosion of VVER vessel steel in conditions of in-vessel corium melt retention (Summarized results of the 1st and 2nd phases of METCOR, examples of plant application)

## Slide 21: Experimental matrix* for a new project: METCOR-P #3592
*) Letters of project support have been received from: - Dr J.H. Song, KAERI, Korea; - Dr H. Tuomisto, Dr O. Kymalainen, FORTUM, Finland; - Dr W Tromm, Dr A. Miassoedov, Forschungzentrum Karlsruhe (FZK),Germany; - Dr D. Bottomley, EUROPAISCHE KOMISSION, Institut fur Transurane (JRC ITU),Germany; - Mr. M. Fischer, AREVA NP GmbH, NEPR-G, Germany; - Dr E. Altstadt, FZR (FORSCHUNGSZENTRUM ROSSENDORF), Germany; - Dr H. Chalaye, CEA, France

## Slide 22: Conclusions
VVER steel corrosion mechanisms have been clarified for different melt compositions
The developed correlations can be used in the analyses of IVR with oxidized and suboxidized coria under different above-melt atmospheres
Finalization of corrosion studies requires the following experiments
- for oxidized corium: in the temperature range of the specimen surface exceeding 1200 oС,
- for suboxidized corium: at the vertical orientation of the specimen surface
- for vessel steel used in European reactors
METCOR-P project proposals #3592 has been prepared and distributed by ISTC in August 2006