## Slide 1: RESEARCH OUTLOOK (METCOR-P)
Presented by V. Khabensky
2nd METCOR-P project meeting
July 9, 2008, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: METCOR-P experimental matrix

## Slide 3: Proposals for the update of current experimental matrix
Task 1. Test: Interaction of the metallic melt enriched with U and Zr with a vertically-positioned vessel steel specimen
Proposals
Test: Interaction of the two-layered molten pool (metallic phase Fe-U-Zr-Cr-Ni-O – in the top, oxidic phase (С-70) – in the bottom) with a vertically-positioned vessel steel specimen.
The test will be made after the US system for corrosion kinetics measurement is appropriately adapted.
OR
Test: Interaction of molten suboxidized corium С-30 (С-70) with a horizontally-positioned vessel steel specimen.
The test is made to verify the developed model understanding and get the boundary temperature of the interaction ~ 1300ºC.

## Slide 4: Proposals for the update of current experimental matrix (2)
Task 2.
Test: Transients of C30 melt oxidation with inert atmosphere replacement by steam
Objective: determine oxidation kinetics
Proposal:
Test: Transients of C30 melt oxidation with water supply on top of the molten pool
Objective: determine oxidation kinetics
Test: Transients during the oxidation of metallic melt Fe-U-Zr-Cr-Ni-O, when neutral atmosphere is replaced by steam
Objective: determine heat fluxes and oxidation kinetics
Proposal:
Test: Transients at the two-layered molten pool oxidation by steam. Metallic Fe-U-Zr-Cr-Ni-O melt on top, suboxidized oxidic melt С70 – in the bottom of the pool
Objective: determine oxidation kinetics

## Slide 5: Proposals for the update of current experimental matrix(3)
Task 3.
3.1. Test: Interaction of suboxidized C30 melt with a European reactor vessel steel in the Ar atmosphere.
3.2. Test: Interaction of molten corium С100 with a European reactor vessel steel in the steam atmosphere.
Proposal
Test 3.1: according to the test matrix
Test 3.2: to replace it with a test on the interaction of molten corium C 100 and UO2+x-ZrO2-FeOy (in one test) with vessel steel in air
Objective: Study the corrosion rate and determine the interaction interface temperature, from which the corrosion intensification starts.