## Slide 1: Status of the ISTC project #3592 (METCOR-P)
Presented by V. Khabensky
2nd METCOR-P project meeting
July 9, 2008, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: METCOR-P project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZD, Germany
FORTUM, Finland
Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel (#3592 METCOR-P)

## Slide 3
Objectives of METCOR-P project
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:
Interaction at the vertical position of vessel steel specimen surface
European vessel steel specimen behavior
Oxidation effects

## Slide 4: Experimental matrix for the METCOR-P project

## Slide 5: Decisions of the 1st meeting (May 30, 2007, St. Petersburg) on the update of METCOR-P Work Plan matrix and test sequence
Task 1: to replace reference test with experiment “Interaction of molten corium UO2+x-ZrO2 with vessel steel in the oxidizing above-melt atmosphere. Test МСР-2»
Task 1: to conduct experiment “Interaction of molten corium Fe-U-Zr-Gr-Ni-O with vertically positioned vessel steel specimen in the argon atmosphere” after the МСР-1 posttest analysis, improvement of the corrosion kinetics measuring system and completion of МСР-2 and МСР-3 tests
Test МСР-2 to be followed by Task 2 test “Steam oxidation effect on the interaction zone of C-32 corium with vessel steel: МСР-3 test”
In order to prepare Task 3 implementation with the European vessel steel specimens to send a request with specimen dimensions and grade of steel*
* sent on 16 July 2007

## Slide 6: Tests completed within METCOR-P
Test | Name | Stage | Deliverables
МСР-1 | Interaction of molten corium with vertically positioned vessel steel specimen in the neutral atmosphere | Completed | Report
МСР-2 | Interaction of molten corium UO2+x-ZrO2 with horizontally positioned vessel steel specimen in the steam atmosphere (Instead of reference test) | Completed | Report
МСР-3 | Interaction of suboxidized corium melt with steel at the replacement of neutral atmosphere with steam | Experiment completed. Posttest analysis in progress | -

## Slide 7: METCOR publications
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental Study of Oxides Corium Interaction with Reactor Vessel Steel Samples // RASPLAV Seminar 2000, Munich, Germany, 14-15 Nov., 2000.
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental studies of oxidic molten corium – vessel steel interaction / Nucl. Eng. Design 210, (2001) 193-224.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Gornet G., Kymalainen O. New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel // Proceeding of ICAPP’04, Pittsburgh, P.A. USA, June 13-17, 2004, Paper 4114.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Fischer M., Bottomley D., Tromm W., Barrachin M., Altstadt E., Piluso P., Fichot F., Hellmann S., Defoort F. CORPHAD and METCOR ISTC projects // The first European Review Meeting on Severe Accident Research (ERMSAR-2005), Aix-en-Provence, France, 14-16 November, 2005.

## Slide 8: METCOR publications (2)
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 1: Experimental // Nucl. Eng. Des., 236 (2006) 1810-1829.
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 2: Model development // Nucl. Eng. Des., 236 (2006) 1362-1370.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Piluso P., Miassoedov A., Altstadt E., Willschufz H.G., Fichot F. Experimental Study of Interaction Between Suboxidized Corium and Reactor Vessel Steel // Proceeding of ICAPP’06, Reno, P.A. USA, June 4-6, 2006, Paper 6054.

## Slide 9: Publications during METCOR-P first year
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // Proceeding of ICAPP’08, Anaheim, CA USA, June 8-12, 2008, Paper 8052.
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Krushinov E.V., Kotova S.Yu., Kosarevsky R.A., Barrachin M., Bottomley D., Fischer M., Fichot F. Corium Phase Equilibria from MASCA, METCOR and CORPHAD Results // NED (in print).
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. VVER Vessel Steel Corrosion at Interaction with Molten Corium in Oxidizing Atmosphere // NED, (sent to co-authors for review).*
* Will be discussed in Dr. E. Altstadt presentation.

## Slide 10: METCOR-P current situation
1st year scope of work has been completed
1st year report has not been submitted to the ISTC and collaborators due to the suspended Export Control Commission permit
Agreement between the Rosatom and ISTC is prepared, which will eliminate the export control prohibition for METCOR-P. The agreement will be discussed at the ISTC Managing Board on July17 2008
In case of a positive decision the Project will be implemented in accordance with the Work Plan
If the decision is delayed, the Project will be implemented without submitting reports to the ISTC until an agreement between the Rosatom and ISTC is reached
In case of a negative decision the project implementation is stopped and, on agreement with CEG-SAM and collaborators a new project proposal is prepared, in which funding unused in Project # 3592 METCOR-P will be spent