## Slide 1: UO2+x-ZrO2 Corium Melt / Vessel Steel Interaction in Oxidizing Atmosphere ISTC project #3592 (METCOR-P)
Presented by V. Khabensky
2nd METCOR-P project meeting
July 9, 2008, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: Matrix of tests with refractory corium in oxidizing atmosphere

## Slide 3: MC1, MC2, MC10, MC11, MC12 experimental results
Corrosion of steel interacting with corium UO2+x – ZrO2 – FeOy, intensifies at > 1050С on the interaction interface
For corium UO2+x – ZrO2 – FeOy steel corrosion rate does not depend on the above-melt atmosphere ( air or steam)
For corium UO2+x – ZrO2 the influence of air on corrosion rate has nor been studied
A limited number of experimental regimes for corium UO2+x – ZrO2 has not shown corrosion intensification
A high corrosion rate of steel interacting with corium UO2+x – ZrO2 in comparison with UO2+x – ZrO2 – FeOy at < 1050 С on the interaction interface does not have an explanation
0.6
0.7
0.8
0.9
1
1.1
0.001
0.01
0.1
1
10
U
O
2
+
x
-Z
r
O
2
-
F
e
O
y
air MC1, MC2
s
t
e
a
m MC11
a
i
r
M
C12
s
t
e
a
m
M
C
1
2
(
W
/
q
)
=
2
.
6
Ч
1
0
3
e
x
p
(
-
1
0
1
0
0
0
/
(
R
T
s
)
)
+
1
.
3
Ч
1
0
1
9
e
x
p
(
-
5
0
9
0
0
0
/
(
R
T
s
)
)
U
O
2
+
x
-
Z
r
O
2
s
t
e
a
m MC10
(
W
/
q
)
=
4
.
9
Ч
1
0
3
e
x
p
(
-
1
0
1
0
0
0
/
(
R
T
s
)
)

## Slide 4: Experimental objectives of МСР-2 Interaction of UO2+x-ZrO2 corium with steel in he oxidizing atmosphere
Determine the influence of atmosphere (air, steam) on corrosion rate
Identify a reason for a higher corrosion rate of steel interacting with corium UO2+x-ZrO2 in comparison with UO2+x-ZrO2-FeOy, at Ts<1050ºC on the interaction interface
Determine the probability of corrosion intensification, when the interaction interface temperature approaches the temperature of steel melting
Specify the corrosion mechanism by the posttest analysis of the specimen, interaction zone and ingot and develop numerical correlation

## Slide 5: Results of tests with corium UO2+x-ZrO2 in the oxidizing atmosphere. Tests МС10, МСР-2
All experimental points for corium UO2+x-ZrO2 in the semi-logarithmic coordinates are described by the linear correlation. The corrosion rate intensification is not observed
For corium UO2+x-ZrO2 steel corrosion rate is identical in the air and steam atmosphere

## Slide 6: Results of the posttest physicochemical SEM/EDX analysis of the interaction zone for corium UO2+x-ZrO2
Corrosion layer composed by FeO is mostly or completely liquid
Corium crust, which has a considerable thickness in case of high-temperature corium, contains liquid-phase eutectic inclusions in the bottom part near the corrosion layer; it is mostly solid-phase
Crust of the UO2+x-ZrO2-FeOy corium, differently from the crust of UO2+x-ZrO2 corium, has through liquid-phase channels at Ts>1050ºС on the interaction interface
Corium crust is thicker than the corrosion layer by more than one order

## Slide 7: SEM-images of the interaction zone and the crust

## Slide 8: Interpretation of posttest analysis data
The final liquid-phase condition of the UO2+x-ZrO2 corrosion layer and its small thickness in comparison with the solid-phase corium crust (the linear corrosion rate from Ts temperature is maintained in the semi-logarithmic coordinates) means that the main diffusion resistance for Fe ions, which determine the corrosion rate, is corium crust
Absence of through liquid-phase channels in the UO2+x-ZrO2 corium crust, which are typical for corium UO2+x-ZrO2-FeOy at Ts>1050ºС does not cause the corrosion rate intensification in the studied temperature range on the interaction interface
A higher steel corrosion rate in comparison with corium UO2+x-ZrO2-FeOy at identical Ts values can be explained by a higher rate of Fe ion diffusion caused by a large difference of Fe concentrations on the steel surface and in the melt
Available results enable to specify corrosion mechanism and numerical correlation

## Slide 9: Specified structure of numerical correlation for UO2+x-ZrO2 corium
Corrosion model based on the Tamman equation is used for determining the structure of numerical correlation (1) where Ea – activation energy; А – const; δ – diffusion layer thickness for Fe2+; Т – diffusion layer temperature, K; R – universal gas constant.
δ is evaluated by the heat conductivity equation on the condition that the main diffusion resistance for Fe ions is corium crust
(2)
where λ – thermal conductivity of crust; Tsol, Ts – corium solidus temperature and steel surface temperature, respectively; q – density of heat flux from melt to steel.
By substituting (2) into (1) taking into account λ=const, T=Ts, we get the structure of a correlation generalizing the experimental data for corium UO2+x-ZrO2

## Slide 10: Numerical correlation for determining vessel steel corrosion rate at its interaction with corium UO2+x-ZrO2
Experimental data for corium UO2+x-ZrO2 , taking into account that for this composition Tsol=2723 K, are generalized by the correlation for determining steel corrosion rate

## Slide 11: CONCLUSIONS
Experimental studies have been completed on determining the corrosion rate of steel interacting with molten corium UO2-ZrO2 in a wide temperature range on the interaction interface in the atmosphere of air or steam
Atmosphere (air, steam) has not been found to influence the corrosion rate
Steel corrosion rate is not intensified in the whole Ts experimental range
Steel corrosion rate depends on the diffusion resistance of corium crust. The diffusion resistance of corrosion layer is small
A correlation is developed, which determines the steel corrosion rate at its interaction with molten corium UO2-ZrO2 in the oxidizing atmosphere
Taking into account that steel corrosion is more intensive at the interaction with corium UO2-ZrO2-FeOy at Ts>1050ºС, it is advisable to replace the test on the interaction of a European reactor steel specimen with corium UO2-ZrO2 with a test on the interaction with corium UO2-ZrO2-FeOy at high Ts values (Task 3)