## Slide 1
Status of the ISTC project #3690 on the “Fuel assemblies behaviour under severe accident top quenching conditions in the PARAMETER-SF test series”
(PARAMETER-SF3 and PARAMETER-SF4 experiments)
FSUE SRI SIA “LUCH”
IBRAE RAS
OKB “GIDROPRESS”
ISTC
CEG-SAM – 16, Moscow, Russia, September 8-9, 2009

## Slide 2
Status of the ISTC project #3690 on the “Fuel assemblies behaviour
under severe accident top quenching conditions in the
PARAMETER-SF test series (PARAMETER-SF3 and PARAMETER-
SF4 experiments):
The results of the PARAMETER-SF4 experiment. V. Nalivaev;
Results of PARAMETER-SF3/SF4 pre and post-test numerical modeling. A. Kiselev;
Post-test examinations of the PARAMETER-SF fuel assemblies.
T. Yudina
Progress reports

## Slide 3: The Structure of Project
The basis:
- The decision on financial support of the Project #3690 from ISTC 13.07.2007;
- The agreement under the Project #3690 between ISTC and FSUE SRI SIA “LUCH” 01.12.2007
The basic participants:
FSUE SRI SIA “LUCH”
IBRAE RAS
OKB “GIDROPRESS”
Another participants:
JSC “VNIINM”
SSC RF-IPPE
RSC “Kurchatov Institute”
Foreign collaborators:
FZK, JRC-ITU, GRS (Germany)
PSI (Switzerland)
EdF, CEA (France)
AEKI (Hungary)
INRNE (Bulgaria)

## Slide 4: Acknowledgement
Ch. Bals, K. Trambauer (GRS)
E. Beuzet, J.-S. Lamy (EdF)
J. Burchley (PSI)
O. Coindreau, F. Fichot (IRSN)
Notes: 4
4

## Slide 5
Experimental results of the PARAMETER-SF4 Experiment
Presented by V. Nalivaev
(Status of Project # 3690)
CEG-SAM – 16, Moscow, Russia, September 8-9, 2009
FSUE SRI SIA “LUCH”
IBRAE RAS
OKB “GIDROPRESS”
ISTC
Notes: 5
5

## Slide 6
The study of behaviour of FA of VVER-1000 under severe accident during bottom quenching of the assembly heated up to the temperature 1750°C in the environment of air
Objective

## Slide 7
Scenarios of PARAMETER-SF4 experiment

## Slide 8
The monitoring system of air
The analysis of oxygen
OLCT-20D
Controll gas - О2
Range of measurements - 0 - 30 % v.
The basic error:
Resulted 0 - 5 %v. - ±5 %;
Relative - 5 - 30%v. - ±5 %
Measurement of air flow rate
IN - FLOW
Controll gas - (20 %) O2 + (80 %) N2
Range of measurements - 0 - 3,75 kg/h
Accuracy of measurements - ±0,5 %

## Slide 9
Central rod of monitoring system of air

## Slide 10
Test bundle
Main technical characteristics
Main technical characteristics
Bundle type VVER-1000
number of fuel rods 19
- heated 18
- unheated 1
Grid type triangle
Grid pitch, mm 12.75
Spacing grid Zr1%Nb
- height, mm 20
- spacing, mm 255
Shroud Zr1%Nb
- shape cylinder
- height, mm 1450
Thermal insulation ZrO2 ZYFB-3
- thickness, mm 23
- height, mm 1450

## Slide 11
Some results of PARAMETER-SF4 experiment
Electrical power

## Slide 12
Flow rate of steam, argon and air

## Slide 13
Gas pressure of test bundle

## Slide 14
Claddings temperature

## Slide 15
Claddings temperature at level Z=1300

## Slide 16
Claddings temperature at level Z=900-1250

## Slide 17
Claddings temperature at level Z=400-800

## Slide 18
Claddings temperature at level Z=0-300

## Slide 19
Temperature of central rod, shroud and thermoinsulation
Temperature of central rod
Temperature of shroud
and thermoinsulatin

## Slide 20
Measuring of volumetric oxygen concentration

## Slide 21
Pressure into the bundle during bottom flooding

## Slide 22
Temperature of upper and bottom parts of bundle
Claddings temperature
of upper part of test
bundle
Claddings temperature
of bottom part of test
bundle

## Slide 23
Measuring of volumetric hydrogen concentration
Volumetric hydrogen
concentration
Mass of hydrogen

## Slide 24
Appearance of bundle after tests
upper part
(1000 – 1300)
central part
(500 – 1000)
bottom part
(100 – 500)

## Slide 25
CONCLUSIONS
1. Experiment PARAMETER-SF4 on simulating the initial stage of severe accident, including the stages of the air ingress and the bottom flooding, has been carried out.
2. The main parameters of experiment:
- the steam flow rate ~ 3.5 g/s at temperature ~ 500 °С;
- the argon flow rate ~ 2.0 g/s at temperature ~ 300 °С;
- the air flow rate  0.5 g/s;
- the duration of the pre-oxidation stage ~ 6000 s at temperature ~ 1200 °С;
- the temperature of bundle at the moment of switching on the system of the bottom flooding – 1740 °С.
3. The total of hydrogen measured by continuous monitoring systems of hydrogen (SOV-3), has not exceeded ~110 g. The hydrogen measured the duration of the pre-oxidation stage has not exceeded ~21 g.
4. The cooling overheated up to ~ 1740°C of the bundle has been achieved for
~ 1000 s at the water flooding from bottom with flow rate ~ 80 g/s.
5. Conservation and preliminary cutting of the bundle has been carried out.