## Slide 1
ISTC Project #3831
Heating and Retention of Corium
Stage I: middle scale
A. V. Kondrashenko, VNIIEF
(edited by J. Stuckert, KIT)

## Slide 2
Test facility

## Slide 3
4 gas burners before test initiation on 16.12.2009; 16:00

## Slide 4
60°
5 m
PyroTechnic Compound (PTC):
Zr + Fe2O3 briquettes (mbr=120 g)
introduced with Dt ~ 7 s
during ~ 500 s
with 280 J/briquette
mirror
2nd camera
1st camera

## Slide 5
burning phases

## Slide 6
splashes after briquette introduction; m splashes ~ 1.5-2 kg

## Slide 7
TC placement: 2 W/Re (19, 20),
20 bottom NiCr/Ni (13-18, 21-34),12 sidewall NiCr/Ni (1-12),
3 pyrometer plate positions (35 – 37)
bottom TC:
3 TC depth 5 mm
5 TC depth 10 mm
5 TC depth 20 mm
5 TC depth 25 mm
4 TC depth 30 mm

## Slide 8
3 points of pyrometer measurements: W, Mo, Ta foils at crucible bottom;
view from crucible top

## Slide 9
NiCr/Ni TC measurements at elevation -30 mm

## Slide 10
crucible bottom
W/Re TC measurement
“W”
“Re”
relocation
of contact
“W” – Fe – “Re”

## Slide 11
Frozen melt tablet and lateral scale

## Slide 12
Frozen melt tablet, top view; D~45 cm

## Slide 13
Frozen melt, side view; m=105 kg, H~18.5 cm

## Slide 14
Crucible bottom.
Concrete bottom ablation: 30 mm
Concrete side
ablation: 25 mm

## Slide 15
hotel
“Oktyabrskaya”
icy Oka river
Jahrmarktdom
Chkalov staircase from Kremlin to Volga
icy Volga
Nizhny
Novgorod,
January 2010