## Slide 1
Numerical simulation of Oxidation
of the Suboxidated corium melt
Presented by Sergey Smirnov
METCOR-P Seminar 2010
St-Petersburg , Russia
June, 1, 2010
D.V. Efremov Scientific Research Institute of Electrophysical Apparatus
A.P. Alexandrov Research
Institute of Technology

## Slide 2
Objective:
Prove the possibility of correct numerical simulation
of the oxygen deposition rate on the melt free surface
Reason:
Preparation a paper
“Oxidation kinetics of the corium melt under a hard accident PWR”
based on materials presented on METCOR-P Seminar
May, 2009
St-Petersburg , Russia

## Slide 3
Furnace Schematic
1 – Tanks with Ar and O2; 2 – Mass flow controller; 3 – Mixing device; 4 – Electrochemical oxygen sensor; 5 - Inductor furnace; 6 – Middle area filter; 7 – Analytical filter; 8 – Scrubber; 9 – Gas flow meter; 10 – Fan; 11 – Vibrator; 12 – Copper gas main

## Slide 4
Pr1-EV1 experiment
(Geometry without inner quartz tube)
Ar flow rate (Gar5),
O2 flow rate (Gar6),
Inlet oxygen component part (Ox1),
Outlet oxygen component part (Ox2),
Outlet gas temperature (ТС22)
Experimental Oxygen deposition rate is 9.3±0.3 mg/s

## Slide 5
Experimental Oxygen deposition rate is 15±1 mg/s
2. EV1 experiment
(Geometry with inner quartz tube)
Ar flow rate (Gar5),
O2 flow rate (Gar6),
Inlet oxygen component part (Ox1),
Outlet oxygen component part (Ox2),
Outlet gas temperature (ТС22)

## Slide 6
Mathematical model describes
3D unsteady flow of Ar:O2 gas mixture
taking into account:
Heat and mass transfer (convection, radiation, molecular heat conductivity, molecular diffusion and thermal-diffusion);
Gravitation forces (free convection);
Turbulence (Large Eddy Sumulation);
Oxygen deposition on the free melt surface

## Slide 7
Governing equations for modeling heat and mass transfer
Continuity
Heat transfer
Mass transfer
Navier-Stokes
equation with effective viscosity
1
(3)
(1)
(2)
(4)

## Slide 8
Smagorinsky model for turbulent viscosity – Large Eddy Simulation
Radiative heat transfer along opaque/transparent boundary
(7)
(5)
(6)
Heat transfer along solid/solid interfaces, gas/liquid interfaces
Governing equations for modeling
of the heat and mass transfer
2

## Slide 9
Equations for the oxygen deposition rate on the melt surface
Hertz–Knudsen equation for
deposition rate
on a surface
Sticking coefficient
Oxygen partial pressure on the melt surface
3

## Slide 10
(2) Inlet total flow rate – Qinl = 10 slm;
(6) Gas velocity on the walls – ;
(4) Outlet pressure – ;
(1) Inlet gas mixture – Ar:O2 = 0.8:0.2;
(7) Melt free surface temperature – Tsurf = 2560 oC
(5) Side wall temperature – Tw = 27 oC;
(3) Inlet gas temperature – Tinl = 27 oC;
Boundary conditions
Geometry with
inner quartz tube

## Slide 11
Computational domain
Gaps between tubes of the cold crucible are inlets for gas flow into the volume over the free melt surface

## Slide 12
COMPUTATIONS
RESULTS

## Slide 13
13
Animations without quartz tube -
Pr1-EV1
Temperature, y = 1 mm
Oxygen fraction, y = 0 mm
y – the distance of the horizontal cross section from the melt free surface

## Slide 14
14
Animations with quartz tube -
EV1
Temperature, y = 1 mm
Oxygen fraction, y = 0 mm
y – the distance of the horizontal cross section from the melt free surface

## Slide 15
15
Free melt surface
Animations of the oxygen deposition rate without quartz tube - Pr1-EV1
Dynamic evolution

## Slide 16
Free melt surface
16
Oxygen deposition rate with quartz tube - EV1
Quasi -Steady
Distribution

## Slide 17
17
Comparison of the experimental data
and computations results
Pr1-EV1
EV1
Computations
mg/s
10.80 (±0.6)
12.80 (±0.05)
Experiment
9.3 (±0.3)
15.0 (±0.8)
Relative deviation
%
+15
-16
Possible reasons for divergence of experimental data and calculations:
Non-uniform temperature distribution on the melt free surface
Different gaps between crucible sections
Insufficiently accurate description of conditions near crucible sections

## Slide 18
18
Conclusions:
Installation of internal quartz tube stabilizes above-melt gas flow.
Calculated and experimental data of oxygen deposition rate on the melt free surface have a good agreement.
Perspectives for numerical model development:
Take into account the sensitivity of equilibrium pressure and oxygen sticking coefficient to local parameters of the melt free surface.
Describe multi-component gas mixtures with heterogeneous and gas-phase chemical reactions.

## Slide 19
19
Thank you for the attention!