## Slide 1: Preliminary PARAMETER SF4 post-test calculation with ATHLET-CD
Ch. Bals, W. Luther Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany

## Slide 2: Content
  Boundary conditions for PARAMETER SF4 experiment and simulation with ATHLET-CD
  Input model and options for ATHLET-CD post-test calculation
  Results of PARAMETER SF4 post-test calculation:
    Temperatures
    Quench fronts
    Hydrogen generation
  Conclusions

## Slide 3: PARAMETER SF4: Boundary Conditions and Simulation with ATHLET-CD (1)
Power supply – temperature:
cold bundle at start of test: 21 °C at 0 s
pre-oxidation phase: max. plateau temperature of ~1200 °C is reached at ~ 8000s with power increase to ~7 kW; temperature is kept until ~ 14000 s with power regulation between 7 and 8 kW;
at 14000 s power reduction to ~ 4 kW to reduce Tmax to ~ 900 °C before air injection is started at t=16000s
again power increase to ~ 6 kW during air injection phase; power is switched off at 17412 s (max. temperature of 1740 °C is measured)
bottom injection of water is started at 17434 s; valve of air supply is closed at 17511 s
bottom flooding is finished at 17908 s when bundle is cooled down

## Slide 4: PARAMETER SF4: Boundary Conditions and Simulation with ATHLET-CD (2)
Argon inlet flow : - constant rate of 2.0 g/s - switch to upper injection after start of reflood - T ~ 280°C
Steam inlet flow: - starts at 1716 s with flow rate of ~ 3.5 g/s until 16022 s when air injection is started, - T ~ 500°C
Air inlet flow: - 0.5 g/s (0.1 g/s O2, 0.4 g/s N2 for simulation) - air injection starts at 16035 s - air injection is switched off at 17511 s (after opening the bottom flooding valve)
Bottom flooding : - initial water level of 450 mm below inlet pipe - is initiated at 17434 s (Tmax=1740 °C is reached; power is switched off at 17412 s) - Water flow rate: 80 – 30 - 80 g/s, Water temperature: 25 °C - is finished at 17908 s (bundle is cooled down)
Bundle pressure: ~ 4 bar (constant bound. condition for simulation)

## Slide 5: Input model for PARAMETER calculations with ATHLET-CD
as for pre-test calculation:
Flow Channels
    Central Bundle (with rods) CORE2 85.7 %
    Outer Bypass CORE3 14.3 %
    Cross connection
    Cooling Jacket
Structures
    Rods: ROD1 (1 unheated rod) ROD2 (6 heated rods) ROD3 (12 heated rods)
    Grids (6)
    Shroud / Insulation
    Cooling Jacket Wall
    Structures at top of bundle (upper plate, separation sheet)
Changes compared to previous calculations (SF2, SF3):
    Additional fills O2FILL, N2FILL for air injection

## Slide 6: Options for ATHLET-CD post-test calculation of SF4
  Zr / steam cladding oxidation model: Cathcart / Prater-Courtright correlation (IOXMOD = 15) was used instead of Leistikow / Prater-Courtright correlation (IOXMOD = 19) (for SF4 pre-test calculation and SF2 post-test calculation IOXM=19 was taken; for SF3 post-test calculation IOXMOD = 15 was used for better agreement of H2 data);
  Zr / air oxidation model: Correlation derived for Ar / O2 mixture (AEKI, IOXAIR=6) and IOXAIR=1 (Air, Powers) were used (SF4 pre-test calculation: IOXAIR=1); for presented results IOXAIR=6 was used
  Candling velocity of melt : WSL= 0.006 m/s (instead of 0.01 m/s)
  External resistance 1 mΩ/rod (same as for pre-test calculation)
  Hydraulic diameter in core region: DH=3.8·10-3 m (=DH at grid position) (as for pre-test calculation)
  Default values for other models (e.g. interfacial friction model, quench model) are used

## Slide 7: Options for ATHLET-CD post-test calculation of SF4
Available correlations for Zr /air oxidation in ATHLET-CD

## Slide 8: Results of PARAMETER SF4 post-test calculation
Temperatures during pre-oxidation period (before air oxidation):
  - maximum temperature is calculated at 1250 mm elevation as in test
  - given time function for power leads to a maximum plateau temperature of Tmax = 1150 °C which is slightly underestimated compared to data;
  - during temperature decrease between 14000 s and 16000 s a max. temperature of ~ 800 °C is achieved ; lower than measured

## Slide 9: Results of PARAMETER SF4 post-test calculation
Temperatures (air ingress period):
  - due to oxygen starvation in the upper bundle region the higher air oxidation and therefore the stronger temperature excursion move to lower elevations in agreement between measured data and calculation (nitride formation is not considered up to now in the simulation);
  - maximum temperature of 1740 °C is reached at t=17412 s in test; (highest temp. at bundle elevations 500 - 800 mm); max. temperature in simulation at 500 mm position (T=1840°C)
  - calculation with IOXAIR=6 (derived for Ar/O2 mixture) shows better agreement of temperature increase compared to IOXAIR=1 (Powers air correlation, with IOXAIR=1 temperature increase too fast)

## Slide 10: Results of PARAMETER SF4 post-test calculation
Oxygen starvation:
  - after a time period of ~ 1300 s following the start of air injection (t=16035 s) oxygen starvation can be observed at the elevations above ~ 600 mm
- resulting time period of oxygen starvation in upper bundle region (until start of injection): Δt=134 s (17300 - 17434 s)

## Slide 11: Results of PARAMETER SF4 post-test calculation
Temperatures (quenching period):
- bottom flooding is initiated at 17434 s (Tmax = 1740 °C is reached in exp.)
- after start of flooding temperature increase in simulation is underestimated compared to test data (steam oxidation) (max. temperature T=1984°C at 17 510 s in 300 mm elevation)
- due to cooling only from the bottom last quench is calculated at the upper bundle elevations; comparison with data is difficult due to failure of many thermocouples
- total cooling of the bundle slightly shorter compared to data (~ 400 s)

## Slide 12: Results of PARAMETER SF4 post-test calculation
Shroud temperatures:
- temperature increase during air oxidation phase is calculated in good agreement with test data with option IOXAIR=6
- temperature escalation after start of flooding is underestimated in the simulation

## Slide 13: Results of PARAMETER SF4 post-test calculation
Hydrogen generation:
- mass of hydrogen generated during pre-oxidation period : 17,5 g 21 g measured
→ only slightly underestimated with used correlation IOXM=15
- Hydrogen generated during quench: ~ 17 g 86 g measured → strongly underestimated with used correlation IOXM=15

## Slide 14: Conclusions
  ATHLET-CD calculates in good agreement the maximal temperatures within the pre-oxidation phase with the given time function for power;
  Air injection with a rate of 0.5 g/s leads to a oxygen starvation at the positions above ~ 600 mm after a time period of 1300 s (at ~17300 s, start of air injection at 16000 s); therefore the elevation of the maximum temperature moves to lower positions in agreement with test data (no nitride formation is considered up to now);
  Temperature increase during air oxidation phase is calculated in good agreement with test data with IOXAIR=6;
  Temperature increase after start of reflood (steam oxidation) seems to be underestimated in the simulation (max. temperature = 1984°C = 2257°K); comparison with measured data is difficult due to the failure of many thermocouples; the status of the bundle after the test shows that there had been higher temperatures than really measured )
  Time needed for bottom quenching: ~ 400 s (slightly shorter compared to test);
  Total hydrogen generation is 34 g, much lower than measured (107 g);