## Slide 1
Fuel assembly tests
under severe accident conditions
Status of Project # 3194
FSUE SRI SIA “LUCH”
IBRAE RAS
FSUE EDO “GIDROPRESS”
Presented by W. Nalivaev
March, 2006, Paris

## Slide 2
Progress reports
Experimental results of complex starting-up and
adjustment actions on preparation of the PARAMETER-SF1 Experiment.
2. Numerical simulation of the PARAMETER-SF1
Experiment.
3. Presentation of specification on simulation of PARAMETER facility by collaborators.
Presented by W. Nalivaev
Presented by T. Judina
Presented by A. Kisselev

## Slide 3
Experimental results of complex starting-up and adjustment actions on preparation of the PARAMETER-SF1 Experiment
March, 2006, Paris
FSUE SRI SIA “LUCH”
IBRAE RAS
FSUE EDO “GIDROPRESS”
Presented by W. Nalivaev

## Slide 4
Main Tasks:
- Development of technological systems for carrying out of Experiment
- Check up of technological systems
- Carrying out of control test up to 1000 C
- Program of the PARAMETER-SF1 Experiment

## Slide 5
Main technical characteristics
Test bundle
Bundle type VVER-1000
number of fuel rods 19
- heated 18
- unheated 1
Grid type triangle
Grid pitch, mm 12.75
Spacing grid Zr1%Nb
- height, mm 20
- spacing, mm 255
Shroud Zr1%Nb
- shape hexahedron
- height, mm 1650
Thermal insulation ZrO2 ZYFB-3
- thickness, mm 29/24,5
- height, mm 1525

## Slide 6: Test instrumentation

## Slide 7: Test facility
Functional scheme
Main technological systems for carrying out of Experiment:
System of separate input of argon;
The monitoring system of balance of steam and water;
System of top flooding;
The monitoring system of hydrogen

## Slide 8
The rate of argon and hydraulic characteristics steam-gas a path
№№ items | Parameter | Size of parameter
1 | Gar |  2 g/s
2 | par | 1,0 MPa
3 | T6 | 450 C
4 | p bn | 0,34 MPa
5 | p10 | 0,34 MPa
6 | p11 | 0,1 MPa
7 | p12 | 0,17 MPa
8 | R5 |  2 g/s

## Slide 9
Parameters of a steam flow
№№ items | Parameter | Size of parameter
1 | T1 | 570 C
2 | p1 | 0,8 MPa
3 | p2 | 0,4 MPa
4 | T2 | 550 C
5 | Gs | 3±0,1 g/s
6 | Tst in | 420 C

## Slide 10
Monitoring system of balance of steam and water
№№ items | Parameter | Size of parameter
1 | Gs | 3±0,1 g/s
2 | Mass (M5) | 18,4 kg
3 | Time | 6000 s
4 | Gs (M5) | 3,07 g/s

## Slide 11
Parameters of the top flooding system
№№ items | Parameter | Size of parameter
1 | G7, g/s | 44,4; 40,5; 39,5; 35,8
2 | p7, MPa | 1,0
3 | p bn, MPa | 0,1; 0,26; 0,36; 0,45
4 | Mass (M4), kg | 3,82; 3,56; 3,32; 2,94
5 | Time, s | 86; 88; 84; 82

## Slide 12
Monitoring system of hydrogen on reference gas mixtures (Ar + X%H2)
№№ Items | Reference gas mix. (Ar + X %H2), X%
1 | 0,5
2 | 4,0
3 | 10

## Slide 13
Some experimental results of control Test
Sequence diagram of tests

## Slide 14
Shroud and Thermoinsulation Temperatures
Electrical Power
Bundle Temperature
Measuring rod
Test Bundle parameters

## Slide 15
Results of top flooding
№№ items | Parameter | Size of parameter
1 | G7, g/s | 40 - 38
2 | p7, MPa | 1,0
3 | p bn, MPa | 0,30 – 0,34
4 | T bn, C | 800
5 | Time, s | 180

## Slide 16
The PARAMETER-SF1 Experiment
Stage | Stage substance | Main parameters |  |  | 
 |  | Bundle temperature, С | Medium | Heating/ cooling rate | Time, s
1 | Electric heating of the fuel bundle within argon | 500 | argon with flow rate of 2 g/s | 0.16 | 0-3000
2 | Electric heating of the fuel bundle within the steam and argon flow | 500 | steam and argon with flow rate of 3/2 g/s | 0 | 3000-5000
3 | Heating of the fuel bundle (phase I) | 500-1200 | steam and argon with flow rate of 3/2 g/s | 0.2 K/s | 5000- 8500
4 | Pre-oxidation of the fuel bundle |  1200 | steam and argon with flow rate of 3/2 g/s | 0 | 8500-11500
5 | Heating of the fuel bundle (phase II) | 1200-1900 | steam and argon with flow rate of 3/2 g/s | 0,1-0,3 K/s | Define experimentally as deign temperature will be reached
6 | Flooding of the fuel bundle from the top (~5 s after Tmax=1900 C reached) | up to saturation | water with flow rate of 40 g per bundle | 100 – 10 K/s | 300