## Slide 1: Progress report on the UO2 – CaO system
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology
Presented by E. Krushinov
3rd PRECOS Project Meeting
June 2, 2010, St. Petersburg
ETU
Saint-Petersburg
SPbSIT (TU)

## Slide 2
Contents
Available binary diagrams
Experimental matrix
Test procedures
Test results
Conclusions

## Slide 3: Available UO2-CaO phase diagrams
Alberman K.B., Blakey R.C.,
Anderson J.S.
(1951)
Amato I.
(1966)
Teut =2080±20 °C
(eut) – 55%mol.CaO
UO2(ss) – 47%mol.CaO

## Slide 4: Available UO2-CaO phase diagrams (2)
Holc J., Kolar D.
(1986)
Teut =1850±20 °C
eut – 63%mol.CaO
UO2(ss) – 30%mol.CaO
CaO (ss) – 0.35%mol.UO2
The published versions of the phase diagram differ by:
the CaO melting temperature and Tliq curve position
presence/absence of chemical compounds
limits of components solubility in solid solutions and compositions of the latter
eutectic point coordinates

## Slide 5
Experiment | Content, mol.% |  | Atmosphere | Experimental objectives
 | UO2 | CaO |  | 
PRS4 | 50.0 | 50.0 | Nitrogen | Determination of the liquidus temperature. Determination of the components final solubility in the formed solid solutions
PRS5 | 1.0 | 99.0 |  | Determination of the liquidus temperature.
PRS6(1) | 17.2 | 82.8 |  | 
PRS6(2) | 10.2 | 89.8 |  | 
PRS10 | 36.2 | 63.8 |  | Determination of the liquidus temperature. Determination of the components final solubility in the formed solid solutions
PRS11 | 30.0 | 70.0 |  | 
PRS12(1) | 60.0 | 40.0 |  | Determination of the liquidus temperature
PRS12(2) | 70.0 | 30.0 |  | 
LPH |  | 100 | Air | Determination of the CaO melting temperature
Experimental matrix
- Carried out during the reported quarters

## Slide 6
Test procedures
Of the tests in the PRS series included the following operations:
Molten pool production and homogenization
Molten pool depth and bottom crust thickness measurement
Molten pool surface shifting above the inductor upper coil, registration of liquid/solid regions formation on the melt surface
Molten pool returning to the initial position, pool exposure at this position for the restoration of heat and electromagnetic losses in cooled components of the furnace
Melt sampling
Shifting the molten pool surface above the inductor upper coil to the previously fixed position, video recording of formation of liquid/solid regions on the melt surface
Repetition of operations 4,5,6
Of the tests aimed at the eutectic nucleus formation the additional operations included:
Molten pool shifting below the inductor lower coil until a noticeable change of the induction heating parameters
Switching-on of the mechanism of molten pool pulling out from the inductor at 8-10 mm/h
HF heating disconnection after the complete melt crystallization

## Slide 7
Experimental objectives
Tliq determination
Determination of the components final solubility in the formed solid solutions
Charge composition
Mol% 36.2UO2 + 63.8CaO
Tliq was measured 2 times by VPA IMCC with melt sampling
Samples
Tliq
From 4000 s, the pool was pulled out from inductor at 8.5 mm/h for 2 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
PRS 10 test results

## Slide 8
VPA IMCC: Example of thermogram 2 from the test showing melt surface
    Results of Tliq measurements: 1876, 1886oC
Sample | ChA | XRF
 | UO2 mol.% | 
№1 | 38.1 | 41.4
№2 | 35.7 | 38.6
PRS 10 test results (2)

## Slide 9
SEM/EDX analysis of the melt sample (top) and ingot periphery (bottom)
Dendritic microstructure of the melt sample
Sample | ChA | XRF | EDX
 | UO2 mol.% |  | 
№1 | 38.1 | 41.4 | 34.9
№2 | 35.7 | 38.6 | 33.9
Primary crystallization phase
 | UO2 | CaO
 | mol.% | 
P1 | 53.8 | 46.2
Compositions of melt samples of the unsaturated solid solution have been determined
There is a discrepancy between the results of SEM/EDX and (XRF+ChA)
Quenched
sample
300µm
70µm
PRS 10 test results (3)
CaUO3 |  | UO2 | CaO
EDX | mass % | 84.5 | 46.9
 | mol% | 53.1 | 68.7
CaO |  | UO2 | CaO
EDX | mass % | 8.4 | 91.7
 | mol% | 1.9 | 98.1

## Slide 10
Eutectic |  | UO2 | CaO
EDX | mass % | 69.1±0.7 | 30.9±0.2
 | mol.% | 31.8±0.3 | 68.2±0.3
Eutectic |  | UO2 | CaO
EDX | mass % | 70.4±1.0 | 29.6±1.3
 | mol% | 33.1±0.2 | 66.9±1.3
UO2 ss |  | UO2 | CaO
EDX | mass % | 83.3 | 16.7
 | mol.% | 50.8 | 49.2
Ca2UO4 |  | UO2 | CaO
EDX | mass % | 68.7 | 31.3
 | mol.% | 31.3 | 68.7
UO2 ss |  | UO2 | CaO
EDX | mass % | 81.1 | 18.9
 | mol.% | 47.2 | 52.8
Phase mix |  | UO2 | CaO
EDX | mass % | 61.0 | 39.0
 | mol.% | 24.5 | 75.5
SEM/EDX analysis of the ingot (central zone)
A eutectic crystallization zone with the final solid solution has been formed. Compositions of the eutectics and the solid solution have been determined
Composition of the final solid solution
PRS 10 test results (4)

## Slide 11
Eutectic |  | UO2 | CaO
EDX | mass % | 72.0±1.8 | 28.0±1.4
 | mol.% | 34.8±0.6 | 65.2±1.6
SEM/EDX analysis of the ingot (eutectic zone)
The eutectic composition has been determined by EDX in the eutectic crystallization zone without solid solutions
PRS 10 test results (5)
25µm
2.86µm

## Slide 12
Experimental objectives
Tliq determination
Determination of the components final solubility in the formed solid solutions
Charge composition
mol.% 30UO2 + 70CaO
Tliq was measured 3 times by VPA IMCC with melt sampling
From 4829 s, the pool was pulled out from inductor at 8.5 mm/h for 2.4 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Samples
Tliq
PRS 11 test results

## Slide 13
VPA IMCC: Example of thermogram 3 from the test showing melt surface
    Results of Tliq measurements: 1912, 1910, 1907oC
Sample | Cha | XRF
 | UO2 mol.% | 
№1 | 30.5 | 32.0
№2 | 30.1 | 32.9
№3 | 30.8 | 34.5
Melt samples
composition
PRS 11 test results (2)
SEM/EDX in progress

## Slide 14
Experimental objectives
Tliq determination at high UO2 content
Two melt compositions have been
realized within one melting cycle
6 melt samples were taken and Tliq was
measured 6 times by VPA IMCC
Charge composition
mol.% 60UO2 + 40CaO
Samples
Tliq
Samples
Tliq
PRS 12 test results

## Slide 15
VPA IMCC: Fragment of the experiment thermogram 3 showing melt surface
    Tliq was measured 3 times: 2440, 2420 and 2432oC
Melt samples composition
Sample | Cha | XRF
 | UO2 mol.% | 
№1 | 57.3 | 55.03
№2 | 52.3 | 56.3
№3 | 59.3 | 55.1
PRS 12 test results (2)
Charge composition, mol.% 60UO2 + 40CaO
SEM/EDX in progress

## Slide 16
VPA IMCC: Fragment of the experimental thermogram 4 showing melt surface
    Tliq was measured 3 times: 2589, 2620 and 2595oC
Charge composition (after CaO addition into the melt)
mol.% 70UO2 + 30CaO
Melt samples composition
Sample | Cha | XRF
 | UO2 mol.% | 
№4 | 71.6 | 70.3
№5 | 64.8 | 70.1
№6 | 64.0 | 68.6
SEM/EDX in progress
PRS 12 test results (3)

## Slide 17
CaO Melting Point Measured by LPH in IVTAN
Experimental Thermogram
Peculiarities of CaO:
Low absorption coefficient below 1500-2000K
Boiling temperature of approximately 3300K, which is close to the melting temperature
Specimens melting procedure:
- Preliminary heating up to 1750K
- Controlled heating with a profiled laser pulse
- Coupling temperature measurement with a high-speed spectropyrometer
- Melt surface temperature fields registration with a high-speed camera
- Thermograms mathematical processing
Supposing that ε=0.85-0.9→Tmelt= 3160 ± 30K
ε for CaO will be refined in a different test

## Slide 18
Comparison of CaO solubility with CEA data
BSE images of the URAN3 ingot
BSE images of the URAN7 ingot
Micrograph of the VP-U1 test
The PRECOS tests with the UO2-CaO system, as well as similar CEA tests, have shown a high degree of CaO solubility in UO2 and discovered such a chemical compound as UCaO3
According to GEMINI2 and the TDBCR001 modeling (Chevalier, 1997) the first solid phase (a-phase) has the following compositions: U0.59Zr0.22Ca0.19O1.80 for the URAN3 composition (without silica), U0.76Zr0.21Ca0.02O2.02 for the URAN7 composition (with 12%wt silica) and U0.42Zr0.45Ca0.11O1.86 for the VP-U1 composition
One phase for the VP-U1 composition depleted in zirconium with a general composition: “UCaO3”
α –phase: U0.40Zr0.38Ca0.22O1.6.
α-phase: U0.44Zr0.28Ca0.28O1.8
α-phase: U0.35Zr 0.37Ca 0.26O 1.7
U0.47Ca0.53O1.78
UCaO3

## Slide 19
Test results on the UO2 - CaO system
Compositions of the final solid solutions and the eutectics will be refined after SEM/EDX has been performed for PRS12
The posttest analysis of samples from the corium ingot from VULCANO VP-U1, an ECOSTAR test, has detected CaO solubility in UO2 (aproximately 47.9 мол.%) in one of the samples

## Slide 20
Test results on UO2 - CaO system
Test | Sample No. | Content, mol.% |  | Tliq, °С
 |  | UO2 | CaO* | 
PRS-4 | Sample 1 | 49.803.5 | 50.20 | 2188±33
 | Sample 2 | 50.053.5 | 49.95 | 2195±33
PRS-6 | Sample 1 | 26.051.7 | 73.95 | 2417±36
 | Sample 2 | 26.251.7 | 73.75 | 2370±36
 | Sample 3 | 17.371.1 | 82.63 | 2550±38
PRS-10 | Sample 1 | 39.752.8 | 60.25 | 1876±28
 | Sample 2 | 37.152.6 | 62.85 | 1886±29
PRS-11 | Sample 1 | 31.252.2 | 68.75 | 191229
 | Sample 2 | 31.502.2 | 68.50 | 191029
 | Sample 3 | 32.652.3 | 67.35 | 190729
PRS-12 | Sample 1 | 56.173.9 | 43.83 | 244036
 | Sample 2 | 54.303.8 | 45.70 | 242036
 | Sample 3 | 57.204.0 | 42.8 | 243236
 | Sample 4 | 70.954.9 | 29.05 | 258939
 | Sample 5 | 67.454.7 | 32.55 | 262039
 | Sample 6 | 66.304.6 | 33.70 | 259539
*) determined from the residue
The table presents compositions of samples averaged on the basis of chemical and XRF analyses
The EDX analysis is still underway, therefore the table does not contain final compositions of the eutectics and solid solution

## Slide 21: Conclusions
Experimental results confirm the Holc’s version of the UO2-CaO phase diagram in the liquidus domain and allow its refinement.
The preliminary results on CaO solubility in UO2, as well as the discovered chemical compounds, confirm the subsolidus part of the diagram by Amato
Investigations of this system are to be concluded in Quarter 9 by: - refining compositions of the final solid solutions and of the eutectics (samples have been already prepared, however problems with SEM/EDX exist)
- refining the degree of CaO emissivity and its melting point (at IVT RAN)
Upon completing SEM/EDX for PRS11 and 12, a decision about the necessity in additional tests will be taken