## Slide 1
First results on UO2 – FeO – SiO2 and UO2 – FeO – CaO systems
Presented by S. Kotova
3rd PRECOS Project Meeting
June 2, 2010, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology
ETU
Saint-Petersburg
SPbSIT (TU)

## Slide 2
Contents
Available binary diagrams and test planning
UO2 – FeO - SiO2 system
- thermodynamic prediction
- experimental matrix
- description of PRS 13 test
- posttest analysis for PRS 13
- GPRS 33-36 test results
UO2 – FeO - СаО system
- thermodynamic prediction
- experimental matrix
- description of PRS 14 test
- posttest analysis for PRS 14

## Slide 3
UO2–FeO–SiO2 system
Pt | UO2 | FeO | Objectives
 | mol % |  | 
1 | 5.0 | 63.3 | eutectic (5 UO2 – 95 Fe2SiO4)
2 | 30.0 | 46.7 | liquidus solidus
3 | 70.0 | 20.0 | 
4 | ~3 | ~71 | eutectic
5 | ~3 | ~58 | 
6 | 15.0 | 46.7 | liquidus solidus
7 | 35.0 | 20.0 | 
8 | 20.0 | 7.0 | miscibility gap
9 | 10.0 | 10.0 | 
10 | 5.0 | 25.0 | 
2500
Fe2SiO4
80
60
40
20
UO2
1600
1300
1900
2200
T, C
2800
mol % Fe2SiO4
?
UO2
SS
1300
1700
2100
2500
20
40
60
80
FeO
FeO, mol. %
T, °C
L+SS
L
Published
UO2
SiO2
FeO
CORPHAD
CORPHAD+PRECOS
Fe2SiO4
?
?
1
2
3
4
5
6
8
10
9
7
SiO2
FeO
1200
1400
1600
1800
80
60
40
20
1723
1377
T, C
Fe2SiO4
L1 + L2
crystobalite
+ L
tridymite + L
tridymite + fayalite
L +
wustite
fa + w
Воwen N. L., J. P. Sсhairer, Amer. Journ. Sci., 24, 141, 177, 1932.
Allen W. C, R. B. Snow, Journ. Amer. Ceram. Soc, 38, № 8, 264,1955.
1377
2FeOSiO2
FeO, mol. %
90
80
70
SiO2
FeO
1204±2
1177±2
1150
1250
1350
T, C
In progress

## Slide 4
UO2–FeO–CaO system
1300
1700
2100
2500
UO2
20
40
60
80
FeO
FeO, mol %
T, °C
SS
L+SS
L
Published
Pt | UO2 | FeO |  | Objectives
 | mol % |  |  | 
1 | 50.0 |  | 0 | CaUO4-x Ca2UO4
2 | 33.3 |  | 0 | 
3 | 20.0 |  | 50.0 | 
4 | 6 |  | 75 | eutectic
5 | ?*) |  | ? | 
6 | ? |  | ? | 
7 | ? |  | ? | liquidus solidus
8 | ? |  | ? | 
9 | ? |  | ? | 
10 | ? |  | ? | 
Allen W. C, R. B. Snow, Journ. Amer. Ceram. Soc, 38, № 8, 264,1955.
?
CaO
UO2
FeO
CORPHAD
3
CaUO4-x
Ca2UO4
In progress
*) – Compositions to be discussed

## Slide 5
Thermodynamic prediction of the eutectic point position calculated by GEMINI2+NUCLEA05
UO2–FeO–SiO2 system
The composition was determined using data on the eutectic points of binary systems. A point in the center of a triangle that forms at the ‘pure phase’ and ‘eutectics’ lines intersection was taken as the starting point
Presumably, the FeO–based phase will be the phase of primary crystallization in this point
The eutectic temperature is about 111050С
?
Ternary eutectic
PRS 13

## Slide 6
UO2 – FeO – SiO2 system
Experimental matrix

## Slide 7
UO2 – FeO – SiO2 system: PRS 13 test results
Experimental objectives
Charge composition
Mol% 30.00 UO2 + 46.67 FeO +23.33 SiO2
Tliq was measured 4 times by VPA IMCC and accompanied by melt sampling
From 3276 s, the pool was pulled out from inductor at 9 mm/h for 3.6 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Tliq determination by VPA IMCC.
Determination of the ternary eutectic composition
Samples
Tliq

## Slide 8
UO2 – FeO – SiO2 system: PRS 13 test results (2)
Procedure

## Slide 9
# 3
# 4
# 2
UO2 – FeO – SiO2 system: PRS 13 test results (3)
VPA IMCC: Example of thermogram 1 from the test showing melt surface
    Results of Tliq measurements: 2055, 2083, 2092, 2079oC

## Slide 10
Corium ingot longitudinal section
А flake was chipped out from zone I for an analysis in the Galakhov microfurnace. A visual judgement of the microstructure allowed a suggestion that it was the eutectic zone
A metallic inclusion with a mass of 1.1 g was discovered in the corium ingot lower part (Fe content according to XRF is 98.35 mass %). This finding proves the absence of Fe+3 in the ingot
The ingot mass is sufficiently smaller than that of the charge, therefore melt composition cannot be correctly determined from the loaded charge
Material balance
UO2 – FeO – SiO2 system: PRS 13 test results (4)
Metallic inclusion
Zone I
Posttest analysis

## Slide 11
Chemical analysis of melt samples
UO2 – FeO – SiO2 system: PRS 13 test results (5)
In progress:
- SEM/EDX analysis of melt samples;
- chemical analysis of other fused products (ingot, crusts, dry spillages and aerosols) for composing the elemental material balance

## Slide 12
UO2 – FeO – SiO2 system: PRS 13 test results (6)
Tliq and Tsol determination in the Galakhov microfurnace
Sample 2
1704C
1755C
1846C
1898C
2017C
Visual polythermal analysis in the Galakhov microfurnace Tsol= 1755С; Tliq=2017С
Tliq, determined by the VPA IMCC (208330С) and by the Galakhov method (2017С) for the composition in question differ by 66С, presumably, due to the interaction of the sample with the holder in the Galakhov microfurnace
Beginning of melting
Complete spreading

## Slide 13
UO2 – FeO – SiO2 system: PRS 13 test results (7)
Visual polythermal analysis in the Galakhov microfurnace Tsol=1118С; Tliq=1528С The difference of Tsol from Tliq indicates the noneutectic sample composition (e.g., the sample was chipped out from not eutectic zone)
Tliq and Tsol determination of sample cut out from Zone 1 in Galakhov microfurnace
1118C
1179C
1191C
1264C
1528C
Beginning of melting
Complete spreading

## Slide 14
Experimental objectives
Annealing, melting and quenching in the Galakhov microfurnace (estimation of ternary eutectic position)
Test | Content, mol.% |  |  | Tempera-ture, С | Exposure time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS33 | 5.0 | 70.0 | 25.0 | 1100 | 60 | Annealing
 |  |  |  | 2100 | 5 | Melting and quenching
GPRS34 | 10.0 | 80.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 5 | Melting and quenching
GPRS35 | 20.0 | 73.0 | 7.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 5 | Melting and quenching
GPRS36 | 1.7 | 65.5 | 32.8 | 1100 | 60 | Annealing
 |  |  |  | 1300 | 20 | Melting
 |  |  |  | 1300-900 | 240 | Cooling at 100C/h
Tliq determination
Ternary eutectic point determination
UO2
SiO2
FeO
Fe2SiO4
GPRS33
GPRS35
GPRS34
GPRS36
8
10
9
UO2 of >99.0 % purity, SiO2 of 99.99% purity, charge mass – 150 mg, molybdenum crucibles  6 mm.
UO2-FeO-SiO2 system:GPRS 33-36 test results(8)

## Slide 15
UO2-FeO-SiO2 system:GPRS 33-36 test results (9)
XRD of sample of GPRS 36 test
2
The analysis was done using FARAD desktop diffractometer with CrKα1 radiation (λ = 0.22897 nm)

## Slide 16
UO2-FeO-SiO2 system:GPRS #33-36 test results(10)
SEM/EDX GPRS 33
Conditions:
Charge composition, mol% 5 UO2 + 25 FeO +70 SiO2
isothermal exposure at 1100°С for 1 h., heating up to 2100°С, 5-min. exposure, quenching
SQ1
167 m
25 m
0.92 m
.P1
.P2
.P3
No macostratification was found in the oxidic part of the polished section
Microstructure resembling that of the ‘heavy’ liquid in the UO2-SO2 system. As a result of the interaction between the melt and the crucible, the composition got depleted in Fe, but no molybdenum was found in the oxidic part

## Slide 17: SEM/EDX GPRS 34
Fe
UO2
SiO2 with inclusions
FeSiO3
124 m
25 m
49.9 m
12.5 m
100 m
UO2-FeO-SiO2 system:GPRS #33-36 test results(11)
Conditions:
Charge composition, mol% 10 UO2 + 10 FeO +80 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1950°С and a 5-min. exposure, quenching
Indication of MG
The microstructure is nonuniform. Inclusions of irregular shape indicate that the melt exposure time was insufficient (equilibrium was not reached). The globules of heavy liquid contain Femet drops
6.67 m
100 m
SiO2 with inclusions
Mo(Fe)
UO2
SQ2
SQ1
SQ3

## Slide 18
UO2-FeO-SiO2 system:GPRS #33-36 test results(12)
SEM/EDX GPRS 35
4 m
2.5 m
167 m
6.67 m
144 m
Conditions:
Charge composition, mol%
20 UO2 + 7 FeO +73 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1850°С, 5-min. exposure, quenching
SQ1
SQ3
SQ2
Though the macrostructure is uniform, the microstructure is extremely inhomogeneous and resembles that in UO2-SiO2 near the critical point

## Slide 19: SEM/EDX GPRS 36
UO2-FeO-SiO2 system:GPRS #33-36 test results(13)
SQ2
144 m
40.1 m
1.67 m
SQ1
Conditions:
Charge composition, mol% 1.7 UO2 + 32.8 FeO +65.5 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1300°С, 20-min. exposure, chilling from 1300 down to 900°С for 240 min.
Microstructure in the lower part of the crucible shows the eutectic crystallization. In terms of composition, this eutectics lies within a specific triangle UO2-Fe2SiO4-SiO2.

## Slide 20
UO2-FeO-SiO2 system: GPRS #33-36 test results(14)
SiO2
Bulk composition of the total microstructure in GPRS 35
‘Heavy’ liquid in GPRS 34 (T from Tq up to Tm)
Composition of the light matrix in GPRS 34 (T~Tm)
Composition of the ‘light’ liquid with globules in GPRS 34 (T~Tq~1850C)
Composition of the liquid at T~Tq~1950C (above MG)
Characteristic points of the diagram
Initial composition of the charge
Light matrix composition in GPRS 35 (T is presumably around Tm)
Composition of globules in the light matrix in GPRS 35 (T is presumably around Tm)
Triple eutectics composition in GPRS 36
Solid phase composition in GPRS 36
Bulk composition in GPRS 33 (no MG)

## Slide 21
UO2-FeO-SiO2 system
Summary:
Stratification has been confirmed for the compositions obtained in the tests GPRS 34 and 35. However, compositions of the coexisting liquids should be refined, since melt exposure in these test was insufficient for attaining equilibrium
The temperature in GPRS 35 was around the critical value
Melt composition in GPRS 33 is beyond MG
The problems with performing GPRS tests are connected with:
-SiO2 evaporation (SiO);
-Fe - Mo interaction, which causes a shift in the composition relative to the initial charge
First data on ternary eutectic composition have been obtained in GPRS 36 test
It is proposed to carry out the following tests:
  A test with the composition (mol.%) 5 UO2 + 25 FeO +70 SiO2, though with a smaller content of Fe and quenching from a lower temperature of 1900°С
  A test with the composition (mol.%) 10 UO2 + 10 FeO +80 SiO2 at 1950°С with a longer exposure time and a smaller content of Fe
  Quenching of the composition (mol.%) 20 UO2 + 7 FeO +73 SiO2 from 1800°С for determining the monotectic temperature and composition of the phases that coexist in the vicinity of the monotectic composition
  Refinement of the monotectic composition (e3), synthesis of e1 and e2, since the question of the binary section Fe2SiO4-UO2 is still open

## Slide 22
UO2–FeO–CaO system
Thermodynamic prediction of the eutectic point position calculated by GEMINI2+NUCLEA05
A Gemini calculation for the proposed point predicts the appearance of a liquid phase composed of (mol.%) 68.7 FeO, 3.4 UO2, 27.9 CaO at 1019oС. The point is located practically on the boundary (adjoins the UO2-CaO and CaO-FeO binary eutectics) of a triangle bounded by binary eutectics
Ternary eutectic

## Slide 23
UO2–FeO–СаO system
Experimental matrix

## Slide 24
UO2 – FeO – CaO system: PRS 14 test results
Experimental objectives
Charge composition
Mol.% 20.1UO2 + 66.7FeO +13.2CaO
Tliq,,was measured by VPA IMCC 3 times; video record of one measurement could not be deciphered. Samples were taken 3 times
Samples
From 4519 s, the pool was pulled out from the inductor at 9 mm/h for 5.9 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Tliq determination by VPA IMCC.
Determination of eutectic composition
Tliq

## Slide 25
PRS-14 test procedure
UO2 – FeO – CaO system: PRS 14 test results (2)

## Slide 26
UO2 – FeO – CaO system: PRS 14 test results (3)
VPA IMCC: Example of thermogram #2 showing melt surface
    Results of Tliq measurements: 1238, 1247oC
# 3

## Slide 27
Corium ingot
Insignificant debalance and closeness in masses of the ingot and charge make it possible to assess composition of the melt on the basis of charge composition
Material balance
UO2 – FeO – CaO system: PRS 14 test results (4)

## Slide 28
UO2 – FeO – CaO system: PRS 14 test results (5)
XRF and Chemical analysis of melt samples
* - determined from residue
The results of corium samples XRF and chemical analysis were found to differ significantly
XRF results are believed to be more accurate, since the content of CaO was not determined by chemical analysis, but calculated from the residue
In progress: - the SEM/EDX analysis of melt samples; - XRF and chemical analysis of other fused products (ingot, crusts, dry spillages and aerosols) for composing the elemental material balance.

## Slide 29
UO2 – FeO – CaO system
The measured liquidus points: 19.3±1.0 mass % UO2; 66.5±3.3 mass % FeO; 14.2±0.7 mass % CaO
Tliq= 1238±20 °C
19.3±1.0 mass % UO2; 66.7±3.3 mass % FeO; 14.0±0.7 mass % CaO Tliq= 1247±20 °C
A strategy for investigating a system may be devised only after clarity regarding compositions or solid solutions in the CaO-UO2 binary system has been reached. The supposed eutectic point lies, on the one hand, within the eutectic triangle, and, on the other hand, within a triangle bounded by FeO-Ca2UO4-CaO. After the ingot has been cut and the zone of the final crystallization examined by SEM/EDХ, it will become clear if the eutectic composition had been synthesized or not. If not, then it is proposed to investigate a composition from the UO2-CaUO4-x-FeO subsystem, mol.%: 80 FeO, 15 UO2, 5 CaO + 1 mass % of getter (carbonyl iron).
Summary: