## Slide 1: PRECOS experimental matrix Logic of experimental process Experimental program (1 st & 2 nd quarters)
ISTC PRECOS Project
#3813
A.P. Alexandrov Research Institute of Technology
Presented by Victor Gusarov
1st PRECOS Meeting
ISC RAS
Saint-Petersburg

## Slide 2: PRECOS Matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U–Zr–Fe–O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
 | U–O |  |  |  | 
2 | ZrO2–FeOy | Air and oxygen | liquidus, solidus, solubility limits | 2 | 3
 | UO2–SiO2 | Argon | liquidus, solidus, tie-lines in the miscibility gap, eutectic point | 1 | 7
 | CaO–UO2 |  | liquidus, solidus, solubility limits, eutectic point | 1 | 7
3 | UO2–FeO–SiO2 |  | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2–FeO–CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10
 | ZrO2–FeO–SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2–FeO–CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by French partners (1 system), System (atmosphere) proposed by German partners (1 system), System (atmosphere) proposed by Russian partners (1 system) | 2 | 3

## Slide 3: Logic and sequence of system study
simple
complex
one
many
Number of components
well
studied
little studied
Study
Experimental methods
developed
not enough
developed
Facilities
checked
update and test are needed
Sequence of system study
known
unknown
systems
methods
use of complex methods
developement of methods
invoke additional methods
- methods have area of intersection (test of results according to convergence of data of different techniques)
- methods complement each other
Reliability of results

## Slide 4: Complex of methods
Chemical composition of a system before, during a process and after experiment
Phase transformation depending on temperature and pO2
Phase composition of a system (quantitative and qualitative analysis)
Chemical composition of the phases
Peculiarities of investigated systems (1st, 2nd quarters)
The determined parameters for phase diagram construction
Phase structure
U-Zr-Fe-O – interaction with crucibles
UO2±, SiO2 (SiO) – high volatility at high temperatures
FeOx, UO2± – control of oxygen partial pressure in gas phase is required
– difficulty of oxygen content determination in non-stoichiometric phases
– redistribution of oxygen between coexisting phases during heating-cooling

## Slide 5: Complex of methods
Visual-polythermal analysis (Induction melting in the cold crucible, Galakhov microfurnace, high-temperature microscopy)
Complex thermal analysis (DTA(DSC)/TG/Mass-spectrometry)
In situ measurements
X-ray powder diffraction
X-ray fluorescent analysis
Post-test analysis
Chemical analysis
Scanning electron microscopy/energy-dispersion X-ray analysis (wave- dispersion analysis)
Mössbauer spectroscopy
Reduction melting in carbon crucibles
Laser pulse method

## Slide 6: Logic and sequence of system study
The systems |  |  |  | 
Metal-oxide systems |  | Oxide systems |  | 
binary | multicomponent | binary | ternary | multicomponent
 |  | UO2-SiO2 |  | 
 |  |  | UO2-SiO2-FeO | 
 | U-Zr-Fe-O |  | ZrO2-SiO2-FeO | 
 |  | UO2-CaO |  | 
 |  |  | UO2-FeO-CaO | 
 |  |  | ZrO2-FeO-CaO | 
 |  |  |  | realistic complex corium mixture
U-O
ZrO2-FeOx

## Slide 7
?
?
?
?
?
1st & 2 nd quarter experimental work
ZrO2
FeO
Fe2O3
Fe3O4
?
ss
CORPHAD
SiO2
FeO
UO2
?
CORPHAD
CORPHAD
Fe2SiO4
?
?
?
?
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2080
2070±10
mol % SiO2
UO2-SiO2
ZrO2-FeOy
UO2-FeO-SiO2

## Slide 8
?
?
?
?
1st & 2 nd quarter points
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2080
2070±10
mol % SiO2
UO2–SiO2
1
2
3
4
5
6
7
8
9
10
Pt | SiO2, mol % | Objectives
1 | 97.5 | eutectic
2 | 95.0 | liquidus
3 | 90.0 | Miscibility gap determination (T=2080C)
4 | 78.0 | Miscibility gap determination (T=2500C) (T=2300C)
5 | 70.0 | Miscibility gap determination (T=2080C)
6 | 60.0 | liquidus
7 | 50.0 | 
8 | 40.0 | 
9 | 30.0 | 
10 | 20.0 | 
PRECOS matrix – 7 points

## Slide 9
?
?
ZrO2
FeO
FeO1.5
FeO1.33
?
ss
CORPHAD
1st & 2 nd quarter points
FeO (mol %)
1300
1700
2100
2500
80
60
40
20
T, C
FeO
ZrO2
(1332±5)C
2900
Published
1300
1700
1900
2100
2300
2500
2700
Т, C
mol %
60
40
FeO1.5
10-7
10-5
10-3
10-1
101
103
air
80
10-1
101
10-7
10-5
10-3
103
105
105
air
ZrO2
20
Fe0.938O
700
900
1100
1500
FeO
10-1
10-3
ZrO2–FeOy
Pt | FeO1.5, mol % | Atmosphere | Objectives
1 | 95 | air | eurectic
2 |  | O2 | 
3 | 90 | air | 
 |  | O2 | 
4 |  |  | 
5 | 20 | air | solid solutions
 |  | O2 | 
6 |  |  | 
7 | 10 | air | 
8 |  | O2 | 
9 | 60 | air | Miscibility gap determination
10 |  | O2 | 
11 | 50 | air | 
 |  | O2 | 
12 |  |  | 
13 | 40 | air | 
 |  | O2 | 
14 |  |  | 
PRECOS matrix – 3 points

## Slide 10
?
1st & 2 nd quarter points
1300
1700
2100
2500
UO2
20
40
60
80
FeO
FeO, mol %
T, °C
SS
L+SS
L
Published
2600
SiO2
80
60
40
20
UO2
2000
1600
1800
2200
2400
T, C
2800
mol % SiO2
SiO2
UO2
UO2–FeO–SiO2
FeO
CORPHAD
CORPHAD
Fe2SiO4
?
Pt | UO2 | FeO | Objectives
 | mol % |  | 
1 | 1 | 1 | eutectic
2 | 2 | 2 | liquidus solidus
3 | 3 | 3 | 
4 | 4 | 4 | eutectic
5 | 5 | 5 | 
6 | 6 | 6 | 
7 | 7 | 7 | liquidus solidus
8 | 8 | 8 | stratification
9 | 9 | 9 | 
10 | 10 | 10 | 
PRECOS matrix – 10 points
?
2500
Fe2SiO4
80
60
40
20
UO2
1600
1000
1300
1900
2200
T, C
2800
mol % Fe2SiO4
?
1
2
3
4
5
6
8
10
9
7
FeO, мол. %
1200
1400
1600
1800
80
60
40
20
SiO2
FeO
1723
1377
T, C
Fe2SiO4
Ж1 + Ж2
кристоб. + Ж
трид. + Ж
трид. + фаялит
Ж +
вюстит
фаялит + вюстит

## Slide 11
1st & 2 nd quarter publications
Eutectic crystallization in the ZrO2–Fe2O3–Fe3O4 system
(Rus. J. Inorg. Chem?)
UO2–SiO2 – manuscript preparation
Phase diagram of the UO2–SiO2 system – manuscript preparation and sending (JNM?)
Structural and chemical transformations of the ZrO2(FeOy) solid solutions during heat treatment in different gas atmospheres
(J. Eur. Ceram. Soc.?)
ZrO2–FeOy – manuscript preparation

## Slide 12
Conclusions