## Slide 2: AREVA Proposition for Task 4 of the ISTC PRECOS Programme
André Fargette
PEPA-G
St Petersburg, June 2011

## Slide 3: Selection of corium composition
Typical EPR core inventory
  UO2 ~ 146 tons
  ZrO2 ~ 49 tons (from ~ 36 tons of Zr)
Pit MCCI: addition of ~ 120 tons of concrete

## Slide 4: Selection of corium composition
Suggested oxidic composition:
Constituent | mass fraction (-)
UO2 | 0.476
ZrO2 | 0.160
SiO2 | 0.168
Fe2O3 | 0.138
Al2O3 | 0.015
CaO | 0.043

## Slide 5: Thermodynamic properties
Calculations performed with:
  Database: NUCLEA10
  G minimizer: CHEMAPP
Solidus ~ 1100°C
Liquidus ~ 1945°C
Phases at equilibrium: FCCC1, SPINEL, TCHERNOBYLITE, CWSWALASTONITE, ANORTHITE, TRIDYMITE, U4O9, U3O8

## Slide 6: Thermodynamic properties

## Slide 7: Thermodynamic properties
Liquid composition near solidus:
Constituent | Mass fraction (-)
Al1O1.5 | 1.70%
Al1Ca0.5O4Si1 | 19.23%
Ca1O3Si1 | 40.45%
Fe1O1 | 5.36%
Fe1O1.5 | 11.62%
O2Si1 | 21.22%
O2Zr1 | 0.25%
Remaining solid near liquidus: FCCC1 (UO2, ZrO2)