## Slide 1: New results in the SiO2-FeOx system
ISTC PRECOS
Project #3813
A.P. Alexandrov
Research Institute of Technology
Presented by Svetlana Kirillova
4rd PRECOS Meeting
ETU
Saint-Petersburg

## Slide 2
2
  Miscibility gap boundaries and eutectic determination
Research objectives
Experimental technique
  High temperature microscope (annealing, melting, quenching)

## Slide 3
FeOx-SiO2 system results problems
Mezentseva L.P. et al (2006)
1723
1500
1600
1400
1700
FeOx 20 40 60 80 SiO2
mol.%
L
1535
Fe3O4 + L
SiO2 +L
SiO2 + L
L1+L2
Fe2O3 + SiO2
1388
1473
1800
Fe3O4 + SiO2
T, С
2 FeOSiO2
FeO
FeO1.5
SiO2
20
40
60
80
20
40
60
80
20
40
60
80
mol. %
FeOFe2O3
1500
1400
Crystob.
Iron
W
H
M
F
1300
L1+L2
Muan A. (1955)
3
Mark`s questions
In Air

## Slide 4
Initial composition
4
 | By synthesis | By analysis (EDX data)
SiO2 content, mol. % | 60.0 | 67.1
1723
1500
1600
1400
1700
FeOx 20 40 60 80 SiO2
mol.%
L
1535
Fe3O4 + L
SiO2 +L
SiO2 + L
L1+L2
Fe2O3 + SiO2
1388
1473
1800
Fe3O4 + SiO2
T, С
In Air
15
20
25
30
40
45
55
60
65
70
75
80
35
50
2, deg
-
SiO
2
(Quarz)
-
SiO
2
(Cristobalite)
-
Fe
2
O
3
(Hematite)
Annealing at T=1300 C in air (8 h)

## Slide 5
HTM investigations
5
1400 С
1435 С – start of sample motion
1550 С – start of sample melting
1600 С – begin of intensive melting

## Slide 6
Test matrix
6
Test | T, C | Exp. time, min | Note
1 | 2105 | 5 | Annealing
 | 2163 | - | Quenching
2 | 1530 | 5 | Annealing
 | 1604 | - | Quenching
3 | 1600 | 5 | Annealing
 | 1603 | - | Quenching
4 | 1586 | - | Quenching
5 | - | - | Uncontrolled overheating
6 | 1650 | 5 | Annealing
 | 1692 | - | Quenching
7 | 1700 | 5 | Annealing
 | 1750 | - | Quenching
Test | T, C | Exp. time, min | Note
8 | 1800 | 5 | Annealing
 | 1868 | - | Quenching
9 | 1900 | 5 | Annealing
 | 1878 | - | Quenching
10 | 1950 | 5 | Annealing
 | 1924 | - | Quenching
11 | 1888 | - | Quenching
12 | 2000 | 5 | Annealing
 | 2000 | - | Quenching
Peculiarities: 10 C/min. exposure, quenching

## Slide 7
Preliminary results
7
1500
1600
1400
1700
FeOx 20 40 60 80 SiO2
mol.%
L
Fe3O4 + L
SiO2 +Ж
SiO2 + L
L1+L2
Fe2O3 + SiO2
1435
1550
1800
Fe3O4 + SiO2
T, С
1650
1900
?
2000
?
?

## Slide 8
8
Conclusions
The miscibility gap in the FeOx-SiO2 system was observed
Monotectic and eutectic temperatures is outlined
Tie lines was estimated Twelve experiments have been made
There is very many differences with previous works
A research strategy modifications and step by step calculation adjustment is needed