## Slide 1: Plans for further and their experimental realization
Presented by S. Bechta
3rd METCOR-P project meeting
May 27, 2009, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: METCOR-P experimental matrix
5 remaining tests

## Slide 3: Interaction at the vertically positioned interface (1)
U-Zr- Fe(Cr, Ni)-O; atmosphere: Ar The composition corresponds to that of the metallic melt, e,g, С-30+40% SS, Ts =1400ºC →MC6 (in accordance with the matrix)
US measurement scheme
USS with mirror
Radial location of USS
Test 1.2

## Slide 4: An alternative: horizontal orientation of the interface
No indication of significant influence of orientation on the final corrosion state from MCP-1 test results
But corrosion kinetics was not measured due to technical difficulties of ultrasonic diagnostic application
Guaranteed measurement of the interaction kinetics and better accuracy of the IZ temperature boundary determination for horizontally oriented interface
Interaction at the vertically positioned interface (2)
Test 1.2

## Slide 5: Molten corium oxidation transients (1)
Melt: UO2 + ZrO2 + Zr (С-30)
A considerable more accurate determination of the oxidation rate
A possibility of the pool surface temperature measurement
Oxidizer: Ar + O2 instead of steam (in contrast to the matrix)
Objective: determination of influence of the oxide pool surface crust on the oxidation rate (oxygen diffusion coefficient)
3 steady-state temperature regimes; the final oxidation index is С-50 An option: replacement of the atmosphere with Ar after every oxidation transient, exposure and steady-state measurements for posttest crust thickness modeling
Posttest calculations of oxygen diffusion coefficient
Test 2.2

## Slide 6: Molten corium oxidation transients (2)
Objective: determination of influence of the metal pool surface crust on the oxidation rate (oxygen diffusion coefficient)
Test 2.3
Variant 1
Oxidation of solid U-Zr- Fe(Cr, Ni)-O specimens in air at Т = 900 and 1000ºC with different exposure time (analogous to METCOR)
Variant 2
Two-liquid pool: C-30 + 40% SS (molten metal at the top) Oxidizer: Ar + O2
Option 1
Vertical water-cooled tube (permitting measurement of water temperature at different heights) along the pool axis
Option 2
Determination of the crust crystallization peculiarities under thermogradient conditions (primary crystallization zones)

## Slide 7: Molten corium oxidation transients (3)
Alternatives to the tests 2.2 and 2.3
Option 1
Variant 1 Melt: С-30 in Ar
Objective: determination influence of the crust formation conditions on its composition and properties
Rapid melt crystallization on the water-cooled rod (e.g. annular tube) dipped into the melt
Option 2
The same, with slow (8 mm/hour) submerging of rod into the melt
Heat fluxes to the rod are measured during the tests
Posttest analysis of the crust
Variant 2
Melt: С-30+Boron
Objective: determination of the influence of В on the interaction of the suboxidized molten corium with vessel steel
2 tests with different melt composition, e.g. B concentration

## Slide 8: Interaction of molten corium with European vessel steel
Test 3.1
Test 3.2
Melt: UO2+ZrO2+Zr, C-30, in Ar, Ts=1400C (MC6) in accordance with the matrix
UO2+x+ZrO2, air instead of steam
2-3 steady-state temperature regimes, Ts=900…1200C
Addition of Fe into the melt, its oxidation and formation of the UO2+x+ZrO2-FeOy melt
3 – 4 steady-state temperature regimes, Ts=1200…900C
Option 1
Option 2
Option 3
Europe steel blanks have arrived thanks to AREVA good offices, custom clearance is done by ISTC, transportation from Moscow is in progress

## Slide 9: Conclusions
Collaborator comments and recommendations to the proposed tests are welcomed
Next tests on the corium interaction with European vessel steel should be coordinated ASAP (during this meeting if possible)