## Slide 1
“Examination of VVER fuel behaviour under severe accident conditions”
Progress report on the project # 1648.2
Presented by A.Goryachev, RIAR

## Slide 2
Study of the spent fuel rod segments behavior under reflood conditions.
Integral experiment of QUENCH type using model bundle with 31 VVER fuel rod simulators.
Development of models and codes to describe VVER core behavior under severe accident conditions (“quench” stage).
1648.2 Project ISTC structure
Involved Institutions: RIAR, IBRAE, JSC MSZ, FZK, IRSN, JRC-ITU, CEA/DEN/DSNI

## Slide 3
Study of the spent fuel rod segments behavior under reflood conditions.

## Slide 4
Study of the spent fuel rod segments behavior
under reflood conditions.
Stages of work

## Slide 5
Unirradiated Simulator
Test rig furnace

## Slide 6
Design test regime

## Slide 7
Preoxidation stage

## Slide 8
Heating stage
Ar
Ar+ steam
Ar

## Slide 9
Quench stage
Ar
Ar+ steam
Ar

## Slide 11
0 50 100 150
Temperature gradient along the sample

## Slide 12
Water injection
Steam
Unirradiated sample test diagram
Pre-oxidation position
Full immersion
Water level touch

## Slide 13
New test regime

## Slide 15
Quench bundle test

## Slide 16: FA Quench Model Development of models and codes to describe VVER core behavior under SA conditions
Development of the requirements to models and codes
The requirements to the SVECHA code models (mainly concerning the material properties) were elaborated in order to be able to describe VVER reactor behavior under severe accident conditions.
Preparation and adaptation of models and codes
The preliminary stage of the adaptation of the models of high temperature oxidation and mechanical behavior of VVER cladding tubes was performed with respect to:
Comparison of the results obtained during examination of "fresh" and spent claddings;
Development of physical model of time-dependent high temperature cladding oxidation based on the PWR Zry-4 cladding oxidation model developed in IBRAE;
Further development of cladding mechanical behaviour model developed in IBRAE for PWR Zry-4 claddings and application of modified model to describe examined VVER fuel rods.
8th CEG-SAM Meeting Podolsk September 14-16, 2005

## Slide 17: Cladding Oxidation Model Adaptation to VVER Materials (1)
Simulation of the -Zr and ZrO2 layers growth kinetics in the RIAR isothermal tests on Zr-1%Nb cladding oxidation in steam at 1000 and 1100oC
8th CEG-SAM Meeting Podolsk September 14-16, 2005

## Slide 18: Cladding Oxidation Model Adaptation to VVER Materials (2)
Simulation of the -Zr and ZrO2 layers growth and weight gain kinetics in the RIAR isothermal tests on Zr-1%Nb cladding oxidation in steam at 1200oC
8th CEG-SAM Meeting Podolsk September 14-16, 2005

## Slide 19: Cladding Oxidation Model Adaptation to VVER Materials (3)
Calculated oxygen diffusion coefficients in -Zr and ZrO2 phases of Zr-1%Nb and Zry cladding materials
8th CEG-SAM Meeting Podolsk September 14-16, 2005

## Slide 20: Cladding Deformation Model Adaptation to VVER Materials
RIAR Tests on Zr-1%Nb Cladding Ballooning
8th CEG-SAM Meeting Podolsk September 14-16, 2005