## Slide 1
PARAMETER SF3 pre-test calculation with ATHLET-CD H. Austregesilo, Ch. Bals
presented by W. Erdmann
Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany

## Slide 2: Content
Improvement of PARAMETER SF2 post-test calculation as a reference for SF3 pre-test calculation
Specification of the PARAMETER SF3 experiment and simulation with ATHLET-CD
Model parameters of ATHLET-CD
Results of PARAMETER SF3 pre-test calculation:
  Temperatures
  Quench fronts
  Hydrogen generation
  Oxide layer thickness

## Slide 3: Improved input model for PARAMETER calculations with ATHLET-CD
Modelling as previous:
Flow Channels
  Central Bundle 85.7 %
  Outer Bypass 14.3 %
  Cooling Jacket
Structures
  Rods: ROD1 (1) ROD2 (6) ROD3 (12)
  Grids (6)
  Shroud / Insulation
  Cooling Jacket Walls
Improved Modelling:
  Additional volumes below inlet pipes
  Form of OUTPIPE corresponds to steam flow in test
  Hydraulic diameter in bundle region: 3.8·10-3 m
  Separate pipes for Ar and steam inlet pipes

## Slide 4: Improvement of SF2 post-test calculation as a validation basis for SF3 pre-test calculation (1)
Good agreement of calculated temperatures and hydrogen generation already in previous calculation (13th Meeting of CEG-SAM, Budapest, 3-6 March 2008)
Conclusion from previous calculation: Leistikow / Prater-Courtright correlation leads to better results with respect to H2-generation

## Slide 5: Improvement of SF2 post-test calculation as a validation basis for SF3 pre-test calculation (2)
Time and height of final quench now in very good agreement with test data: 16620 s / 1250 mm
Due to the adopted hydraulic diameter in the bundle region and to additional volumes to simulate the lower part of the test section the water discharge during quench could be improved: - entrained liquid at 16620 s: 4.3 kg - totally evaporated liquid: 2.3 kg now agrees well with discharged and condensed liquid in test of 6.5 kg (collected in tank 5)
entrainment until end of quench
collected mass in tank 5

## Slide 6: Specification of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD (1)
Power supply – temperature behaviour: - cold bundle at start of test: 20 °C at 0 s
- heating up to 400 - 500 °C with 1.6 to 2.0 kW within 3500 s - stepwise increase of power to heat up with heating rate of 0.25 K/s, then 0.1 K/s to 1200 °C (at t ~ 7500 s) - pre-oxidation phase: keep constant temperature at T≈1200 °C until 11500 s - increase of power to heat up with heating rate of 0.4 K/s until a max. temperature of Tmax=1600 °C is reached (t~12500 s) - power is turned off when Tmax is reached (at the same time quenching is initiated)

## Slide 7: Specification of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD (2)
Argon inlet flow rate: - 0.2 g/s until 500 s - 2.0 g/s until end of test (t~13000 s)
Steam inlet flow rate: - 0.0 g/s until 1500 s - 3.5 g/s until quenching is initiated and power is turned off
Inlet gas temperatures: - Argon: 450 °C - Steam: 500 °C

## Slide 8: Specification of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD (3)
Top flooding is initiated as soon as Tmax=1600 °C is reached (together with power shut off)
Water flow rate: 40 g/s comparison with SF2: - top flooding: 41 g/s - bottom flooding: 130 g/s
Water temperature: 25 °C
Injection is finished 500 s after initiation
Bundle pressure: - 1 bar until 500 s - increase to 3 bar at 500 s - constant boundary condition of 3 bar until end of calculation (no realistic simulation of condenser in ATHLET-CD calc.)

## Slide 9: Specification of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD (4)
if max. temperature of 1600 °C is reached: → signal ‘quench initiation’ is set, linear increase to full rate of 40 g/s within Δt=10 s
→ electric power is shut off within 1 s after ‘quench initiation’ signal → steam supply is turned off within 5 s starting directly after ‘quench initiation’ signal (reference calc.)

## Slide 10: Model parameters of ATHLET-CD for post-test calculation of SF2 and pre-test calculation of SF3 (1)
Cladding oxidation model: Leistikow / Prater-Courtright correlation was used (IOXMOD = 19) instead of recommended Sokolov correlation (WWER: Zr1%Nb) (IOXMOD = 18)
Default values for interfacial friction parameters are used
1600°C
1200°C

## Slide 11: Model parameters of ATHLET-CD for post-test calculation of SF2 and pre-test calculation of SF3 (2)
Electrical resistance of electrodes defined corresponding to given temperature dependency of Mo, Ta; Brass not considered in calculations (below / above simulated core region)
External resistance 1 mΩ/rod
Hydraulic diameter in core region: DH=3.8·10-3 m (=DH at grid positions)

## Slide 12: Results of PARAMETER SF3 pre-test calculation
Temperatures (0 – 14000 s):
- general temperature development agrees well with previously shown results of pre-test calculations
- given power results in: stabilization phase at ~ 400 °C (1500 – 3500 s), pre-oxidation phase at ~ 1100 - 1150 °C (7500 – 11500 s), max. temperature of 1600 °C is reached at t=12567 s
- maximum temperature is calculated at 1250 mm elevation

## Slide 13: Results of PARAMETER SF3 pre-test calculation
Temperatures (quenching period):
- maximum temperature of 1600 °C is reached at t=12567 s at bundle elevation 1250 mm
- after start of top flooding temperature is calculated to decrease in all bundle elevations
- different to SF2: due to cooling only from the top pre-cooling at upper elevations is higher compared to lower elevations

## Slide 14: Results of PARAMETER SF3 pre-test calculation
Quench fronts:
- quenching of bundle within time period of 253 s after start of top flooding (at 12567 s); injected liquid until end of quenching: 10.1 kg (for comparison SF2: quenching within 112 s, injected liquid until end of quenching: 16.7 kg)
- point of intersection of lower and upper quench front at 900 mm bundle elevation – not at position of maximum bundle temperature (1250 mm) due to lower pre-cooling at lower bundle region

## Slide 15: Results of PARAMETER SF3 pre-test calculation
Hydrogen generation:
- Total mass of hydrogen generated: 26.1 g, (18.7 g in bundle region) calculated with Leistikow / Prater-Courtright correlation as for SF2

## Slide 16: Results of PARAMETER SF3 pre-test calculation
Oxide layer thickness:
- oxide layer during pre-oxidation phase has a maximum value of ~ 200 µm (as intended)
- a max. layer thickness of 427 µm is reached at the end of the calculation (1250 mm elevation)

## Slide 17: Conclusions
ATHLET-CD calculates temperature development as expected with the given boundary conditions
Time needed for quenching: 253 s (SF2: 112 s)
Total hydrogen generation is 26.1 g (Leistikow / Prater-Courtright correlation was used as for SF2 post-test calculation)
Max. thickness of oxide layer is 427 µm at the end of the calculation
Time variation to turn off the steam injection within the range from 0 to 10 s has no visible influence on the results due to the quick cooling in all elevations