## Slide 1
PARAMETER SF3 post-test calculation with ATHLET-CD Ch. Bals, H. Austregesilo
presented by W. Erdmann
Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany

## Slide 2: Content
Conditions of the PARAMETER SF3 experiment and simulation with ATHLET-CD
Input model and model parameters for post-test calculation
Results of PARAMETER SF3 post-test calculation:
  Temperatures
  Quench front
  Hydrogen generation
  Oxide layer thickness
Conclusions

## Slide 3: Conditions of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD
Power supply: - preparation phase (0 – 4506 s): heating up to ~500 °C with ~2.0 kW - heat up phase (4506 s – 9760 s): stepwise increase of power to ~8 kW to heat up bundle to ~1200 °C - pre-oxidation phase (9760 s – 13725 s): regulation of power to keep constant temperature at T≈ 1200 °C (power increase to 9.1 kW, Tmax= 1260 °C) - transient phase (13725 s – 14481 s): increase of power to ~13 kW to heat up the bundle to a max. temperature of Tmax= 1600 °C - flooding phase (14486 s – 14960 s): power is turned off when Tmax is reached; at the same time quenching is initiated

## Slide 4: Conditions of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD
Argon inlet flow rate: - start of argon supply corresponding to test data at ~500 s - mass flow 2.0 g/s, T ~400 °C - switch from bottom to top injection at 14550 s, mass flow 2.0 g/s, until end of test (t= 15064 s)
Steam inlet flow rate: - start of steam supply at ~2300 s - mass flow 3.5 g/s, T ~500°C until 14470 s (before quenching is initiated and power is turned off)

## Slide 5: Conditions of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD
Initial liquid level in lower part of test section assumed for calculation: 450 mm below steam / argon inlet, as shown in /1/, Fig. 5
Top flooding is initiated as soon as Tmax= 1600 °C is reached (together with power shut off) - experiment: t= 14486 s - calculation: t= 14526 s (40 s later)
Average water flow rate: 40 g/s
Water temperature: 25 °C
Injection is finished 474 s after initiation - experiment: t= 14960 s (T< 130 °C) - calculation: t= 15000 s (same mass of liquid injected as in exp.)
/1/ Protocol of PARAMETER-SF3 Results, 2008

## Slide 6: Conditions of the PARAMETER SF3 Experiment and Simulation with ATHLET-CD
Bundle pressure: - 1 bar until 500 s - increase to 3.5 bar until 1000 s - constant boundary condition of 3.5 bar at outlet (PHCOROUT) until end of calculation (no realistic simulation of condenser in ATHLET-CD calc.)
Cooling Jacket water flow rate: 52 g/s

## Slide 7: Input model for PARAMETER calculations with ATHLET-CD
Flow Channels:
  Central Bundle CORE2 85.7 %
  Outer Bypass CORE3 14.3 %
  Cross connection
  Cooling Jacket
Structures:
  Rods (in CORE2): ROD1 (1 unheated rod) ROD2 (6 heated rods) ROD3 (12 heated rods)
  Grids (6)
  Shroud / Insulation
  Cooling Jacket Wall
  Structures at top of bundle (upper plate, separation sheet)
  Additional features
  Form of OUTPIPE corresponds to steam flow in test
  Hydraulic diameter in bundle region: 3.8·10-3 m

## Slide 8: Model parameters of ATHLET-CD for post-test calculation of SF3
Electrical resistance of electrodes defined corresponding to given temperature dependency of Mo, Ta; Brass not considered in calculations (below / above simulated core region)
External resistance 1 mΩ/rod, increased to 6 mΩ/rod (t > 13700 s) to get the correct thermal behavior during the transient phase
Hydraulic diameter in core region: DH= 3.8·10-3 m (= DH at grid positions) as in previous calculations

## Slide 9: Model parameters of ATHLET-CD for post-test calculation of SF3
Cladding oxidation model: Cathcart / Prater-Courtright (IOXMOD= 15) correlation was used instead of Leistikow / Prater-Courtright (IOXMOD= 19) correlation (used for post-test correlation of SF2 and pre-test calculations of SF3, SF4) and instead of recommended Sokolov correlation (IOXMOD = 18) (WWER: Zr1%Nb) to get H2 mass in better agreement with test data
All other options and parameters are the same as used for previous post-test calculation of SF2 and pre-test calculations of SF3, SF4 (e. g. standard values for interfacial friction model, quench model)
1600°C
1200°C

## Slide 10: Results of PARAMETER SF3 post-test calculation
Cladding Temperatures (0 – 15000 s) in upper bundle region (1000-1500 mm):
- good agreement of general temperature development besides underestimation at topmost position (1500 mm)
- maximum temperature: in experiment reached at 1300 mm pos. (1578 °C, t= 14486 s) in calculation reached at 1250 mm pos. (1600 °C, t= 14526 s)
- high scattering of measured temperatures, e.g. at 1250 mm / 1400 mm height (influence of damaged heaters?); low difference in calculation between temperatures of inner ring (ROD2) and outer ring (ROD3)

## Slide 11: Results of PARAMETER SF3 post-test calculation
Cladding Temperatures (0 – 15000 s) in lower bundle region (0-800 mm):
- temperatures during pre-oxidation phase are generally slightly overestimated
- during transient phase time dependency of temperatures is kept very well

## Slide 12: Results of PARAMETER SF3 post-test calculation
Shroud- and Thermoinsulation Temperatures (0 – 15000 s):
- temperatures are generally overestimated besides insulation temperature at height of 1100 mm
- decrease of shroud temperature after 10000 s (e.g. at 1100 mm elevation) probably due to damage of adjacent heaters, cannot be simulated

## Slide 13: Results of PARAMETER SF3 post-test calculation
Cladding Temperatures during quench phase in upper bundle region (1000-1500 mm):
- start of top cooling 40 s delayed compared to experiment: experiment: t= 14486 s (Tmax= 1578 °C) calculation: t= 14526 s (Tmax= 1600 °C)
- cooling of maximum temperature (1250 mm position for calculation) within the scattering region of measured data

## Slide 14: Results of PARAMETER SF3 post-test calculation
Cladding Temperatures during quench phase in lower bundle region (0-800 mm):
- quenching time of elevations 500 - 800 mm still in agreement with measured data, but in experiment: cooling from upper to lower positions, in calculation: cooling from lower to upper positions
- cooling at bottom of bundle too early compared to measured temperatures

## Slide 15: Results of PARAMETER SF3 post-test calculation
Quench fronts:
- quenching of bundle within time period of 304 s after start of top flooding (at 14526 s);
- good agreement of upper quench front; due to higher velocity of cooling from the bottom compared to test data final quench is calculated ~100 s earlier (use of standard data for quench front model, exp. data from /2/)
- injected liquid until end of quenching: 12.2 kg injected liquid until end of injection: 19.0 kg
/2/ V. Nalivaev, Status of the ISTC project #3690 on the “Fuel assemblies behaviour under severe accident conditions in the PARAMETER-SF test series”, CEG-SAM-15, Villingen, Switzerland, March 10 - 12, 2009

## Slide 16: Results of PARAMETER SF3 post-test calculation
Hydrogen generation:
- very good agreement of time dependency besides a short period at the beginning of pre-oxidation phase - very good agreement of total amount of hydrogen generation
- total mass of hydrogen generated: calculation: 24.4 g from bundle 9.5 g from shroud, grids
33.9 g total amount
experiment: 34.5 g

## Slide 17: Results of PARAMETER SF3 post-test calculation
Oxide layer thickness:
- oxide layer at the end of pre-oxidation phase (13725 s) has a maximum value of ~400 µm (intended: 200 µm)
- a max. layer thickness of ~450 µm is reached in the simulation
- the maximum oxide layer is calculated in the bundle height of 1250 mm where the maximum temperature is reached
no comparison with data available up to now

## Slide 18: Conclusions
Overall thermal behavior is calculated in good agreement with measured temperatures; temperatures during pre-oxidation phase are generally slightly too high; the temperature increase during the transient phase is calculated correctly
Cooling from the top is simulated very well (with standard data for quench model); due to too early cooling also from the bottom quenching is finished after 304 s instead of ~400 s; quenching of maximum temperatures is calculated within the scattering of data
Total hydrogen generation is 33.9 g compared to 34.5 g in the experiment (98 %); the oxidation behavior of the Zr1%Nb claddings can be simulated in good agreement with data with the available oxidation correlations
Max. thickness of oxide layer is higher than intended at the end of the pre-oxidation period; at the end of the calculation a maximum value of 450 µm is reached at 1250 mm bundle height (data from experiment are not available up to now for comparison)
It seems that a lower loss of liquid compared to the test (shroud failure not simulated) results in a higher accumulation of liquid at the bottom of the bundle; this causes an overestimated cooling from the bottom and therefore a too early total quenching of the bundle
It is intended to run further calculations with a better simulation of the liquid mass distribution (liquid loss through shroud, interfacial friction) to get the correct behavior of the lower quench front