## Slide 1: PARAMETER-SF4 pre-test calculation with MAAP4.07
Emilie BEUZET, Jean-Sylvestre LAMY

## Slide 2: Content
PARAMETER-SF4 test section
Specification of PARAMETER-SF4 test
Model parameters used in MAAP4.07
Results of SF4 pre-test obtained with MAAP4.07
 Temperatures
 O2 flow rates
 Oxide layer thickness
Conclusion

## Slide 3: PARAMETER-SF4 test section
PARAMETER cross section PARAMETER test facility

## Slide 4: Specification of PARAMETER-SF4 test
Pre-test calculation for PARAMETER SF4 has been carried out with a local version of MAAP4.07, containing extensions developed by EDF, specifically :
- Zr oxidation by air, - introduction of material properties of the heater element materials (tantalum, molybdenum and brass) used in PARAMETER.
The simulation covers :
- the initial power ramp and heat up, - establishment of a stable pre-oxidation plateau, - power reduction, - air ingress phase, - bottom reflood.

## Slide 5
Specification of PARAMETER-SF4 test
Argon 2g/s
Air 0.5g/s
Steam 3.5g/s
1500 s
16000 s
16875 s
~873 k
~1473 k
~1873 k
~300 µm
Bottom reflood 80g/s

## Slide 6: Model parameters used in MAAP4.07
58 meshes
3 rows
Steam pre-oxidation = Cathcart + Urbanic correlation
Air oxidation = NUREG correlation
External resistance : 8.5mΩ / rod
Distribution in : - 3 rows : 1 unheated rod / 6 rods / 12 rods + 12 ‘little’ rods , - 58 axial meshes : 5 for the lower plenum, 48 for the core and 5 for the upper plenum.

## Slide 7: Results of SF4 pre-test obtained with MAAP4.07
Temperatures all simulation long :

## Slide 8: Results of SF4 pre-test obtained with MAAP4.07
Temperatures during air ingress :

## Slide 9: Results of SF4 pre-test obtained with MAAP4.07
O2 flow rates :

## Slide 10: Results of SF4 pre-test obtained with MAAP4.07
Oxide layer thickness :

## Slide 11: Conclusion
Confidence in our simulation  until start of air ingress phase :
- good agreement in steam oxidation between MAAP modelling and QUENCH experiments,
- during air ingress, in case of O2 starvation : nitriding phenomenon = not taken into account  may attenuate the temperature escalation at the hot spot.
EDF is very interested in getting experimental data from SF4 :
- to improve the understanding of air oxidation phenomenon,
- to know how well our model reproduces the experiment,
- to indicate areas of weakness of our model and to improve it.

## Slide 12
Thanks for your attention …