## Slide 1
PARAMETER-SF4 post-test calculation with MAAP4.07
Andreas SCHUMM, Emilie BEUZET
March 2011
September 2010

## Slide 2
Sommaire
1. PARAMETER-SF4 test section
2. Specification of PARAMETER-SF4 test
3. Model parameters used in MAAP
4. Comparison with the previous post-calculations
5. Results of PARAMETER-SF4 post-test calculation
 Temperatures at different elevations (pre-ox)
 Hydrogen production
 Temperatures at different elevations (air)
 O2 flow rates
6. Conclusions

## Slide 3: PARAMETER-SF4 test section
PARAMETER cross section
PARAMETER test facility

## Slide 4: Specification of PARAMETER-SF4 test (1/2)
Pre-test and post-test calculations for PARAMETER SF4 have been carried out with a local version of MAAP4.07, containing extensions developed by EDF, specifically :
- Zr oxidation by air,
- introduction of material properties of the heater element materials (tantalum and molybdenum) used in PARAMETER.
Pre-test calculations in collaboration lead to the establishment of the PARAMETER SF4 sequence.
The simulation covers :
- establishment of a stable pre-oxidation plateau,
- power reduction,
- air ingress phase,
- bottom reflood.
t0MAAP=tSF4-1452 (the simulation begins with steam injection)

## Slide 5: Specification of PARAMETER-SF4 test (2/2)
Argon 2g/s
Air 0.5g/s
Steam 3.5g/s
~770 K
~1470 K
~2020 K
Bottom reflood 80g/s
1452 s
16000 s
~1170 K

## Slide 6: Model parameters used in MAAP (1/2)
Steam pre-oxidation = Cathcart + Urbanic correlation
Air oxidation = NUREG correlation
External resistance : 8.5mΩ / rod (established on the other PARAMETER experiments)

## Slide 7: Model parameters used in MAAP (2/2)
First calculation (CEG-SAM of March 2010)
- 3 rows : 1 unheated rod / 6 rods / 12 rods + 12 peripheral rods
- 58 axial meshes : 5 for the lower plenum, 48 for the core and 5 for the upper plenum.
Second calculation (CEG-SAM of September 2010)
- 4 rows : 1 unheated rod / 6 rods / 12 rods / 12 peripheral rods,
(peripheral rods represented seperately)
- 58 axial meshes
‘New’ calculation
- 4 rows : 1 unheated rod / 6 rods / 12 rods / 12 peripheral rods added in all the geometrical characteristics (lower and upper plenums, rods number …),
-> full length rods extend through plenums
- 58 axial meshes

## Slide 8: Comparison with the previous post-calculations (at 200 mm )
simu1 = 3 rows simu2 = 4 rows
new = 4 rows + peripheral rods completly included in the geometry

## Slide 9: Comparison with the previous post-calculations (at 900 mm)

## Slide 10: Comparison with the previous post-calculations (at 1300 mm)

## Slide 11: Comparison with the previous post-calculations (shroud 500, 700 and 1100mm – bottom bundle improved)

## Slide 12: Cladding temperatures at 500 mm high (pre-ox)

## Slide 13: Cladding temperatures at 1250 mm high (pre-ox)
Tcl2 and tcl3 almost identical in simulation

## Slide 14: Hydrogen production
rather good prediction of the hydrogen production during pre-oxidation phase
( 21.8g for the experiment and 19.7g for the simulation)

## Slide 15: Cladding temperatures at 500 mm high (air)
Rapid drop after reflow in simulation

## Slide 16: Cladding temperatures at 800 mm high (air)

## Slide 17: Cladding temperatures at 1100 mm high (air)

## Slide 18: Cladding temperatures at 1250 mm high (air)

## Slide 19: O2 flow rates during air ingress
Modelling predicts O2 starvation during air ingress at 17160 s (15710 s in MAAP time) and about 17100 s for the experiment.

## Slide 20: Conclusions
Thermal behaviour :
- new modelling = better (for the overall bundle), slightly worse at 200mm
- good prediction during the steam phase
- good prediction during the air phase -- analysis is difficult for the upper part of the bundle due to thermocouples failure
- shroud : better behaviour in the lower part of the bundle
- flooding = T decrease too fast with the calculation
Hydrogen production :
- good prediction during pre-oxidation phase
- hydrogen production during the reflood not captured (< 1g) – Tantal oxydation and instant fill-up of lower plenum?
Modelling now predicts O2 starvation with a quite good agreement against the experiment, as opposed to the initial simulation
Nitrate formation not simulated (no correlation available)