## Slide 1
PARAMETER SF4 pre-test calculation with ATHLET-CD Ch. Bals, K. Trambauer
Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany

## Slide 2: Content
PARAMETER test facility
Rerun of PARAMETER SF2 post-test calculation as a reference for SF4 pre-test calculation (new ATHLET-CD version 2.2a)
Specification of the PARAMETER SF4 experiment and simulation with ATHLET-CD
Model parameters of ATHLET-CD
Results of PARAMETER SF4 pre-test calculation:
  Temperatures
  Quench fronts
  Hydrogen generation
  Oxide layer thickness
Conclusion

## Slide 3: PARAMETER test facility
General View
Layout

## Slide 4: Input model for PARAMETER calculations with ATHLET-CD
Flow Channels
  Central Bundle 85.7 %
  Outer Bypass 14.3 %
  Cooling Jacket
  Separate pipes for Ar and steam inlet pipes
Structures
  Rods: ROD1 ( 1) ROD2 ( 6) ROD3 (12)
  Grids (6)
  Shroud / Insulation
  Cooling Jacket Walls
Changes compared to previous calculations:
  Ar fill at top to switch Ar injection from bottom to top after start of reflood
  Additional structures at top of bundle (upper plate, separation sheet)

## Slide 5: Rerun of SF2 post-test calculation as a validation basis for SF4 pre-test calculation (1)
Repetition of SF2 post-test calculation
due to the use of the new ATHLET version 2.2a for calculation of SF4
Small changes in modelling have to be verified:
  additional structures at top of bundle
  switch of Argon injection to top of bundle after start of flooding
  heat transfer between shroud / insulation and jacket tube calculated by the code (previously a constant value was used)
Small differences in results compared to previous calculation (maximum temperatures slightly reduced, integral hydrogen production slightly lower)

## Slide 6: Rerun of SF2 post-test calculation as a validation basis for SF4 pre-test calculation (2)
Time of final quench 8s delayed compared to experiment (16628 s); height of last quench in agreement with test data at 1250 mm;
The water discharge during quench is determined as previously - entrained liquid at 16628 s: 4.3 kg - totally evaporated liquid: 2.3 kg and agrees well with discharged and condensed liquid in test of 6.5 kg (collected in tank 5)
collected mass in tank 5

## Slide 7: PARAMETER SF4 Specification and Simulation with ATHLET-CD (1)
Specification according to Jon Birchley, (e-mail, 11.11.2008)
Power supply – temperature behavior: - cold bundle at start of test: 25 °C at 0 s
- power initially based on SF3 specification; adjusted to achieve max. plateau temperature of ~1200 °C with given time function - at 12000 s (oxide scale thickness of 300 µm is assumed to be reached) power reduction to 5.5 kW to reduce Tmax to ~ 900 °C before air injection is started at t=14000s - constant power of 5.5 kW during air injection phase is switched off when max. temperature of 1750 °C is reached; at same time bottom injection of water is started

## Slide 8: PARAMETER SF4 Specification and Simulation with ATHLET-CD (2)
Argon inlet flow : - constant rate of 2.0 g/s - until start of reflood from bottom, - then switch to upper injection - T= 450°C
Steam inlet flow: - 0.0 g/s until 1500 s - 3.5 g/s until 14000s, when air injection is started, - T=500°C
Air inlet flow: - 0.8 g/s (0.16 g/s O2, 0.64 g/s N2) - air injection starts at 14000s - air injection is switched off when bottom water injection is started

## Slide 9: PARAMETER SF4 Specification and Simulation with ATHLET-CD (3)
Bottom flooding is initiated as soon as Tmax=1750 °C is reached (together with power shut off)
Water flow rate: 80 g/s (base case) comparison with SF2: - top flooding: 41 g/s - bottom flooding: 130 g/s
Variation (second case): water flow rate: 40 g/s
Water temperature: 25 °C
Injection is finished when Tmax < 200°C
Bundle pressure: 3 bar - constant boundary condition of 3 bar until end of calculation (no realistic simulation of condenser in ATHLET-CD calc.)

## Slide 10: Model parameters of ATHLET-CD for post-test calculation of SF2 and pre-test calculation of SF4 (1)
Cladding oxidation model: Leistikow / Prater-Courtright correlation was used (IOXMOD = 19) instead of recommended Sokolov correlation (WWER: Zr1%Nb) (IOXMOD = 18)
Default values for interfacial friction parameters are used
1600°C
1200°C

## Slide 11: Model parameters of ATHLET-CD for post-test calculation of SF2 and pre-test calculation of SF4 (2)
Electrical resistance of electrodes defined corresponding to given temperature dependency of Mo, Ta; Brass not considered in calculations (below / above simulated core region)
External resistance 1 mΩ/rod
Hydraulic diameter in core region: DH=3.8·10-3 m (=DH at grid positions)

## Slide 12: Results of PARAMETER SF4 pre-test calculation
Temperatures in pre-oxidation period (before air oxidation):
- maximum temperature is calculated at 1250 mm elevation
- given time function for power leads to a maximum plateau temperature of Tmax = 1281 °C (expected Tmax ~ 1200 °C);
- Temperature decrease between 12000 s and 14000 s to ~ 900 °C is achieved as desired

## Slide 13: Results of PARAMETER SF4 pre-test calculation
Temperatures (air ingress period):
- after a time period of ~ 600 s following the start of air injection (t=14000s) oxygen starvation can be observed at the elevations above ~ 1000 mm
- due to oxygen starvation in the upper bundle region the higher air oxidation and therefore the stronger tempe- rature excursion moves to lower elevations;
- maximum temperature of 1750 °C is reached at t=14666 s at bundle elevation 700 mm

## Slide 14: Results of PARAMETER SF4 pre-test calculation
Temperatures (quenching period):
- bottom flooding is initiated at 14666s when Tmax = 1750 °C is reached
- after start of flooding only small temperature increase of ~ 100°C is calculated for both flooding rates (80 g/s and 40 g/s) when liquid enters the heated bundle (steam oxidation)
- due to cooling only from the bottom last quench is calculated at the upper bundle elevations

## Slide 15: Results of PARAMETER SF4 pre-test calculation
Quench fronts:
- quenching of bundle within time period of 212 s after start of bottom flooding for base case (80 g/s), injected liquid until end of quenching: 17.0 kg
- second case (40 g/s) : 367 s needed for quenching of the bundle; injected liquid 14,7 kg (for comparison SF2: top / bottom quenching within 112 s, injected liquid until end of quenching: 16.7 kg)
- last quench at ~ 1500 mm bundle elevation (nearly no progress of upper quench front)

## Slide 16: Results of PARAMETER SF4 pre-test calculation
Hydrogen generation:
- Total mass of hydrogen generated: 29.4 g, (20.2 g in bundle region) calculated with Leistikow / Prater-Courtright correlation as for SF2
- Hydrogen generated during quench: 2.96 g at 80 g/s, 2.81 g at 40 g/s.

## Slide 17: Results of PARAMETER SF4 pre-test calculation
Oxide layer thickness:
- oxide layer at the end of the pre-oxidation phase has a maximum value of ~ 450 µm (intended oxide scale thickness is ~ 300 µm)
- max. increase of oxide scale during air oxidation phase ~ 110 µm at 800 mm elevation
- a max. layer thickness of 465 µm is reached at the end of the calculation (1250 mm elevation)

## Slide 18: Conclusions
ATHLET-CD calculates slightly higher maximal temperatures within the pre-oxidation phase than expected with the given time function for power (calculated: ~1280°C, expected: 1200°C); the temperature decrease to 900°C within 2000 s before the start of air injection is in agreement with the desired value; the maximal temperature within the air ingress phase of 1750°C as the start point for bottom water injection is reached earlier than expected (calculated: 14666 s, expected: 15060 s)
Air injection with a rate of 0.8 g/s leads to a oxygen starvation at the positions above 1000 mm after a time period of ~ 600 s (at ~14600s, start of air injection at 14000s); therefore the elevation of the maximum temperature moves to lower positions;
Time needed for bottom quenching: 212 s for calculation with injection rate 80 g/s, 367 s for case with 40 g/s injection rate
Total hydrogen generation is 29.4 g, about 3 g during quench (Leistikow / Prater-Courtright correlation was used as for SF2 post-test calculation)
Oxide layer thickness at the end of the pre-oxidation phase is calculated higher than expected with the given power curve (450 µm instead of 300 µm); oxide layer at the end of the calculation is 465 µm