## Slide 1: Miscibility gap in the UO2-FeO-SiO2 system
ISTC PRECOS
Project #3813
A.P. Alexandrov
Research Institute of Technology
Presented by Svetlana Kirillova
5th PRECOS Meeting
ETU
Saint-Petersburg

## Slide 2
2
  Miscibility gap boundaries determination
Research objectives
Experimental technique
  Galakhov microfurnace (melting, annealing, quenching)
UO2 of >99.0 % purity, SiO2 of 99.99% purity, FeO of >99.0 % purity,
charge mass – 150 mg
molybdenum crucibles  6 mm

## Slide 3
3
First experimental series (GPRS 33-35)
UO2
SiO2
FeO
CORPHAD
CORPHAD+PRECOS
Fe2SiO4
Tm=1700 C
Tm=2080 C
Test | Content, mol.% |  |  | T, C | Exp. time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS33 | 5.0 | 70.0 | 25.0 | 1100 | 60 | Annealing
 |  |  |  | 2100 | 5 | Melting and quenching
GPRS34 | 10.0 | 80.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 5 | Melting and quenching
GPRS35 | 20.0 | 73.0 | 7.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 5 | Melting and quenching
35
34
33

## Slide 4
4
First experimental series (GPRS 33 results)
0
0.2
0.4
FeO
1
0.8
SiO2
33
Tm=2080 C
Tm=1700 C
2100
10 m
MG not detected (Above the MG)

## Slide 5
5
First experimental series (GPRS 34 results)
0.2
FeO
0.8
SiO2
34
Tm=2080 C
Tm=1700 C
1850
5 m
250 m
Tm < 1850 - ?
T, C | Type | UO2 | FeO | SiO2
1850 | Heavy liquid | 11.81.2 | 20.91.9 | 67.31.7
 | Light liquid | 4.00.3 | 6.61.3 | 89.41.6
Tm | Heavy liquid | 12.21.5 | 23.43.6 | 64.44.4
 | Light liquid | 1.70.1 | 2.80.3 | 95.50.4
<Tm | Area 1 | 21.30.7 | 10.00.3 | 68.80.4
300 m
MG detected
(macro and micro segregation)
Area 1

## Slide 6
6
First experimental series (GPRS 35 results)
0.2
FeO
0.8
SiO2
35
Tm=2080 C
Tm=1700 C
30 m
250 m
T, C | Type | UO2 | FeO | SiO2
<Tm | Heavy liquid | 20.18.6 | 15.01.8 | 64.96.8
 | Light liquid | 3.30.5 | 3.30.5 | 93.51.0
1950 | Homogeneous | 12.20.5 | 7.20.6 | 80.50.6
<1950 | Unhomogeneous | 8.71.3 | 7.30.9 | 84.11.9
MG detected
(micro segregation only)
< Tm - ?
1950

## Slide 7
7
Second experimental series (GPRS 59-64)
Test | Content, mol.% |  |  | T, C | Exp. time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS59 | 18.0 | 77.0 | 5.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS60 | 18.0 | 77.0 | 5.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
GPRS61 | 12.0 | 78.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS62 | 12.0 | 78.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
GPRS63 | 6.0 | 79.0 | 15.0 | 1100 | 60 | Annealing
 |  |  |  | 1750 | 10 | Melting and quenching
GPRS64 | 6.0 | 79.0 | 15.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 10 | Melting and quenching
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
59-60
61-62
63-64
Research objectives: Tm determination, exposure answers solving, tie lines near Tm determination

## Slide 8
8
Second experimental series (GPRS 59-64)
70 m
59
Peculiarities: 10 min. exposure, quenching
T= 1750С
T= 1850С
60
200 m
61
150 m
62
200 m
63
200 m
64
700 m

## Slide 9
9
Second experimental series (GPRS 59-61 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
Tm > 1850
1850 > Tm > 1750
MG not detected
for GPRS 59-61
70 m

## Slide 10
10
Second experimental series (GPRS 62 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
1850 > Tm > 1750
1850
MG detected for GPRS 62
(micro segregation only)
T, C | Type | UO2 | FeO | SiO2
1850 | Heavy liquid | 19.22.6 | 22.111.7 | 58.713.3
 | Light liquid | 2.50.7 | 5.31.2 | 92.21.8
200 m
20 m

## Slide 11
11
Second experimental series (GPRS 63 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
1750 > Tm
MG detected for GPRS 63
(micro segregation only)
700 m
T, C | Type | UO2 | FeO | SiO2
1750 | Heavy liquid | 11.92.4 | 34.73.4 | 53.44.2
 | Light liquid | 1.80.5 | 6.61.4 | 91.61.9
30 m

## Slide 12
12
Second experimental series (GPRS 64 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
1850
MG detected for GPRS 64
(micro segregation)
700 m
T, C | Type | UO2 | FeO | SiO2
1850 | Heavy liquid | 13.01.2 | 26.74.2 | 60.34.8
 | Light liquid | 2.90.5 | 7.21.1 | 90.01.4
1750
40 m

## Slide 13
13
Third experimental series (GPRS 67-72)
Test | Content, mol.% |  |  | T, C | Exp. time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS67 | 18.0 | 77.0 | 5.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 10 | Melting and quenching
GPRS68 | 18.0 | 77.0 | 5.0 | 1100 | 60 | Annealing
 |  |  |  | 2050 | 10 | Melting and quenching
GPRS69 | 12.0 | 78.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1900 | 10 | Melting and quenching
GPRS70 | 12.0 | 78.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 10 | Melting and quenching
GPRS71 | 6.0 | 79.0 | 15.0 | 1100 | 60 | Annealing
 |  |  |  | 1700 | 10 | Melting and quenching
GPRS72 | 6.0 | 79.0 | 15.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 10 | Melting and quenching
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
67-68
69-70
71-72
Research objectives: Tm determination, tie lines determination

## Slide 14
14
Third experimental series (GPRS 67-72)
300 m
67
Peculiarities: 10 min. exposure, quenching
T= 1950С
T= 2050С
68
300 m
69
900 m
70
300 m
71
300 m
72
900 m
T= 1900С
T= 1950С
T= 1700С
T= 1950С

## Slide 15
15
Third experimental series (GPRS 67 and 71 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
1850 > Tm > 1750
MG not detected
for GPRS 67 and 71
300 m
2050 > Tm > 1950
1750 > Tm > 1700

## Slide 16
16
Third experimental series (GPRS 68 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
2050
MG detected for GPRS 68
(micro segregation only)
700 m
T, C | Type | UO2 | FeO | SiO2
2050 | Heavy liquid | 26.010.8 | 12.28.9 | 61.811.9
 | Light liquid | 6.30.7 | 3.20.4 | 90.51.0
7 m

## Slide 17
17
Third experimental series (GPRS 69 results)
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
1900
MG detected for GPRS 69
(micro segregation only)
T, C | Type | UO2 | FeO | SiO2
1900 | Heavy liquid | 15.02.7 | 22.84.5 | 62.26.6
 | Light liquid | 3.00.8 | 5.21.3 | 91.92.0
200 m
6 m

## Slide 18
18
SEM/EDX for GPRS 72
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
600 m
1950
T, C | Type | UO2 | FeO | SiO2
1950 | Heavy liquid | 10.00.8 | 19.01.0 | 71.01.6
 | Light liquid | 3.50.1 | 7.61.0 | 88.91.1
Tm | Heavy liquid | 15.71.5 | 20.55.6 | 64.27.4
 | Light liquid | 2.60.6 | 4.50.9 | 92.81.2

## Slide 19
19
Forth experimental series (GPRS 79-81, 84)
Test | Content, mol.% |  |  | T, C | Exp. time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS79 | 18.0 | 77.0 | 5.0 | 1100 | 60 | Annealing
 |  |  |  | 2150 | 10 | Melting and slow cooling down
 |  |  |  | 2000 | 10 | Annealing and quenching
GPRS80 | 12.0 | 78.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 2000 | 10 | Melting and slow cooling down
 |  |  |  | 1800 | 10 | Annealing and quenching
GPRS81 | 6.0 | 79.0 | 15.0 | 1100 | 60 | Annealing
 |  |  |  | 2000 | 10 | Melting and slow cooling down
 |  |  |  | 1725 | 10 | Annealing and quenching
GPRS84 | - | 80.0 | 20.0 | 1100 | 60 | Annealing
 |  |  |  | 2100 | 10 | Melting and slow cooling down
 |  |  |  | 1700 | 10 | Annealing and quenching
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
79
80
81
Research objectives: Tm determination, tie lines determination
84

## Slide 20
20
Forth experimental series (GPRS 79-81, 84)
300 m
79
Peculiarities: overheating, slow cooling down, 10 min. exposure, quenching
T= 2000С
T= 2050С
84
300 m
80
900 m
81
300 m
T= 1800С
T= 1725С

## Slide 21
21
SEM/EDX for GPRS 79
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
< Tm
2000
200 m
T, C | Type | UO2 | FeO | SiO2
2000 | Recrystallization | 14.71.3 | 5.50.6 | 79.81.9
 | Light liquid | 6.60.7 | 2.40.6 | 91.11.0
MG detected
for GPRS 79
(nonequilibrium)

## Slide 22
22
SEM/EDX for GPRS 80
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
< Tm
600 m
T, C | Type | UO2 | FeO | SiO2
1800 | Heavy liquid | 39.31.9 | 17.42.5 | 43.23.5
 | Light liquid | 3.90.4 | 3.10.7 | 93.00.7
 | Total | 6.20.6 | 6.00.6 | 87.81.2
MG detected
for GPRS 80
(micro segregation only)

## Slide 23
23
MG in the UO2-SiO2-FeO System
0.2
FeO
0.8
SiO2
Tm=2080 C
Tm=1700 C
~ Tm
1850 > Tm > 1750
2000
1750 > Tm > 1700
~ Tm
1950
2050 > Tm > 1950
~ Tm
1900
2050
1750 > Tm
1850

## Slide 24: Scheme of spinodal decomposition
A
B
T, °C
B
2
3
binodal
spinodal
1
1
2
3
2
3

## Slide 25
25
Conclusions
The miscibility gap in the UO2-FeO-SiO2 system was observed
Monotectic plate is outlined (with accuracy about 100C)
Ten tie lines was constructed
Ten points were settled to be done (three points for MG region) Twenty experiments have been made in only MG region
There is many uncertainties and incomprehensibilities which distort MG observations in this ternary system