## Slide 1: Final report of the UO2-SiO2 system
ISTC PRECOS
Project #3813
A.P. Alexandrov
Research Institute of Technology
Presented by Vyacheslav Almjashev
5th PRECOS Meeting
ETU
Saint-Petersburg

## Slide 2
2
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2070±10
mol.% SiO2
Lungu’s data
mol.% SiO2
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
1200
1000
1400
1600
Lungu, 1973
To spinodal decomposition
in the UO2-SiO2 system

## Slide 3
3
  Miscibility gap – binodal curve and critical point determination
  Liquidus curve from the UO2 side
Research objectives

## Slide 4
Fourth experiment done by IMCC (PRS 8)
81.4 mol.% SiO2
by synthesis
100 m
(sample of melt)
81.0±3.0 mol.% SiO2
100 m
1 mm
80.4 mol.% SiO2
84.0 mol.% SiO2

## Slide 5
Fourth experiment done by IMCC (PRS 8)
81.4 mol.% SiO2
by synthesis
200 m
83.9 mol.% SiO2
1 sm
84.8 mol.% SiO2
1 mm
1 mm
1 mm
90.7 mol.% SiO2
83.5 mol.% SiO2
ingot
ameboid microstructure has the dynamic nature
The new type of instability
T
Instability
edge

## Slide 6
6
Fifth experiment done by IMCC (PRS 9)
Experimental objectives
Determine liquidus temperature at high UO2 content
VPA IMCC: Fragment of the experimental thermogram showing melt surface
Charge composition
mol.%: 75.0 UO2 + 25.0 SiO2
    Tliq was measured three times: 2560oC, 2563oC and 2550oC  Tliq=2558±40oC

## Slide 7
7
15 m
~2560 С
(sample of melt)
20.5±3.3 mol.% SiO2
(ingot nearby crucible)
26.9 mol.% SiO2
80 m
(central zone of ingot)
30.2±0.6 mol.% SiO2
350 m
25 mol.% SiO2
by synthesis
Fifth experiment done by IMCC (PRS 9)
6.9 mol.% SiO2
37.1±0.8 mol.% SiO2

## Slide 8
8
Fourth experimental series (GPRS 14-17)
1 mm
Peculiarities: 10 min. exposure, quenching, T= 2125±25 С
Liquid phase composition measurements
63.2 ±2.9 mol.% SiO2
62.8±1.4 mol.% SiO2
65.0±1.6 mol.% SiO2
68.0±2.0 mol.% SiO2
50 mol.% SiO2
by synthesis
(48.3 by analysis)
60 mol.% SiO2
by synthesis
(55.9 by analysis)
40 mol.% SiO2
by synthesis
(34.6 by analysis)
50 mol.% SiO2
by synthesis
(47.7 by analysis)
the solid phase in all samples at the isotherm 2125C has been found
average liquid phase composition is 64.8±4.4 mol.% SiO2

## Slide 9
9
Fifth experimental series (GPRS 19-22)
Peculiarities: 10 min. exposure, quenching, T= 2200С
50 mol.% SiO2
by synthesis
(50.2±1.3 by analysis)
60 mol.% SiO2
by synthesis
(58.7±1.5 by analysis)
40 mol.% SiO2
by synthesis
(42.9±0.9 by analysis)
50 mol.% SiO2
by synthesis
(50.2±1.9 by analysis)
Liquid phase composition measurements
64.4 mol.% SiO2
63.0±1.9 mol.% SiO2
67.6±1.2 mol.% SiO2
61.1±0.4 mol.% SiO2
the solid phase in all samples at the isotherm 2200C has been found
liquid phase composition is 64.0±3.9 mol.% SiO2

## Slide 10
10
Sixth experimental series (GPRS 23, 24, 26, 28)
Peculiarities: 10 min. exposure, quenching, T= 2300С
Liquid phase composition measurements
Fully melted
62.8±2.2 mol.% SiO2
Fully melted
Fully melted
60 mol.% SiO2
by synthesis
(59.9±0.5 by analysis)
60 mol.% SiO2
by synthesis
(59.7±0.1 by analysis)
50 mol.% SiO2
by synthesis
(49.0±2.2 by analysis)
60 mol.% SiO2
by synthesis
(55.0±0.5 by analysis)

## Slide 11
11
Peculiarities: 10 min. exposure, quenching
81.4 mol.% SiO2 by synthesis
Seventh experimental series (GPRS 18, 25, 27, 32)
2175 С
2160 С
2130 С
2200 С
GPRS18
GPRS25
GPRS27
GPRS32
Above critical point
Below critical point
GCORD4, 81.4 mol.% SiO2
1 min., 2200 С
Above critical point
(80.3±0.3 by analysis)
(80.8 by analysis)
level | mol.% SiO2
top | 82.2±2.9
ameboid | 79.1±0.5
bottom | -
level | mol.% SiO2
top | 82.2±0.6
ameboid | 79.5±0.7
bottom | 72.7±0.4
level | mol.% SiO2
top | 79.2
ameboid | 78.6
bottom | 74.0
(80.8 by analysis)

## Slide 12
2070±10
2070±10
12
UO2-SiO2 phase diagram
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2080
mol.% SiO2
L1 + L2
2080
2000
2200
2400
60
80
PRS1
PRS3
4-S
5-S
GPRS-18
GPRS-25
GPRS-27
GPRS-32
4-S
5-S
GPRS-18
GPRS-25
GPRS-32
GPRS-27
PRS9 nearby crucible
ChA
SEM/EDX
Galakhov

## Slide 13
13
Conclusions
The miscibility gap limits are re-examined. With the accuracy of 15C the miscibility gap critical point was pointed out
The liquidus curve in the observed system was constructed from the UO2 side
Seven points were settled to be done Forty experiments have been made